## Slide 1
Cryogenic operation of
GaAs laser power converters
Bora Kim1,2, Mijung Kim1,2, Brian Li1,2, Ryan Hool2,3, and Minjoo Larry Lee1,2
1Electrical and Computer Engineering, University of Illinois Urbana-Champaign
2Nick Holonyak Micro and Nanotechnology Laboratory, University of Illinois Urbana-Champaign
3Materials Science and Engineering, University of Illinois Urbana-Champaign
1
Acknowledgments

## Slide 2: Outline
w/ high barrier
T=83K
Motivation and background
Cryogenic 1J-GaAs LPC results
  Effect of carrier freeze-out on band diagrams
  Strategies for T-invariant RS
  Improved LPC performance at low-T
  Towards 70% low-T efficiency
  Conclusions
+
EC
EF
EV
p-GaAs
Base
p-InGaP
BSF
High majority hole barrier, T=83K
p+GaAs
Base
EC
EV
EF
p+AlGaAs
BSF
+
Low majority hole barrier, T=83K
w/ high barrier
w/ low barrier+DLARC
T=83K
ID | PIn, density (W/cm2) | FF (%) | Efficiency (%)
High barrier | 0.27 | 74.4 | 39.1
Low barrier | 0.71 | 93.3 | 62.1
ID | PIn, density (W/cm2) | FF (%) | Efficiency (%)
High barrier | 0.27 | 74.4 | 39.1

## Slide 3: Cryogenic power-over-fiber
[1] B. Abi et al., JINST 15, T08008 (2020).
Power-over-fiber (PoF)
  Suitable in harsh environment due to spark-free operation
PoF in deep underground neutrino experiments
  Convey power to electronics embedded in high voltage (V=300kV) and LAr (T=83-89K)
Anode
Cathode (V=−300 kV)
Neutrinos
from
Fermi lab
Liquid Argon (LAr), 83-90K
Readout electronics
PMTs
[1]
Inaccessible environment
Optical fiber
Transmitter unit
Receiver unit
Laser diode
Laser driver
LPC
Electronic
circuits

## Slide 4: LPC material selection
[1] H. Helmers et al., Phys. Status Solidi RRL 15, 2100113 (2021).
GaAs-based LPC
  High efficiency>50%
  Highest efficiency: 68.9%[1] with thin-film, back-surface reflector
GaAs or GaAs/AlGaAs
Single junction
T = 298K
Si
InGaAs
InGaP
GaSb
InGaAsP
w/ thin-film
& back surface reflector

## Slide 5: Laser wavelength (𝜆) selection
Zero transmittance loss in LPCs with Ephoton>Eg
Ephoton<Eg
Transmittance loss
Conduction band
EV
EC
Eg
Ephoton
Valence band
+

## Slide 6: Laser wavelength (𝜆) selection
[1] M. D. Sturge et al., Phys. Rev. 129, 2835 (1963).
[2] O. D. Miller et al., IEEE J. Photovolt. 2, 303-311 (2012). [3]. F. Urbach, Phys. Rev. 92, 1324 (1953).
Ephoton>Eg
Thermalization loss
Incomplete absorption loss
Conduction band
EV
EC
+
Eg
Ephoton
Valence band
827
816
805
795
0.6
0.8
1.0
1.2
x104
Wavelength (nm)
𝛼 (cm-1)
GaAs, 90K
[1]
-
-
+
Lattice heat
T=83K-90K
Absorber thickness=2.08 um
Thermalization loss
Zero transmittance loss in LPCs
Trade-off between thermalization and incomplete absorption losses
  Coupled with 808 nm laser
Thermalization loss
Incomplete absorption loss [1-3]
Minimal 𝛴loss
808 nm

## Slide 7: Effect of operating temperature
[1] R. Hoheisel et al., IEEE J. Photovolt. 2, 398-402 (2012).
In theory,
  T ↓  𝜂 ↑ (JSC ↓, VOC ↑, FF ↑)
  Radiative limit efficiency increased from 69.8% (298K) to 80.8% (83K)
  In practice, FF can decrease at low-T
Simulation conditions
Absorber thickness=2.08 um
𝜆=808 nm
Power density=0.7W/cm2
298K
T↓  JSC ↓
T↓  VOC ↑
298K
83K
T (K) | JSC (A/cm2) | VOC (V) | FF (%) | η (%)
298 | 0.434 | 1.248 | 90.1 | 69.8
83 | 0.403 | 1.449 | 96.9 | 80.8
VOC
Theoretical IV
Experimental IV
[1]
0
1.0
0.8
1.2
1.4
0
10
20
30
Current density (mA/cm2)
Voltage (V)
GaAs solar cell
163K
123K
100K
80K
RS ↑ as T ↓
 FF ↓
JSC
High RS

## Slide 8: Effect of RS on IV characteristics
[1] C. Algora et al., Joule, 6, 340-368 (2022). [2] M. D. Sturge et al., Phys. Rev. 129, 2835 (1963).
[3] O. D. Miller et al., IEEE J. Photovolt. 2, 303-311 (2012). [4]. F. Urbach, Phys. Rev. 92, 1324 (1953).
RS: Induce voltage drop itself and dissipate power as heat
FF ↓ as RS ↑
Impact of RS significantly ↑ as light intensity ↑
J
V
JL
h𝜈
RSH
RS
Jd
Low RS
High RS
Increasing RS
 FF ↓
Low RS
High RS
Low Illumination
High Illumination

## Slide 9: LPCs growth and characterization
[1] S. Lu et al., Nanoscale Res. Lett. 6, 576 (2011). [2] S. T. Hwang et al., Sol. Energy Mater. Sol. Cells, 155, 264-272 (2016).
Solid-source molecular beam epitaxy (MBE)
  Sources: Al, Ga, In, As, P
  Dopants: Si, Be
  TSub: 460˚C-610˚C

## Slide 10: LPCs growth and characterization
[1] S. Lu et al., Nanoscale Res. Lett. 6, 576 (2011). [2] S. T. Hwang et al., Sol. Energy Mater. Sol. Cells, 155, 264-272 (2016).
Solid-source MBE growth
  Sources: Al, Ga, In, As, P
  Dopants: Si, Be
  TSub: 460˚C-610˚C
  DLARC only on structure C
p-GaAs Substrate
Buffer (7e18) p-GaAs 200 nm
BSF (1e18) p-InGaP 50 nm
Base (1e17) p-GaAs 2 um
Emitter (1e18) n-GaAs 50 nm
Window (1e18) n-AlInP 20 nm
Base (2e18) p-GaAs 50 nm
Contact (6e18) n-GaAs 250 nm
Structure A
Typical solar cell design[1-2]
p-InGaP; 98% Be deactivation
p-GaAs Substrate
Buffer (3e18) p-GaAs 400 nm
BSF (0.1~3e18) p-GaAs 100 nm
Base (1e17) p-GaAs 1 um
Emitter (3e18) n-GaAs 80 nm
Contact (6e18) n-GaAs 20 nm
Structure B
Control cell
No heterointerface blocking
Emitter (1e18) n-GaAs 80 nm
p-GaAs Substrate
Buffer (7e18) p-GaAs 400 nm
Base (1e17) p-GaAs 2 um
Window (8e18) n-InGaP 500 nm
BSF (0.1~7e18) p-GaAs 100 nm
BSF (6e18) p-AlGaAs 100 nm
Contact (6e18) n-GaAs 250 nm
Structure C
Low RS targeted at 83K
p-Al0.1GaAs; minimal deact.
Sliver sample stage
Electrical tester
LN2
N2
LN2
sample stage
Vacuum
P<1e-5 Torr
Electrical tester
T-dependent characterizations
  EQE, DIV, 808nm-IV, TLM
  with two types of cryostats
    T range=83K-298K

## Slide 11: Structure A : T-dependent RS analysis
Dark diode Structure A
Structure A
  Increasing RS with decreasing T
  No change in ∑Rbulk or RC
  Thus, RInt is main cause
RInt
RC
𝛴RBulk
 | 83K | 298K
RS | 1.17e-1 | 2.88e-2
𝛴RBulk | 5.78e-4 | 6.98e-4
RC | 1.06e-4 | 8.94e-5
Rint (estimated) | 1.16e-1 | 2.80e-2
Substrate p+-GaAs
Buffer p+-GaAs
BSF p-InGaP
Base p-GaAs
Emitter n-GaAs
Window n-AlInP
Base p-GaAs
Contact n+-GaAs
Ti/Au
Cr/Au
RS
83K
298K
1
RC
RBulk
RInt
Chart: R (𝛺∙cm2)
| 83K | 298K
𝛴Rbulk | 0.000578 | 0.000698
RC | 0.000106 | 8.94e-05
Rint | 0.116 | 0.028
100
10-1
10-2
10-3
10-4
83K
298K
RS
Chart: R (𝛺∙cm2)
| 83K | 298K
𝛴Rbulk | 0.000578 | 0.000698
RC | 0.000106 | 8.94e-05
Rint | 0.116 | 0.028
100
10-1
10-2
10-3
10-4
83K
298K
RS
 | 83K | 298K
RS | 1.17e-1 | 2.88e-2
𝛴RBulk | 5.78e-4 | 6.98e-4
RC | 1.06e-4 | 8.94e-5

## Slide 12: Structure A : T-dependent band diagram analysis
Severe carrier deactivation in p-type
Moderately doped p-InGaP shows 98% carrier deactivation
Structure A
  High majority carrier blocking at p-GaAs/p-InGaP heterointerface
    Due to partial carrier freeze-out in p-InGaP BSF layer
298K
77K
298K
77K
InGaP
298K
p-GaAs Base
p-InGaP
BSF
+
EF
EC
EV
p-GaAs Substrate
Buffer (7e18) p-GaAs
BSF (1e18) p-InGaP
Base (1e17) p-GaAs
Emitter (1e18) n-GaAs
Window (1e18) n-AlInP
Base (2e18) p-GaAs
Contact (6e18) n-GaAs
Structure A
83K
EC
EF
EV
+
Thicker tunneling barrier
Tunneling-dominated

## Slide 13: Structure B & C : T-dependent band diagram analysis
Structure B
  No majority/minority blocking
Structure C
  No majority blocking
  Sufficient minority blocking
p-GaAs Base
p+GaAs BSF
+
298K
EF
EC
EV
+
83K
EF
EC
EV
p+GaAs BSF
p+AlGaAs BSF
298K
+
p-GaAs Base
+
EF
EC
EV
83K
p-GaAs Substrate
Buffer (3e18) p-GaAs
BSF (0.1~3e18) p-GaAs
Base (1e17) p-GaAs
Emitter (3e18) n-GaAs
Contact (6e18) n-GaAs
Structure B
Control cell
No heterointerface blocking
Emitter (1e18) n-GaAs
p-GaAs Substrate
Buffer (7e18) p-GaAs
Base (1e17) p-GaAs
Window (8e18) n-InGaP
BSF (0.1~7e18) p-GaAs
BSF (6e18) p-AlGaAs
Contact (6e18) n-GaAs
Structure C
Low RS targeted at 83K
p-Al0.1GaAs; minimal deact.

## Slide 14: T-dependent RS analysis
298K
83K
High
RS
Structure A
Structure B
Structure C
Structure A
Structure B
Structure C
  Structure B and C
    T-invariant RS
      At 83K, 10-14x smaller than that of structure A
Structure A
  Increasing RS with decreasing T
  No change in ∑Rbulk or RC
  Thus, RInt is main cause

## Slide 15: QE comparison
298K
Structure A
Structure B
Structure C
808 nm
92.6%
74.0%
91.3%
83K
298K
Structure C+DLARC
Structure A
Structure B
808 nm
76.6%
62.2%
43.3%
At 298K, IQE808 nm of structure A ≈ structure C >> structure B
At 83K, decrease in EQE808 nm due to
  Decrease in minority carrier diffusion length
  Decrease in absorption coefficient at 808nm
  EQE808 nm~76.6% in structure C+DLARC

## Slide 16: 808-IV comparison
FF decreases in structure A with increasing power density due to high RS
  FF in structure C > FF in structure B
Structure A
Structure B
Structure C + DLARC
T=83K
Structure A
Structure B
Structure C + DLARC
    Peak 𝜂 of 62.1% in structure C under power density of 0.7W/cm2

## Slide 17: Roadmap to 70% LT efficiency
Need to improve EQE (JSC)
T=83K Absorber thickness=2.08 um Power density=0.7 W/cm2 | EQE808 nm (%) | VOC (V) | FF | 𝜂 (%)
Radiative limit | 88.3 | 1.45 | 0.969 | 80.8
Structure C | 76.6 | 1.40 | 0.933 | 62.1
Fraction of radiative limit | 0.867 | 0.966 | 0.963 | 0.769
T=83K Absorber thickness=2.08 um Power density=0.7 W/cm2 | EQE808 nm (%) | VOC (V) | FF | 
Radiative limit | 88.3 | 1.45 | 0.969 | 80.8
Structure C | 76.6 | 1.40 | 0.933 | 62.1
Fraction of radiative limit | 0.867 | 0.966 | 0.963 | 0.769
  Strategy: increase absorption of photons
    DBR, back surface mirror
+
-
Incomplete absorption
Light
Absorption
GaAs absorber
GaAs substrate
+
-
Radiative recombination
photon
GaAs absorber
GaAs substrate

## Slide 18: Roadmap to 70% LT efficiency – (1) DBR
Need to improve EQE (JSC)
86.0% EQE808 nm with DBR
  73.2% 𝜂 expected
  Strategy: increase absorption of photons
    DBR, back surface mirror
  However, high RS and low FF due to carrier deactivation
  Other DBR structures under investigation
GaAs absorber
GaAs substrate
Reflection
DBR
83K
298K
808 nm
w/o DBR
w DBR
76.6%
86.0%
w DBR
w/o DBR
808 nm
95%
+
-

## Slide 19: Roadmap to 70% LT efficiency – (2) BSR
Need to improve EQE (JSC)
Additional advantage
  Photon recycling
  Strategy: increase absorption of photons
    DBR, back surface mirror
  However, low yield and high RS due to non-optimized fabrication techniques
+
-
GaAs absorber
Back surface reflector/metal contact
Reflection
Total internal reflection
Escape cone
+
-
Reabsorption
Inverted epilayers
GaAs substrate
(a) MBE-grown inverted epilayers
Back contact
Inverted epilayers
GaAs substrate
(b) Back contact metallization
Back contact
Inverted epilayers
GaAs substrate
Handle wafer (Si)
Back contact
Inverted epilayers
Back contact
Back contact
(d) Etch GaAs substrate
Handle wafer (Si)
Epilayers
Back contact
Handle wafer (Si)
Back contact
(e) 2 step Photolithography
(c) Metal-metal bonding by thermo-compression

## Slide 20: Conclusion
Majority hole blocking acted as a strong performance-limiting factor in cryogenic LPCs
By selecting proper barrier material with high doping and minimal freezeout
  FF>90% and peak efficiency of 62.1% were measured
ID | EQE808 nm (%) | PIn, density (W/cm2) | JSC (A/cm2) | VOC (V) | FF (%) | ηMax (%)
A | 62.2 | 0.27 | 0.102 | 1.385 | 74.4 | 39.1
B | 43.3 | 1.05 | 0.282 | 1.387 | 89.2 | 33.2
C | 76.6 | 0.71 | 0.339 | 1.400 | 93.3 | 62.1
Structure A
Structure B
Structure C + DLARC