## Slide 1: LQXFA/B01 Horizontal Test Status and Preliminary Results
Guram Chlachidze
Jun. 6, 2023

## Slide 2: LQXFA/B01 Test Status
MQXFA03 (B)
MQXFA04 (A)
Lead End

## Slide 3: Initial Electrical Checkouts
Cryo-assembly was received at the test facility with one open heater (YT223 in MQXFA03) and one open voltage tap EE152
Room temperature insulation (Hipot) tests: no failures
  Coil-to-structure at 2.5 kV for Top plate leads (3) w/o magnet
  Coil-to-ground at 368 V
  Quench heater-to-coil at 460 V

## Slide 4: LQXFA/B01 controlled cooldown
19 days of cooldown: Mar 15 - Apr 3
  About 5 days of downtime due to various issues
  First week running with the 50 K temperature difference requirement
  GHe mass flow rate varied from 5 g/s to 18 g/s
Platinum RTDs 505/506 are installed on the CM end plates

## Slide 5: LQXFA/B01 Controlled cooldown (2)
ΔT requirement between the GHe supply and the CM RE changed from 50 K to 80 K
  Delta T (meas) - difference between the temperature readings of the RTD sensors 505/506 located on the cold mass end plates
  Delta T (calc) is based on the magnet resistance measurements

## Slide 6: Cold Electrical Checkouts
Coil-to-ground at 1840 V
Quench heater-to-coil Hipot at 2300 V
MQXFA03: YT213A/B heater failed the Hipot test around 2190 V
No dead short to coil or ground, small current leakage at 200 V
Currently using dummy load instead of YT213

## Slide 7: Preliminary Test Results
Preliminary TC1 results were released on May 8th
  Manual trips at 1000 A and 6000 A
  Ramp 1: Cu/SC leads in the feed box tripped at 15387 A (no quench origin in magnets)
    Due to low LHe level above Lambda-plate
  Ramp 2: SC leads trip at 16388 A (no quench origin in magnets)
    Motion related voltage spike in SC leads
  Ramp 3: Holding 16530 A for 30 min
  Ramp 4: High ramp rate test. 5 min at 16230 A, ramp up/down 30 A/s
  Ramp 5: Endurance test at 16530 A: trip after 32 min at flattop (no quench origin in magnets)
    Dump switch voltage dropped below the limit and initiated slow ramp down
  Ramp 6: Ramp to 16530 A. Quench at 16386 A
    Quench in MQXFA04 negative half-coil, coil 113 (Q2) or 206 (Q3)
  Ramp 7: Repeated test: Holding 16530 A for 30 min
  Ramp 8: Repeated High ramp rate test: 5 min at 16230 A, ramp up/down 30 A/s
  Ramp 9: Endurance test at 16530 A: trip after 85 min at flattop (no quench origin in magnets)
    Due to sudden drop of LHe level above Lambda-plate
  Ramp 10: Demonstrating level of training: 5 min at 16530 A
  Ramp 11: Temperature dependence study at 4.2 K: 30 min at 16230 A
  Next step: Thermal cycle

## Slide 8: LQXFA/B01 Quench Performance in TC1
High ramp rate tests only at 30 A/s. To be repeated in TC2
Two attempts of the endurance (holding current) test
  First trip at Inom+300 A=16530 A caused a minor detraining
  85 min is the longest run. In total Inom+300 A was held for 3+ hours

## Slide 9: Preliminary Test Results (2)
Only one spontaneous quench in magnets
  Quench at 16386 A, in MQXFA04 (Magnet A), coil 113 (P2)
  Quench Integral ~27 MIITs (no external energy extraction)
(P2+P3) - (P1+P4)
P2

## Slide 10: Splice measurements
Two additional splices were made in LQXFA/B01 to add extra length for testing at Fermilab (and CERN)
  Lead length w/o the additional splice is sufficient for the tunnel installation at CERN
Additional splices
in LQXFA/B01

## Slide 11: Splice measurements (2)
Splice measurements were made at 1.9 K for currents up to 5 kA
  8-channel MUX system based on Keithley 2182A Nanovolt Meter
Two-splice segments are measured ~0.7±0.1 nΩ, and single splice
segments - less than 0.3±0.1 nΩ
More measurements at higher
currents are possible

## Slide 12: Warmup and cooldown for TC2
Controlled warmup from May 8 to 16
  No cooldown since May 26
Cernox RTDs TE821/822 installed in the CM shell openings

## Slide 13: Cooldown in TC1 and TC2
First cooldown used for optimizing the controlled cooldown parameters
  Two weeks are expected for 1.9 K cooldown. Further improvement requires upgrade of the heat exchanger in the Helium return line
Cernox RTDs TE821/822

## Slide 14: Next Steps
Currently replacement of the relief valve in progress
  Magnets are floating at around 85 K
Complete cooldown to 1.9 K and continue test according to the Run Plan
  Electrical checkouts
  Endurance (holding current) Test
  High ramp rate test
  Repeat the temperature dependence test
  Magnetic measurements

## Slide 15: Backup Slides

## Slide 16: LQXFA/B01 Test Status (2)
On Apr. 6, LQXFA/B01 was cooled down to 1.9 K
Test Stand overview screen