## Slide 1
Status Update – Jun, 2023

## Slide 2: SSR2 Cavity
Cavity Component Forming
  Nb Material supplied to the vendor
  Expected to start forming from next week
EBW Trials
  Trials completed; Acceptable parameters achieved for all weld types
  WPS, PQR completed for 3.2 mm Nb-Nb, 4.0 mm Nb-Nb, 4.7mm Nb-Nb, 4.0 mm Nb-Ti Grade 2, 13mm Nb-Ti Grade 5
Nb Components
  Machining Completed
  Seam Weld u/p
Weld Fixture scheme and Drawing completed

## Slide 3: SSR2 Tuner
Procurement of Standard Components
  Bellows received at BARC
  Machining of G10 components under progress
Manufacturing under progress
  75% of all components completed.