## Slide 1
The use of high purity aluminum for conduction cooling of SRF cavities
Ram C. Dhuley on behalf of Fermilab’s conduction-cooled SRF project team
2023 TTC Meeting at Fermilab
07 December 2023

## Slide 2
Fermilab’s conduction-cooled SRF program is built on the
use of high purity aluminum thermal links
*R.D. Kephart is also the founding member of Fermilab’s conduction cooled SRF program
High purity Al thermal conductivity, Al-Al and Al-Nb contact resistance near 4 K
4 K cryocooler
4 mm thick
Al plate
Data available at:
R.C. Dhuley, et al. (2018)
https://doi.org/10.1016/j.cryogenics.2018.06.003
Courtesy : Dr. Oleg Prokofiev (Fermilab)
Minemura, Kephart*, et al. (1985) https://doi.org/10.1016/0168-9002(85)91023-X
Superconductor for Fermilab’s CDF solenoid

## Slide 3
Fermilab’s conduction-cooled SRF program is built on the
use of high purity aluminum thermal links
Comparison of measured and simulated link thermal conductance
Al conduction link bolted to the
Nb rings welded to the cavity
Nb3Sn cavity
Computed cavity surface temperature at steady state with ~10 MV/m cw
Ring temperature = 5.95 K,
RF dissipation = 2.4 W
ΔTspatial ~0.12 K
Courtesy : Dr. Roman Kostin (Euclid Techlabs, LLC.)
R.C. Dhuley et al 2022 IOP Conf. Ser.: Mater. Sci. Eng. 1240 012147