## Slide 1: Introduction to Hot-Topic discussion
TESLA Technology Collaboration Meeting
Fermilab, Batavia, IL
4-8 December 2023
Gianluigi Ciovati

## Slide 2: Conduction-Cooled SRF Cavities
Why conduction-cooled SRF cavities?
  Eliminate the need for liquid He cryoplants for SRF accelerators, thereby:
    Reducing footprint
    Reducing capital cost
    Simplifying cryomodule design
    Safer to operate
    Enabling industrial applications
Does conduction cooling of SRF cavities work?
  Use high-quality Nb3Sn thin films
  Use commercial cryocoolers with high cooling power at 4 K
  Single-cell cavities with frequency in the range 0.65 – 2.6 GHz cooled by cryocoolers have been tested up to an accelerating gradient of 10-12 MV/m

## Slide 3: Challenges for Conduction-Cooled SRF Cavities
Choice of cryocooler
  GM, PT, GM-JT
Thermal link design
  Cu, Al, foils, straps, bulk
Nb3Sn thin-film performance
  On Nb: thermal diffusion, magnetron sputtering, electroplating
  On Cu: CVD, PVD, magnetron sputtering, bronze route
Tunability of Nb3Sn-coated cavities
  Warm, cold
Low-loss fundamental power coupler
Thermoelectric magnetic flux
Cryocoolers

## Slide 4: Choice of cryocoolers
7.5 kW for 2 W at 4 K
~$45k
Limited mechanical loading to cold stage
Vibrations at 1.2 Hz
GM-type
PT-type
GM-JT-type
12.5 kW for 2 W at 4 K
~$60k
No moving parts
14.1 kW for 9 W at 4 K
Fixed temperature
Limited mechanical loading to cold stage
Requires separate shield cooler

## Slide 5: Thermal link design
99.9% purity Cu foils
Flexible connection
Apiezon N grease used at interfaces
Cu foils with press-welded terminals
Aluminum bus-bars
Cu thermal braids + Cu clamps
99.9999% purity Al bars
“rigid” connection
Indium foil used at interfaces
Time-consuming assembly
Braided Cu straps
Flexible connection
Indium foil used at interfaces
High clamping force (required for low thermal resistance) can damage the brittle Nb3Sn film

## Slide 6: Nb3Sn thin-film performance
How do we achieve this type of performance reproducibly?
Is Ti contamination of the film from the Ti45Nb flanges as issue?
How do we achieve this type of performance on Cu?
State-of-the-art performance of Nb3Sn thin-film on Nb by vapor diffusion in liquid He:
1.3 GHz single-cell
650 MHz single-cell

## Slide 7: Tunability
How to overcome the brittleness of Nb3Sn?
What is the maximum tuning range at 300 K before degrading performance?
-330 kHz at RT
-3.2 MHz at RT
1.3 GHz single-cell
952 MHz single-cell