## Slide 1: Nb3Sn on Cu:
Different technologies under study:
PVD
  Magnetron Sputtering
    Single Target
    Double Target
  HiPIMS
CVD
Electroplating
Bronze Route
Cheaper than Nb
Higher thermal conductivity
Higher mechanical stability
PVD technology (Nb on Cu) already used for: LEP, LHC, HIE-ISOLDE @ CERN ALPI @ INFN LNL
Motivations for Cu substrate

## Slide 2: Nb3Sn on Cu by PVD
A15 are Brittle materials
Complicated Phase Diagram
Substrate preparation
Low melting point substrate
Interface diffusion
Target Production
Multiple Challenges
Single Target configuration easier to scale into cavities
@ CERN and JLab HiPIMS to densify coating
R&D is Focused on Coating Parameter Optimization to get the right phase at lowest Working T possible
No RF test yet on cavities available
Only a couple of preliminary tests on QPR @CERN
Strategies
Nb Buffer Layer Thickness (μm)
0
1
9
30
50
Tc > 17 K @600 C
@ STFC DCMS-HiPIMS comparision
@ INFN thick Nb buffer layer (barrier and accommodation effect) improve dramatically Tc