## Slide 1
Genfa Wu, Alex Netepenko, Vijay Chouhan, Akshay Murthy
TESLA Technology Collaboration Meeting
5-8 December 2023
Exploring Mode Mixing in PIP-II LB650 Cavities: Impact of 350C Furnace Baking on its Reduction post-HPR and Vertical Tests

## Slide 2: Outline
Mode mixing introduction
300 - 350C Furnace Baking and mode mixing reduction
Sample analysis
Summary

## Slide 3: LB650 Cavity mode mixing introduction

## Slide 4: Mode mixing in PIP-II LB650 cavities
Mode excitation
Mode suppression

## Slide 5: Mode mixing in 1.3 GHz 9-cell cavities
V. Volkov, J. Knobloch, and A. Matveenko, “Monopole passband excitation by field emitters in 9-cell TESLA-type cavities”, Phys. Rev. Spec. Top. Accel Beams, vol. 13, no. 8, 2010
Mode mixing may be caused by electron activities.
The electrons work like those in a klystron.
Pi-mode
7Pi/9-mode
Field emitted electrons gaining up to 830 keV

## Slide 6: Mode mixing in LB650 5-cell cavities
1 pi/5 | 644.071 MHz
2 pi/5 | 645.775 MHz
3 pi/5 | 647.754 MHz
4 pi/5 | 649.380 MHz
5 pi/5 | 649.962 MHz
Passband frequencies
Major processing | Mode mixing
EP only | Yes
EP + 120C | Yes
900C, 800C N2/0 | Yes
900C, 300C | Yes
800C, 350C | No
900C, 350C | No
FNAL: Five cavities, 12 vertical tests.
All experienced mode mixing with 4pi/5 mode
During the mode mixing event, no MP and no X-ray were detected above background.
Starts 7-8 MV/m or 15 MV/m
INFN: The prototype cavity also experienced mode mixing with 4pi/5 mode.

## Slide 7: LB650 cavity multipacting simulation
Chart: Emission current vs acc. gradient
| 5.7275855385023462 | 7.636780718003128 | 8.5913783077535193 | 9.5459758975039097 | 10.500573487254302 | 11.455171077004692 | 12.409768666755081 | 13.364366256505475 | 14.318963846255867 | 15.273561436006256 | 16.228159025756646 | 17.182756615507039 | 18.137354205257427 | 19.091951795007819 | 20.046549384758212 | 21.001146974508604 | 21.955744564258993 | 23.864939743759777
b06 INFN | 0 | 4.8716e-06 | 0.15403 | 0.88567 | 1.215 | 1.3317 | 1.3054 | 1.1719 | 0.99813 | 0.80525 | 0.62598 | 0.46926 | 0.30502 | 0.14886 | 0.05163 | 0.011795 | 0.0020589 | 0
b06 FNAL | 0 | 0 | 0.0075833 | 1.0003 | 1.5101 | 1.6945 | 1.6808 | 1.5263 | 1.3132 | 1.0481 | 0.78406 | 0.53512 | 0.30144 | 0.12763 | 0.053293 | 0.017262 | 0.0018635 | 0 | 0
b09 FNAL | 0 | 0 | 0.010113 | 0.17256 | 0.23708 | 1.301 | 1.7942 | 2.0292 | 2.0906 | 2.0199 | 1.8631 | 1.6483 | 1.4149 | 1.186 | 0.95703 | 0.74689 | 0.54103 | 0.33399 | 0.16864 | 0.074084 | 0.032655
 | 0 | 2.3
 | 0 | 2.3
 | 0 | 2.3
 | 0 | 2.3
 | 0 | 2.3
 | 0 | 2.3
CST simulation by G. Romanov
FishPact simulation by Z. Ninan
Predicted MP band : 7 – 14 MV/m
Measured mode mixing : from 8 (15) MV/m all the way to quench

## Slide 8: Furnace baking and mode mixing reduction

## Slide 9: Medium temperature furnace baking
B61C-EZ-102
B61C-EZ-101
300C
350C

## Slide 10: LB650 Cavity Performance Summary EP only and mid-T Furnace Baking
Each cavity has its own color
Diamond: mid-T baked
Round: EP only

## Slide 11: Mode mixing in PIP-II LB650 cavities
Cavity | Major processing | Mode mixing
B61C-EZ-101 | 800C, 350C | No
B61C-EZ-104 | 800C, 350C | No
B61C-EZ-104 | 900C, 350C | No
B61C-EZ-101 | 900C, 350C | Yes*
*cavity was shelved for four weeks, compared to routine test 1-week after evacuation
Fermilab vertical test has no active pumping.

## Slide 12: Sample Analysis

## Slide 13: SIMS analysis of witness samples (Preliminary)
21_EP
L39-2_300C/3hrs
0101_350C/3hrs
Correlation with MP/Mode-mixing inconclusive
Mode mixing present
High H concentration
Mode mixing present
High H concentration
Thinner but high O concentration
Mode mixing absent

## Slide 14: Summary
Mode mixing has been observed in almost all LB650 cavity tests except some 350C baked cavities.
Predicted MP band has no MP signature but coincided with some of the mode mixing power level.
  There is no explanation when the Eacc is higher than the MP band.
Surface elements of the witness sample is inconclusive.
SEY measurement may be useful. (Future work)

## Slide 15
THE FUTURE OF FERMILAB
Follow us:
http://pip2.fnal.gov/
/showcase/pip-ii/
Thanks for the attention!
Questions?