## Slide 1: Interstitial oxygen tailoring by various surface treatments and how it impacts Q0
Rezvan Ghanbari, Marc Wenskat – on behalf of the UHH SRF R&D Team

## Slide 2
Nb 3d core level
Arbitrary unit
200
204
208
212
Binding energy
X-Ray Photoelectron Spectroscopy (XPS)
Reference
0 HPR cycle
Standard recipe
6 HPR cycles
18 HPR cycles
~ 6.9
~ 7.2
~ 7.6
Extensive HPR → thicker Nb2O5 → more O for mid-T
90%
87%
82%
12%
6%
8%
5%
5%
4%
[Ghanbari, R. TTC Workshop 2022, Aomori]

## Slide 3
18x HPR is not beneficial for Q0
2K

## Slide 4
Different treatments – same rf behaviour
2K

## Slide 5
It‘s not the cavity!
20µm EP between black and red
40µm EP between red and blue
2K

## Slide 6
Dip is deeper for 18xHPR – Δftot similar
T(fmin) ≈ 9.04K
T(End) ≈ 8.9K
Cavity | Treatment | Δfdip/kHz
1DE19 | 4.5h @ 335°C | 1.1
1AC02 | 3.25h @ 335°C | 1.4
1RI04 | 3h @ 250°C | 0.9
1DE07 | 20h @ 250°C | 2.0
1DE79 | 18xHPR + 3h @ 300°C | 3.9

## Slide 7
What information is encoded in f vs. T?
T
Tc
j
Skin depth
Frequency shift is sensitive to interstitial concentration
(equation valid for dirty limit)
Δftot for EXFEL type cavities is typcially 5-6 kHz
Mid-T: more interstitials → larger Δf, but yet no dip

## Slide 8
Microscopic model for disordered superconductor
An increased oxygen concentration reduces Tc of Nb by 0.93K per 1 at.%
- to have a dip minimum at 9.1K we would need ≈ 0.2 at.%
    - „end of dip“ around 8.9K ≈ 0.3 at.%
Solubility limit of O in Nb is 1 at.% @ 500°C and 0.33 at.% at 145°C
We have shown that C diffusion speed in Nb along GB vary with GB orientation, increasing disorder by spatially varying concentration
→ Assume same is true for O: not homogenous distributed within the rf layer, but clusters with uneven O-concentration
→ Expect non-constant (gaussian shaped) Tc reduction
→ Lowest Tc equal to the max. at.% concentration at RT (≈ 0.33 at.%)
→ Only locally saturated – not globally. If SIMS spot size ≈ multiple grains, obtained cO below saturation limit
[Desorbo, W. Phys. Rev. 132 (1963): 107.]
[Kolchin, O.P., et al. Soviet Atomic Energy 45 (4) (1978): p999.]
[Benvenuti, C., et al. 10th SRF (2001): p441.]
[Dangwal Pandey, A., et al. Appl. Phys. Lett. 119(2021): 194102]
Notes: 1nm Nb2O5 can easily saturate several hundred nm of Nb!

## Slide 9
Disordered superconductor show dip
[Barra, M., et al. SUST 18.3 (2005): 271.]
T
Tc,Nb
j
Skin depth
Mathematically speaking, the geomtery constant Γ is not constant
Dip properties cluster distribution causing current redistribution
Observed: Q vs. T still increases at 9.27K
→ Dip caused by clusters and not homogenous O-enriched Nb-layer
Tc < Tc,Nb
Tc < Tc,Nb
<Tc>

## Slide 10
If it acts the same – is it the same?
≈ saturation concentration
20h@250C
18HPR+3h@300C
3h@300C
@2K
near Tc
Too high NSF cO is not good for Q0
Notes: From N_black = N_red which is simply particle conservation, we can predict an anticorrelation between df_tot and df_dip * dT which is what we observe

## Slide 11
… but in different furnaces! is 642nm vs. 773nm
Since both cavities are coated, no Nb-oxide regrowth
Annealed 1DE10 a second time to diffuse more O away from SF w/o source on top
  → Q0 improved
3h@300°C ≠ 3h@300°C
T / °C
t /h
= „thermal budget“
2K
1DE18 and 1DE10 performed similar before and after coating
Coating was done with same parameters
Both cavities underwent 3h@300°C …
Too high NSF cO is not good for Q0
[Wenskat, M., et al SRF2023 TUIBA02.]
[Wenskat, M., et al Supercond. Sci. Technol. 36 (2023) 015010 (11pp).]

## Slide 12
Diffuse O out of RF layer
→ HFQS reappears and Δftot / Δfdip decreases again
High thermal budget → HFQS reappears
2K
Cavity | Treatment | Δftot/kHz | Δfdip/kHz
1DE19 | 4.5h @ 335°C | 11.7 | 1.1
1AC02 | 3.25h @ 335°C | 12.3 | 1.4
1RI04 | 3h @ 250°C | 18.4 | 0.9
1DE12 | 3h @350°C | 8.3 | 0.52
3h@350°C

## Slide 13
Is there an optimal O-concentration?
Too high NSF cO is not good for Q0 (1DE7 / 1DE10)
Too low NSF cO causes HFQS again (1DE12 / 800°C reset)
Is there a sweet spot?
Need a substitute: assuming Δftot depends on cO …
… look for correlation between Q0 and Δftot
Q0,max @ 2K
Δf = f(7K) – f(T>Tc)
Problematic
Deconvolution

## Slide 14
Correlation with thermal budget?
Assumed Δf is depends cO …
and we know that NSF cO goes down with larger thermal budget / larger …
some correlation of Q0 with expected as well – yet weaker as Fick‘s law does not accomodate uneven GB diffusion / saturation effects
2655 nm
1248 nm
865 nm
773 nm
641 nm
560 nm
537 nm
528 nm
512 nm
234 nm

## Slide 15
Conclusion
Too high cO near the surface is not good
        - 18xHPR before midT of 1DE7
  - 1xmidT vs. 2xmidT of 1DE10
Too low cO leads to HFQS again
  - 1DE12 or every 800°C reset
Optimal recipe depends on furnace – „thermal budget“
  - 1DE10 vs. 1DE18
Sweet spot for Q0 seems to exist – right amount of disorder ?
    - continue investigation & model building (Δftot vs. Δfdip, Eacc, grain mapping)

## Slide 16
Thanks…
Questions?
Contact:
Rezvan Ghanbari
Universität Hamburg
Institute of Experimental Physics
E-Mail: rezvan.ghanbari@desy.de
to DESY for the cavity measurements
to you for listening
to the conveners for the opportunity to present this work

## Slide 17: Back Up

## Slide 18
Current Redistribution
[Checchin, M. et al., Appl. Phys. Lett. 117, 032601 (2020)]
[Pambianchi, M. et al., Phys. Rev. B 50, 13659]
Consequence:
Currents shifted away from the surface where “lossy mechanism(s)” occur

## Slide 19
Frequency shift is frequency dependent
Qn = n x 433MHz
Lower frequency fop → lower Δftot
That is because Γ is frequency dependent
If the dip is caused by current redistribution → Δfdip should depend on fop as well