## Slide 1
Katrina Howard, Daniel Bafia, Young-Kee Kim
TTC2023 at Fermilab
5 December 2023
Update on Analysis of Low RRR SRF Cavities

## Slide 2: Continuation of Low RRR Studies
Many SRF studies follow a “clean bulk dirty surface” technique to optimize the BCS resistance by adding extrinsic impurities
  Low temperature bake and N-doping are current focus
What role do intrinsic impurities serve?
  Might perform similar functions as extrinsic impurities which have been shown to improve performance
Goal: use understanding of intrinsic impurities to design future surface treatments for high gradient and quality factor
  Taking new avenue by studying low RRR cavities
  Low purity Nb  increased concentration of intrinsic impurities
  Taking a deep dive in characterizing performance with TMAP

## Slide 3: Continuation of Low RRR Studies
Many SRF studies follow a “clean bulk dirty surface” technique to optimize the BCS resistance by adding extrinsic impurities
  Low temperature bake and N-doping are current focus
What role do intrinsic impurities serve?
  Might perform similar functions as extrinsic impurities which have been shown to improve performance
Goal: use understanding of intrinsic impurities to design future surface treatments for high gradient and quality factor
  Taking new avenue by studying low RRR cavities
  Low purity Nb  increased concentration of intrinsic impurities
  Taking a deep dive in characterizing performance with TMAP
Surface treatments appear to vary cavity performance, but slightly differently when compared to high RRR cavities

## Slide 4: Continuation of Low RRR Studies
Many SRF studies follow a “clean bulk dirty surface” technique to optimize the BCS resistance by adding extrinsic impurities
  Low temperature bake and N-doping are current focus
What role do intrinsic impurities serve?
  Might perform similar functions as extrinsic impurities which have been shown to improve performance
Goal: use understanding of intrinsic impurities to design future surface treatments for high gradient and quality factor
  Taking new avenue by studying low RRR cavities
  Low purity Nb  increased concentration of intrinsic impurities
  Taking a deep dive in characterizing performance with TMAP
Observe many of the phenomena characteristic of each treatment, but again to slightly different extents

## Slide 5: Using TMAP to Further Characterize Performance of Low RRR Cavities

## Slide 6: Sequential TMAP Study on Single Low RRR Nb SRF Cavity
1.3 GHz TESLA-shaped single-cell low RRR (= 61) cavity
RF testing after surface treatments
  Electropolished (40 μm EP for baseline)
  Low temperature bake (120 ℃ x 48 hours)
  N-doping (2/6 recipe with 5 μm EP)
  Underdoped (additional 2 μm EP from N-doped surface)
36 boards
16 RTD’s per board

## Slide 7: Sequential TMAP Study 1/4: EP
  Cavity received 40 μm EP to reset surface
  Low RRR has slightly lower Q0 than high RRR
  Q0 slope begins sooner but less sharp than high RRR

## Slide 8: Sequential TMAP Study 1/4: EP
  Cavity received 40 μm EP to reset surface
  More localized heating but not only at quench location
TMAP Profile Just Before Quench
top iris
equator
bottom iris

## Slide 9: Sequential TMAP Study 2/4: LTB
  Low temperature bake (120 ℃ x 48 hours)
  Low RRR experiences reduced response to LTB treatment
9

## Slide 10: Sequential TMAP Study 2/4: LTB
  Low temperature bake (120 ℃ x 48 hours)
  More widespread heating, including at quench location
10
TMAP Profile Just Before Quench
top iris
equator
bottom iris

## Slide 11: Sequential TMAP Study 3/4: N-doped
  N-doping 2/6 recipe with 5 μm EP
  Much lower Q0 than high RRR but similar gradients reached
11

## Slide 12: Sequential TMAP Study 3/4: N-doped
  N-doping 2/6 recipe with 5 μm EP
  More widespread heating, not specifically at quench location
12
TMAP Profile Just Before Quench
top iris
equator
bottom iris

## Slide 13: Sequential TMAP Study 4/4: Underdoped
  Underdoped (additional 2 μm EP from N-doped surface) to see how decreasing N concentration changes performance
  Significantly lower Q0 but reaches higher gradient than N-doped
13

## Slide 14: Sequential TMAP Study 4/4: Underdoped
  Underdoped (additional 2 μm EP from N-doped surface) to see how decreasing N concentration changes performance
  More localized heating, including at quench location
14
TMAP Profile Just Before Quench
top iris
equator
bottom iris

## Slide 15: Comparing TMAPs for All Studied Treatments
EP LTB N-doped Underdoped

## Slide 16: Comparing TMAPs for All Studied Treatments
EP LTB N-doped Underdoped
Quench locations change between surface treatments
Does the heating behavior at the quench locations also change?

## Slide 17: Comparing Quench Spot Heating Profiles
EP: Change in slope corresponds to onset of HFQS

## Slide 18: Comparing Quench Spot Heating Profiles
EP: Change in slope corresponds to onset of HFQS
LTB: Delay in Q-slope means we do not see onset of additional losses

## Slide 19: Comparing Quench Spot Heating Profiles
EP: Change in slope corresponds to onset of HFQS
LTB: Delay in Q-slope means we do not see onset of additional losses
N-Doped: quench of magnetic origin so we do not see change in heating slope

## Slide 20: Comparing Quench Spot Heating Profiles
EP: Change in slope corresponds to onset of HFQS
LTB: Delay in Q-slope means we do not see onset of additional losses
N-Doped: quench of magnetic origin so we do not see change in heating slope
Underdoped: Large heating corresponds to large losses

## Slide 21: Comparing Quench Spot Heating Profiles
EP: Change in slope corresponds to onset of HFQS
LTB: Delay in Q-slope means we do not see onset of additional losses
N-Doped: quench of magnetic origin so we do not see change in heating slope
Underdoped: Large heating corresponds to large losses
Compare against high RRR EP:
Lower initial heating due to low impurity concentration
Sharper change in slope than low RRR EP because of stronger HFQS onset (thermal quench)

## Slide 22: Cavity Performance Summary
Lower quality factors but reach similar gradients
  ~1.5e10 at ~20 MV/m for 2K
Larger heating at quench locations but less sudden changes in slope
  More magnetic quench behavior (less thermal)
Combined effects of intrinsic and extrinsic impurities
Sample Study: identifying key impurity
Calculation of mean free path from frequency vs temperature data
N-infusion cavity testing and sample study
Next Steps

## Slide 23: Discussion Topics
How was RRR determined and how can we remeasure?
  Cell material from Tokyo Denkai (Ta Wt % .0193, RRR = 61)
How might oxygen and nitrogen behave differently in a Nb lattice with more impurities?
How can intrinsic impurities affect the sensitivity to trapped flux?
  Especially in N-doped and underdoped
This manuscript has been authored by Fermi Research Alliance, LLC under Contract No. DE-AC02-07CH11359 with the U.S. Department of Energy, Office of Science, Office of High Energy Physics. This work was supported by the University of Chicago.

## Slide 24: Extra Slides

## Slide 25: Quality Factor vs Accelerating Gradient at 2 K
Performance of EP, LTB, and N-doped are similar at medium gradients
LTB delays Q0 slope and reaches highest Q0 and gradient
N-doping reaches lowest gradient
Underdoped has lowest Q0

## Slide 26: Residual Resistance vs Accelerating Gradient
Low RRR EP and LTB Rr equal at low and mid fields
LTB treatment enables smallest increase with gradient
N-doped Rr always slightly larger than EP and LTB
Underdoped shows increase from N-doped

## Slide 27: BCS Resistance vs Accelerating Gradient
Low RRR exhibits low BCS behavior
Low RRR RBCS is lowest at mid field
Any benefit of dirty surface is lost at high field in EP and LTB
N-doped has lower RBCS than EP and LTB

## Slide 28: Effect of Doping Severity
N-doping severity effect on BCS resistance
Daniel Bafia’s Thesis Fig 6.7b
N-doping severity effect on heating at quench spots
Daniel Bafia TTC’20
Response of RTD Sensor Closest to Quench Spot vs Magnetic Field