## Slide 1
V. Chouhan
TESLA Technology Collaboration Meeting
5-8 December 2023
EP parameter investigation for low and high beta 650 MHz niobium cavities

## Slide 2: Outline
Introduction and motivation
Initial EP parameters and results
EP optimization for LB650 and HB650 cavities
Cavity performance
Summary
LB650 (0.61) cavity
HB650 (0.92) cavity

## Slide 3: WG1 High-Q/High-G

## Slide 4: Introduction and Motivation
PIP-II linac will accommodate different types of SRF cavities including 5-cell low beta (0.61) and high beta (0.92) 650 MHz elliptical cavities.
The surface of these elliptical cavities are processed with electropolishing (EP).
Motivation: To investigate impact of EP conditions on the surface of these cavities.
Cavity prematurely quenched at 15 MV/m.
Horizontal EP tool ANL/FNAL
2K
Limited by quench
Initial vertical test result of LB650
PIP II CM Spec
Cavity cooling: Water spray on cavity exterior,
Acid: H2SO4+HF

## Slide 5: Standard EP Conditions
Are these EP conditions optimal for 650 MHz cavities?
Parameters | Value
Voltage | 18 V
Cavity temperature | < 25 °C/12 °C
Acid flow rate | ~10 L/min
Cavity rotation | ~1 rpm
Cathode:anode surface area | 5%
Current with low amplitude oscillations
22 °C
18 V
Bulk EP
Current oscillations suggested that EP was optimal?
Removal rate:
  0.14 um/min at 22 °C (Bulk EP)
  0.07 um/min at 12 ° C (Cold EP)
Current profile (warm EP)
Aluminum cathode
Insulating mask
Initial cathode (cathode-I)

## Slide 6: I-V curve and surface of LB650
Cavity temperature~12℃
Linear region: etching region
No current plateau in the I-V curve.
A current plateau is necessary for EP.
The standard EP parameters seem inadequate for EP of 650 MHz cavities.
Typical I-V curve (1.3 GHz 9-cell Cavity)
Cavity temperature~12℃
EP
Etching
EP with standard parameters
9 mm
Step height ~ 32 µm
I-V curve_LB650 (5-cell Cavity)
Initial cathode
Surface (LB650)

## Slide 7: Modified cathode for LB650 cavities
Modified cathode (Cathode-M)
Initial cathode (Cathode-I)
V. Chouhan et al., Nucl. Instrum. Methods Phys. Res. A 1051 (2023) 168234.
V. Chouhan et al., TUPTB041, TUPTB042 SRF2023.
The modified cathode yielded an apparent current plateau (EP plateau).
A large cathode surface may reduce cathode polarization by reducing cathode-acid interface resistance and hydrogen bubble screening effect.
Cathode surface area was enlarged to make it close to 10% of the cavity surface area.
15 °C
Ramp rate: 1 V/12 s

## Slide 8: I-V curves at different cavity temperatures (LB650)
V. Chouhan et al., Nucl. Instrum. Methods Phys. Res. A 1051 (2023) 168234.
V. Chouhan et al., TUPTB041, TUPTB042 SRF2023.
I-V curves with modified cathode
Onset voltage vs cavity temperature
Onset voltage increases with increase in cavity temperature.
Different EP voltages might be suitable to perform warm and cold EP.
The standard EP voltage (18 V) is not high enough for warm EP of 650 MHz cavities.

## Slide 9: Study with HB650 (5-cell cavity)
A new cathode with a larger surface area was designed.
(cathode:anode surface area = 3:10)
The cathode design may:
  Reduce cathode polarization
  Improve acid flow conductance to improve removal uniformity
New cathode (Cathode-N)

## Slide 10: Onset voltage and acid aging
Onset voltage varied with different acid conditions even at the same temperature.
Reaction rate seems responsible for variation in the onset voltage.
Higher reaction rate (higher current):
  Difficult to meet diffusion limited conditions when anode-cathode distance is large?
  High potential drop at cathode-acid interface?
Acid aging
Onset voltage vs current density at ~21 °C
~21 °C
Onset with cathode-M and -N

## Slide 11: Optimal EP conditions
Current oscillations usually signify favorable EP conditions that provides a smooth surface finish of the cavities.
The oscillations amplitude diminishes and eventually disappear with acid aging, particularly at a low temperature.
In such cases, relying solely on current oscillations may not be suffice.
Optimum EP voltage was defined to be at least 5 V above the onset.
5V
Parameters | Initial EP | Modified EP | 
 | Warm/cold EP | Warm EP | Cold EP
Voltage | 18 V | 20-25 V | 16-22 V
Cavity temperature | 22 °C/12 °C | 22-25 °C | 12 °C
Cathode type | Cathode-I (initial) | Cathode-M (modified) Cathode-N (large sized) | 
No oscillations but smooth surface
Onset
EP voltage
EP voltage = Onset + 5 V

## Slide 12: Cavity surface after modified EP
HB650 cavity (B92F-RI-203)
Equator surface after modified EP
A smooth surface was obtained with the modified cathode and a higher voltage.
LB650 cavity (B61C-EZ-104)
Replica image representing equator surface
Average roughness Ra was ~0.5 µm.
23 V, 22 °C, 120 µm
25 V, 25 °C, 160 µm
9 mm

## Slide 13: Baseline vertical test results (modified EP)
EP with the modified cathode and parameters showed good performance in the baseline vertical tests.
The cavities are in process of mid-T or N-doping to improve Q0 value.
No quench
Limited by FE
at 2K
HB650 (5-cell cavities)
PIP II CM Spec
No quench
(Admin limit)
at 2K
PIP II CM Spec
LB650 (5-cell cavities)
Process: EP + 800/900 °C + light EP

## Slide 14: Summary
Initial standard EP conditions yielded a rough equator surface and poor performance of 650 MHz cavities.
EP parameters were studied. The cathode and EP conditions were modified.
The modified cathode and EP conditions yielded a smooth surface and good performance of the LB650 and HB650 cavities.
No significant higher removal on the iris due to cathode proximity and higher voltage was observed.

## Slide 15
THE FUTURE OF FERMILAB
Follow us:
http://pip2.fnal.gov/
/showcase/pip-ii/

## Slide 16: Removal profiles
The large cathode surface area, cathode proximity to the iris, and higher EP voltage do not enhance removal on the iris.
LB650 5-cell cavity
HB650 1-cell cavity
Cathode-N

## Slide 17: Current and temperature profiles (HB650)
< 12 °C
25 °C
A large cathode surface and higher voltage do not increase EP current.
25 V
22 V