## Slide 1: Fabrication and testing of DQW crab cavities for HL-LHC upgrade
Katarzyna Turaj on behalf of WP4 and SY-RF-SRF
TTC meeting, Fermilab, December 5-8, 2023

## Slide 2: HL-LHC Cavity Geometries
/cavity*
()
RF power = 40 kW-CW
Operating Temp = 2 K
*Engineering spec: 4.1 MV dressed for 20% margin
Radio Frequency Dipole (RFD) cavity
– to be used in Point 1 (ATLAS), horizontal
Double Quarter Wave (DQW) cavity
– to be used in Point 5 (CMS), vertical

## Slide 3: Planning
2018-2022 | 2023 | 2024 | 2025 | 2026 | 2027 | 2028
DQW CM SPS-tests
RI-DQW
pre-series (x2)
CERN-DQW
series (x2)
RFD CM SPS-tests
USAUP-RFD proto (x2)
RI-DQW
series (x6)
UK-CERN DQW CMs
series (4 + 1)
USAUP-RFD
pre-series (2)
Canada-CERN RFD CMs
series (5)
USAUP-RFD series (10)
High Power RF system not shown below

## Slide 4: Cavity Manufacturing challenge
Cavities made of high purity bulk Niobium to sustain surface fields in excess of 50 MV/m & 100 mT
Very complex shaping, welding (30+) & assembly accuracy process to reach high final shape
M. Garlasche et al., link

## Slide 5: Reaching the right frequency
A series of precision trimming & RF measurements of sub-assemblies before final welding
Final re-shaping to reach target frequency & metrology
Successfully demonstrated on both DQW CERN & RI cavities
DQW, trimming
DQW re-shaping
Frequency evolution of DQW cavities produced by CERN
N. Valverde (link), A. Edwards et al., (link)

## Slide 6: Surface preparation
A rotational BCP is used to remove during fabrication followed by a high-temperature UHV heat treatment (650°C, 24h)
  Ultrasound measurement in several locations around cavity body
6
L. Ferreira et al., link
Notes: A rotational BCP is used to remove the damaged layer of the RF surface (~250 μm) during fabrication followed by a high-temperature UHV heat treatment

## Slide 7: Cold Test Preparation, SM18
Standard procedure of high-pressure rinsing, clean room assembly and 120°C bake-out
Controlled cool-down to keep the gradient across the cavity to <50K
Nb-coated flanges to minimized RF losses

## Slide 8: HOM Couplers, Antennas, Feedthroughs & RF Lines
4-HOM couplers in the DQW to achieve the strong damping ()
  3 bulk-Nb HOM, 1 HF-HOM (Cu-Nb transitions, complex joining of two heterogenous materials)
HOM couplers withstanding up to 1kW-CW power with special feedthrough for robustness
RF lines to extract HOM power from 2K environment to 300K in vacuum
  Extensive program to design & build the RF lines was necessary
Standardized feedthrough for all HOM couplers
E. Montesinos (link), S. Barriere et al., link
LHC-DQW HOM Coupler
Brazed feedthrough with RF clamp
RF lines
Notes: HL-LHC will circulate a beam current of 1.1 A. To avoid beam instabilities very strong HOM damping is pre-requiste
Elaborate scheme of HOM couplers were designed and validated for both cavities.
A key aspect *high* power HOM couplers withstanding up to 1kW-CW power with special 25Ω feedthrough for robustness extract up to 1 kW of HOM power from 2K environment to 300 K in vacuum requires special care
  316LN coax lines with Cu-sputtering, flexibility with spherical joints & thermalization the Al discs for heat load
Extensive program to design & build the RF lines was necessary

## Slide 9: Cold Tests
Baseline: tested 3 times as bare, jacketed and dressed configuration
  Bare (BC)
  Jacketed (JC): Cold Magnetic Shield + Helium tank assembly (bolted) and TIG welding
  Dressed (DC): JC equipped with RF couplers (3 HOMs, 1 HF HOM, 1 FA + VT input antenna)
Experience shows that:
  1 out of 2 cavities requires 2 additional cold RF tests and additional BCP and/or HPR in bare and dressed configuration
Dressed
Jacketed
Bare

## Slide 10: CERN-DQW, Series (1 & 2)
DQW2: BC, JC, DC
CERN built two series DQW cavities
  DQW2-CERN dressed cavity exceeded the specification target: 4.6MV
    1 CT stopped due to wrong antennas and 2 CT cavity reached 4MV (*)
  DQW1-CERN dressed needs to be retested:
    1 CT cavity reached 3.9MV: degradation observed after the high-power RF conditioning
    2 CT cavity reached 3.5MV
1st series in final HL-LHC configuration qualified!
(*) Eng spec: Vt ≥4.1MV,Q0 ≥3.9×109

## Slide 11: DQW Industrial Series (RI)
8 DQW (BC and JC) cavities produced in industry (Research Instruments, DE)
  All cold tests and dressing of cavities at CERN
1st jacketed cavity achieved excellent cold test results
2nd jacketed cavity cold test was accepted, stopped by purpose at 5MV
  Q slope visible since the beginning of the scan  seen in bare configuration as well
They will be tested in a dressed configuration soon.
Research Instruments (DQW1 & DQW2)
2023 (JC)
2022 (BC)
JC (2023)
BC (2022)

## Slide 12: Challenges, lessons learned & conclusion
The max fields reached are mostly dominated by the presence of field emission.
Poor bare cavities performance (DQW1-RI & DQW1-CERN) can’t be recovered by HPR  light BCP needed
  Both cavities tested 3 times in bare configuration
  DQW1-RI: Q slope visible since the beginning of the scan
Thermal cycle, up to ≈20 K, consistently improved 𝑄0 of both the jacketed and dressed cavities by ≈400%.
Dressed cavities performance limitation: ongoing investigations into field limitations above 4MV to try and surpass the specification.
  Dressed DQW2-CERN achieved 4.6 MV (3rd CT), but dressed DQW1-CERN was tested twice without success despite changes in the process
  As a precaution, dressed cavities are tested at 2.5K and only final measurements are made at 2K.
  120̊C bakeout was implemented recently for the dressed cavity configuration.
  HOMs coupler treatment required several iterations.
Continually learning and implementing actions to improve quality and meet project deadlines.

## Slide 13: Spare: HL-LHC Crab Cavity Series
5 DQW cryomodules | 5 RFD cryomodules | 20 IOT RF Systems
Cavities + processing + helium vessels by Research Instruments (DE) & CERN Cold magnetic shields by UK HOM couplers + antennas by CERN 4 CM by UK (STFC) & 1 CM at CERN with some components from CERN All cavities & CM cold validation tests at CERN (and a backup at Uppsala-Sweden) | Bare cavities by Zanon (IT) under US-AUP Processing + cold magnetic shield + helium vessel + HOM couplers + antennas + cold tests by US-AUP 5 CM by TRIUMF-Canada with some components by CERN CM cold validation tests at CERN | High power amplifiers (IOT) CERN High power RF lines, circulators, loads by CERN (exploring new frontiers) TCA platform for LLRF by CERN
5 DQW cryomodules | 5 RFD cryomodules | 20 IOT RF Systems
Cavities + processing + helium vessels by Research Instruments (DE) & CERN Cold magnetic shields by UK HOM couplers + antennas by CERN 4 CM by UK (STFC) & 1 CM at CERN with some components from CERN All cavities & CM cold validation tests at CERN (and a backup at Uppsala-Sweden) | Bare cavities by Zanon (IT) under US-AUP Processing + cold magnetic shield + helium vessel + HOM couplers + antennas + cold tests by US-AUP 5 CM by TRIUMF-Canada with some components by CERN CM cold validation tests at CERN | 

## Slide 14: Spare: CERN Cavity Test Results – DQW1 & DQW2

## Slide 15: Spare: Bare Cavity Test Results – DQW1-CERN & DQW1-RI
DQW1_CERN

## Slide 16: Spare: Cold tests
DQW cavities
CERN
DQW1
DQW2
RI
DQW1
JC
1 CT
BC
3 CT
JC
1 CT
BC
1 CT
JC
1 CT
BC
3 CT
JC
1 CT
DQW2
BC
1 CT
DC
2 CT
DC
3 CT
DC
DC
...
6 more coming

## Slide 17: Spare: Crab Cavities & “Radio Frequency Auxiliaries”
Double Quarter Wave (DQW) cavity
– to be used in Point 5 (CMS)
HOM Couplers
x 36 units
RF Field Antenna
x 12 units
Fundamental
Power Couplers
x 14 units
HF-HOM Couplers
x 12 units
HOM Couplers, Feedthroughs, Field Antennas HF-HOM and FPC for all LHC-series DQW crab cavities are being manufactured at CERN Main Workshop,
i.e. quantities for 8 cavities including spares