## Slide 1: Experience of testing TEM cavities in FREIA laboratory: ESS series double-spoke cryomodules and CERN Crab cavity
Mykhailo Zhovner on behalf of FREIA team
7 Dec 2023

## Slide 2: Briefly about FREIA laboratory
Vertical cryostat
GERSEMI
HNOSS
Horizontal cryostat
Multiple bare cavity testing is available
Active magnetic field compensation.
3.2m x ø1.1m total volume
2.65m x ø1.1m below lambda plate
Inner size 3.3m x ø1.2m
For a cavity with a helium jacket
Ideal for coupler testing: FPC, HOM
Multiple cavities may be tested at the same time
Cryomodule test stand
Everything needed for cryomodule (CM) + valve box (VB) installation.
Liquefier up to 140 l/h
High power RF plant
Çryomodule test stand
~ 120 l/h liquid He production
90W of continues power dissipation
Two tetrode based 352MHz 400kW pulse amplifier. Up to 16kW @ CW.
NI PXI based LLRF

## Slide 3: ESS prototype Medium-β Double spoke cavities
2 cavities equipped with FPC was tested.
Cavity conditioning history
Q factor is done by the calorimetrical method.
Both SEL and PID operation method are implemented.
The maximum gradient higher than 9 MV/m was achieved.

## Slide 4: Multipacting conditioning of series CM
9MV/m
Low field
mulipacting
5MV/m
During cavity MP conditioning we deal with superposition MP bands from cavity and FPC.
Both MP sources have influence on the beam vacuum.
Usually, only MP from cavity generate X-ray.
Outgassing during warm FPC conditioning
FPC
Cavity
70 – 100 kW

## Slide 5: Local quench at low cavity field
Local quench & thermal feedback is ALWAYS observed at very low field in the spoke cryomodules so far
Vf*
Vr*
Vt*
Low field multipacting can be easy conditioned.
Pulse operation during cavity conditioning prevent from global quench.
Small influence on cryogenic is observed.
He bathe pressure interlock should be activated from the beginning.
Vf*
Vr*
Vt*
* - uncalibrated voltage from LLRF ADC

## Slide 6: Field emission, VT vs Cryomodule. Power dissipation
Field emission onset measured from behavior of X-ray* during RF powering with reference to influents to cryogenics.
HPR after VT, not tested afterwards
*
30 cm
Cav2
Cav1
Field emission onset (DSPK#) comparison between vertical VT (IJCLab) and cryomodule CM (FREIA) tests.
By “historical reasons” both cavities share the same X-ray detector which placed transversal to beam axis between cavities.
Static vs Dynamic (9 MV/m both cavities) heat load
Expected RF heat loss based on VT data is of the order of mW (after multipacting conditioning), which is much lower than the measurement resolution of the calorimetric method at FREIA. This indeed proves that cavity performance has not been significantly degraded after the vertical tests.
arXiv:2306.11333v1
Issue with pressure stability during the measurement.

## Slide 7: Field emission treatment
Eacc [MV/m]
Radiation [a.u.]
FE treatment example. CM11
Initial test
After 1st TC*
+RF condit.
After 2nd TC
VT
9MV/m
Chart: FE onset [MV/m]
| CM02 | CM02 2nd | CM03 | CM03 2nd | CM04 | CM04 2nd | CM09 | CM09 2nd | CM10 | CM10 2nd | CM14
FE onset Cav1 | 9 | 9 | 11 | 10.5 | 9
FE onset Cav2 | 12 | 12 | 11 | 8.5 | 10 | 10.5 | 9
Field emission onset was degraded in CM11
The thermal cycle (Cryogenic failure) to 300K after the 1st test improved the performance.
The cavity power dissipation shows a sharp rise.
9 MV/m in the 1st test  10MV/m in the 2nd test
RF conditioning was tried but small impact.
2nd thermal cycle helped a lot  why?
Future investigation to be continued.
FE onset evolution for CMs which was retested

## Slide 8: Uncertainties, VT vs Cryomodule test stand
Chart: Cavity number
Qt(VT) | 195000000000 | 370000000000 | 400000000000 | 348000000000 | 220000000000 | 210000000000 | 231000000000 | 335000000000 | 231000000000 | 335000000000 | 210000000000 | 155000000000 | 178000000000 | 210000000000 | 200000000000 | 155000000000
Qt_Pr (CM) | 266947335163.2077 | 189906262961.4268 | 451003389064.6182 | 288975993239.02 | 280942968865.6843 | 188326187786.5639 | 219244773001.6938 | 258586003650.181 | 413697939354.0153 | 284422075339.1616 | 274125159290.5115 | 165349136463.1745 | 230075740529.0788 | 214632925123.7657 | 389234327074.7399 | 286802538598.5748
Qt_Pf (CM) | 215063920538.6939 | 317574450435.504 | 390067329417.0809 | 320545808280.4398 | 276533599504.2202 | 230533196890.1588 | 181100080404.7314 | 308591944811.3147 | 327024097824.0731 | 304630777173.1311 | 229228723953.8488 | 151587045239.3889 | 233052359873.7583 | 285037323790.1274 | 301061063822.9384 | 269591285629.4537
Chart: Cryomodule number
| CM09 2nd | CM12 | CM13
Qt (from Orsay) CavIn | 230000000000 | 320000000000 | 230000000000
Qt (from Orsay) CavOut | 185000000000 | 125000000000 | 185000000000
Qt TM FREIA 9MV/m CavIn | 269900000000 | 359000000000 | 373200000000
Qt TM FREIA 9MV/m CavOut | 206800000000 | 165400000000 | 219500000000
For Eacc estimation we using Qt value measured at VT  official numbers
Additionally, Qt estimation from integration of Pr after end of the pulse was implemented for last several CMs.
Visible consistent Qt underestimation from VT.
Qt Cav1 from VT
Qt Cav2 from VT
Qt Cav1 from FREIA
Qt Cav2 from FREIA
Eacc estimation from provided Qt well enough fit with some cavities features as field emission onset.

## Slide 9: He accumulation on cavity walls
Chart: CM09 2nd, Thermocycles
| 0 | 5.5833333333721384 | 18.75 | 50.06666666676756 | 57
PT10 He 4K | 0 | 1.5e-09 | 3.2e-09 | 5.1e-09 | 5.4e-09
PT20 He 4K | 0 | 1.7e-09 | 3.6e-09 | 5.6e-09 | 5.8e-09
PT10 4K+2K | 3.5e-09 | 9.9e-09
PT20 4K+2K | 3.8e-09 | 1.1e-08
2nd thermocycle
3rd
thermocycle
LR: 1.95E-7 mbar l/s
1st
thermocycle.
2K was achieved
4th
thermocycle
LR:2.7E-8 mbar l/s
5th
thermalcycle
LR:1.17E-7 mbar l/s
He signal often observed in beam vacuum during warmup when cavity wall temperature exceed ~10K.
Mass: amu
Faraday: Torr
RGA mass spectrum
He
Beam vacuum [mbar]
Cavity wall temperatures [K]

## Slide 10: Results of CM testing
2 types of major issues cause a CM disqualification:
Courtesy of IJCLab
CM02, CM03, CM04, CM10
CM04, CM09
Under ILCLab investigation
After repairing in IJCLab CMs were retested in FREIA, successfully approved and delivered to ESS.
From A.Miyazaki. IJCLab
All 13 CM are installed in the tunnel
Last, spare, CM under assembly
FREIA
IJCLab

## Slide 11: CERN DQW “Crab” prototype cavity
During reception test after cavity arrival, we didn't found HOM by VNA. Cavity was opened in clean room (Class 10), found broken antenna and attached back for VNA test.
“Cryogenic” foams used to reduce liquid helium volume
Was performed a series of VT at FREIA and CERN, Try to track a variation in cavity performance over the time, transportation, and multiple venting.
Before falling antenna
After antenna repairing + HPR
Q vs Eacc 1st test
arXiv:2011.05210

## Slide 12: Learned lessons
DSPC are robust, ridged and well predicted cavities.
Multipacting relatively tuff but its “field bands ” is well defined and repetitive.
It is easy to quench cavity at low field (<1MV/m), specially, during CW operation.
Low field multipacting can cause difficulties for field probe calibration in VT.
In our case, thermal cycles help a lot to treat FE.
Cold cavity walls able to accumulate He  making small cold leaks invisible during cold operation until warm up.
Having connected RGA to beam vacuum is a good practice.
Accurate Q0 measurement in strongly over coupled case is a big challenge.
From ESS double spoke cavities:
From CERN prototype Crab cavity:
Transportation of SRF cavities on long distance is not a greater idea.
Chemical treatment of cavity surface is mandatory to recover performance after mechanical interaction, like foaling down field probe.
SRF cavities do not become better with age. Clear visible performance degradation with every venting.

## Slide 13: Thank you for attention!
Experience of testing TEM cavities in FREIA laboratory: ESS series double-spoke cryomodules and CERN Crab cavity