## Slide 1: Flux Designations
ROM1, ROL1, REL0, ROL0, …
First two letters are the base formulation, but it’s complicated
  IN – Inorganic.
  OR – organic but NOT resins or rosins (resins and rosins are organic)
  RE – resin which is NOT a rosin (rosin is also a resin)
  RO – rosin, which is resin derived from tree sap
3rd letter is activity level ↔ how much etching it does. This one’s simple: L (Low), M (Medium), H (High). Lower is better … as long as it works
Last letter is halide content. Halides can cause long-term corrosion, so best to avoid
  0 – no detectable halides (<0.05%)
  1 – Measurable halides
Other designations
“No clean”
  Mostly a cosmetic property: not less residue, but transparent residue
  There’s separate tests for conductivity, and I don’t know of any flux used in electronics which does not pass
Water soluble.
  Most fluxes require soap to clean off, though some come off with alcohol
  Water soluble fluxes can be removed with warm water
  Even if not done regularly, can be useful for debugging problems
  Comes at a price
    More acidic at high humidity
    Spreads with condensation

## Slide 2: Kester 44 (ROM1)
A classic! But maybe not suitable here
  More active than needed ↔ etches wire more than necessarily
  Activated with halides ↔ long term wire corrosion
  Corrosion issues confirmed by manufacturer data

## Slide 3: Loctite 362 (ROL1)
Test results not presented in a clean manner. Here’s my interpretation
  Copper Mirror Corrosion (thin copper coating) “Pass” → didn’t completely remove copper. Probably moderate, similar to Kester
  Corrosion test (bulk steel corrosion) “Pass” → no visible corrosion. Probably better than Kester
  Silver chromate – is to detect halides. “Pass” means it doesn’t have more than the “1” designation implies
More benign than Kester 44… but halide-free would be better

## Slide 4: Chipquik SMD3SW (REL0)
Copper Mirror: No breakthrough
Corrosion: No corrosion
Quantitative Halides: <0.05%
Water soluble
The only RE flux considered.
Also the only water-soluble flux
The “0” designation calls for more sensitive halogen test than silver bromide (so that is not listed)

## Slide 5: Kester 285 (ROL0)
Not sure how to compare with Chipquik
  Copper mirror – is “Low” seems better than “No breakthrough”
  Corrosion test – “Low” seems worse than “No corrosion”
Comparable to Chipquik except this is not water soluble.

## Slide 6: Conclusion
My crude tests show Chipquik REL0 wets the Protodune wire just fine at 290C
  But didn’t work well on the AWI wire
Haven’t tried the Kester ROL0 but likely just as good
I suggested water soluble, but after reviewing discussions from early in Mu2e...
  Mu2e tracker is small enough to keep in a humidity-controlled cleanroom. APAs will be in a warehouse, stringent environmental requirements may be expensive
  Mu2e uses tungsten wires, not easily etched. APAs’ copper wire will be more sensitive
The disadvantages of water soluble seem to outweigh advantages in this case
If Chipquik and Kester 285 pass pull tests, suggest going with Kester 285