## Slide 1: 650MHz Cavity, Helium Vessel, and Tuner Status at Fermilab
Chuck Grimm
IIFC POC 650MHz Cavities
Fermilab
(Avinash Puntambekar RRCAT)

## Slide 2: Introduction
Single Cell Cavities
  Current Cavity Orders
  Vertical Test Results & Testing Plans
5-Cell Cavities
  Current Cavity Orders
  Possible “Future” Design Changes
  Spin Forming Seamless Beam Tubes
Helium Vessel
  Design Progress
  Spin Form Seamless Vessel Tubes
  Roll and Seam Weld Vessel Tubes
  Stainless Steel to Titanium Flanged Connection
  Automatic TIG Welding
Tuners
  Blade Tuner
  Lever Tuner
  Wedge Tuner
  Motors

## Slide 3: Single Cell Cavities
Current Fabrication Status
  Advanced Energy Systems (AES) * (6) β=0.9 cavities; complete in-house
  PAVAC Industries * (5) β=0.9 cavities; ordered
  Jefferson National Lab (J-Lab) * (2) β=0.61 cavities; complete in-house (part of MOU)
  Research Instruments (RI) * (3) β=0.61 Fermi design, (3) β=0.61 J-Lab design; ordered
Test Results
  One J-Lab built cavity was vertically tested at FNAL, reached 12 MV/m limited by Q-drop
  The 6 AES cavities are scheduled for VTS in early December.
β= 0.9
β= 0.61 Fermi Design
β= 0.61 J-Lab Design

## Slide 4: Single Cell Cavities
Six β=0.9 cavities produced by AES and delivered to FNAL in 2012

## Slide 5: 5-Cell Cavities
Current Fabrication Status
  AES * (4) β=0.9 cavities; ordered
  PAVAC * (5) β=0.9 cavities; ordered
  RI * No multi-cell cavities on order
Future Design Changes?
  Larger beam tube diameter and iris
  Longer beam tube to accommodate a lever tuner?
  Transition spool re-design for cost reduction
β= 0.9

## Slide 6: 5-Cell Cavity Design Challenges
Considerations for Future Changes Based On:
  Low Bandwidth
  CW Operation
  Tough Requirements For Microphonics
  Small dF/dP (self-compensating and self-tuning schemes)
  Good Tuneability ( small load for piezos and tuner motors)
  Good Efficiency of Tuning (stiffening ring optimization)
  No Limitations in Longitudinal Size but Limitations in Transverse Size
  Problems with Lorentz Detuning
  Compact, Simple and Reliable Course Tuner w/o Backlash
  Inexpensive Cavity Design (design for cost cutting)??
β= 0.9

## Slide 7: 5-Cell Cavity Transition Spool
Transition Spool Redesign (Cost Reduction)
  Raw Material Cost for RRR niobium ~20K
  Multi-Piece Fabrication
  Mixture of RRR Niobium and Reactor Grade Niobium
Fermilab Design
J-Lab Design
RRCAT Design
(A. Puntambekar)

## Slide 8: 5-Cell Beam Tubes

## Slide 9: Helium Vessel
Design of helium vessel (Baseline) – Considerations
  Spin form seamless vessel tubes
  Roll and seam weld vessel tubes
  2-phase pipe connection of He vessels
  Tuner type
Automatic TIG welding machine for cavity dressing
  Moving out of the (glove) box

## Slide 10: Helium Vessel Analysis
Preliminary analysis at 2 Bar pressure at room temperature shows no stresses above 30 Mpa (By Serena Barbanotti)

## Slide 11: Helium Vessel Analysis
Preliminary analysis at 4 Bar pressure cold (2K) shows no stresses above 40 Mpa (By Serena Barbanotti)

## Slide 12: Helium Vessel
Spin form seamless vessel tubes
  Leak check – good
  Dimensional QC – good
  Pull-out test – next
Roll and seam welded vessel tubes
  Leak check – good
  Dimensional QC – good
  Continue prototype fabrication - next

## Slide 13: Flange Connection
Flange test assemblies were fabricated to replicate the helium vessel to cryomodule connection
  Grade 2 titanium connection is the same as the beam flange and will use a common hex seal
  316L stainless steel 2-phase connection uses a groove socket to hold seal in place for an inverted connection (seal shown in photo)
316L Stainless Steel
Grade 2 Titanium

## Slide 14: Flange Connection Cold Shock
Flange assembly was leak checked prior to cold shock testing
  No detectable leaks were found
Flange assembly was submerged in LN2 while system was actively pumping
Assembly was removed once boiling activity stopped

## Slide 15: Tuners
  Blade Tuner
  (Baseline Design)
Lever Tuner
?
Indian
Wedge Tuner
(Currently being shipped to
Fermilab from India)

## Slide 16: Tuner Motors
Purchase complete assembled
units from Phytron
  Planetary gears
  Lifecycle study at Fermilab
  Common design for 325, 650, &
  1300MHz cavities
  About the same cost as current
  design

## Slide 17: Cavity Dressing – TIG Welding
325 MHz Cavity
650 MHz Cavity
Design features
  Movable overhead boom for wire feed system & external purging system
  Movable pre-loading tailstock for various cavity lengths
  Headstock with internal purging capabilities
  Automatic joint tracking system
  Duel monitors offer live welder adjustment capabilities

## Slide 18: What’s Next?
Process single and 5-cell bare cavities
  Test in VTS
  Centrifugal Barrel Polishing (Tumbling)
  HPR, EP, BCP…….Etc.
Continue fabrication of baseline prototypes
  Bladetuner
  Helium vessel
  Assembly and welding fixtures
Dress 5-cell cavity
  VTS tests
  Room temperature tests
  Mechanical test of tuner(s)
  Eventual HTS

## Slide 19: Thank You!