## Slide 1: IMP RFQ Status and Fabrication Tests
Derun Li
Center for Beam Physics
Lawrence Berkeley National Laboratory
PXIE RFQ Meeting, Fermilab, IL
November 29, 2012

## Slide 2: IMP RFQ Status
Beam dynamics frozen
  Beam dynamics design is optimized for 15 mA
  Error analysis complete
Thermal and mechanic analysis complete
Engineering design complete
RF design complete
  Collaboration with Fermilab
  Validation of the RF simulations by IMP in progress
Fabrication tests started
  Formed cutter
  Full length vane (gun drill, e-beam plugs and modulation)
  Braze tests
  Half module (including all features of tuners, pi-mode rods, two ends) in progress
    Allow for low power RF measurements

## Slide 3: IMP RFQ Status
Fabrication drawings
  Delivered rough machining drawings last week
Production copper (from Hitachi) received
  Fabrication (rough machining) to start next month
RF source purchased and will arrive next month
  200 kW total
Interface with LEBT and MEBT to be finalized
RF power couplers
  Design and fabrication by IMP (with LBNL’s assistance)
IMP RFQ schedule
  Fabrication will be carried out at IMP machine shop (upgrade of the shop in progress)
  New hydrogen furnace (arrived in August 2012)
  Complete by end of 2013 (aggressive)

## Slide 4: Fabrication Tests at IMP
Vane cutting tool test
Full length vane fabrication test
Vane braze test
New braze clamp design
Half module

## Slide 5: Braze Tests at IMP
Two braze tests were conducted in the summer of 2012 with unsatisfactory results
Updated clamp design
  Provide strong support to copper
Reduce and control the torque force on the clamps

## Slide 6: Braze Test using New Clamp
Vacuum tight & acceptable distortion

## Slide 7: Temperature Ramping Profile
Chart: 
| 0:53:54 | 0:56:34 | 0:59:14 | 1:01:54 | 1:04:34 | 1:07:14 | 1:09:54 | 1:12:24 | 1:15:04 | 1:17:44 | 1:20:24 | 1:23:04 | 1:25:44 | 1:28:24 | 1:31:04 | 1:33:44 | 1:36:24 | 1:39:04 | 1:41:44 | 1:44:14 | 1:46:54 | 1:49:34 | 1:52:14 | 1:54:54 | 1:57:34 | 2:00:14 | 2:02:54 | 2:05:34 | 2:08:14 | 2:10:54 | 2:13:34 | 2:16:14 | 2:18:44 | 2:21:24 | 2:24:04 | 2:26:44 | 2:29:24 | 2:32:04 | 2:34:44 | 2:37:24 | 2:40:04 | 2:42:44 | 2:45:24 | 2:48:04 | 2:50:44 | 2:53:14 | 2:55:54 | 2:58:34 | 3:01:14 | 3:03:54 | 3:06:34 | 3:09:14 | 3:11:54 | 3:14:34 | 3:17:14 | 3:19:44 | 3:22:24 | 3:25:04 | 3:27:44 | 3:30:24 | 3:33:04 | 3:35:44 | 3:38:24 | 3:41:04 | 3:43:44 | 3:46:24 | 3:49:04 | 3:51:44 | 3:54:24 | 3:57:02 | 3:59:34 | 4:02:14 | 4:04:54 | 4:07:34 | 4:10:14 | 4:12:54 | 4:15:34 | 4:18:14 | 4:20:44 | 4:23:24 | 4:26:04 | 4:28:44 | 4:31:24 | 4:34:04 | 4:36:44 | 4:39:24 | 4:42:04 | 4:44:44 | 4:47:24 | 4:50:04 | 4:52:44 | 4:55:24 | 4:58:04 | 5:00:34 | 5:03:14 | 5:05:54 | 5:08:34 | 5:11:14 | 5:13:54 | 5:16:34 | 5:19:04 | 5:21:44 | 5:24:24 | 5:27:04 | 5:29:44 | 5:32:24 | 5:35:04 | 5:37:44 | 5:40:24 | 5:43:04 | 5:45:44 | 5:48:24 | 5:51:04 | 5:53:44 | 5:56:24 | 5:59:04 | 6:01:44 | 6:04:24 | 6:07:04 | 6:09:44 | 6:12:24 | 6:15:04 | 6:17:44 | 6:20:24 | 6:23:04 | 6:25:44 | 6:28:24 | 6:31:04 | 6:33:44 | 6:36:24 | 6:39:04 | 6:41:44 | 6:44:24 | 6:47:04 | 6:49:44 | 6:52:24 | 6:55:04 | 6:57:44 | 7:00:24 | 7:03:04 | 7:05:44 | 7:08:24 | 7:11:04 | 7:13:44 | 7:16:24 | 7:19:04 | 7:21:44 | 7:24:24 | 7:27:04 | 7:29:44 | 7:32:24 | 7:35:04 | 7:37:44 | 7:40:24 | 7:43:04 | 7:45:44 | 7:48:24 | 7:51:04 | 7:53:44 | 7:56:24 | 7:59:04 | 8:01:44 | 8:04:24 | 8:07:04 | 8:09:44 | 8:12:24 | 8:15:04 | 8:17:44 | 8:20:24 | 8:23:04 | 8:25:44 | 8:28:24 | 8:31:04 | 8:33:44 | 8:36:24 | 8:39:04 | 8:41:44 | 8:44:24 | 8:47:04 | 8:49:44 | 8:52:24 | 8:55:04 | 8:57:44 | 9:00:24 | 9:03:04 | 9:05:44 | 9:08:24 | 9:11:04 | 9:13:44 | 9:16:24 | 9:19:04 | 9:21:44 | 9:24:24 | 9:27:04 | 9:29:44 | 9:32:24 | 9:35:04 | 9:37:44 | 9:40:24 | 9:43:04 | 9:45:44 | 9:48:24 | 9:51:04 | 9:53:44 | 9:56:24 | 9:59:04 | 10:01:44 | 10:04:24 | 10:07:04 | 10:09:44 | 10:12:24 | 10:15:04 | 10:17:44 | 10:20:24 | 10:23:04 | 10:25:44 | 10:28:24 | 10:31:04 | 10:33:44 | 10:36:24 | 10:39:04 | 10:41:44 | 10:44:24 | 10:47:04 | 10:49:44 | 10:52:24 | 10:55:04 | 10:57:44 | 11:00:24 | 11:03:04 | 11:05:44 | 11:08:24 | 11:11:04 | 11:13:44 | 11:16:24 | 11:19:04 | 11:21:44 | 11:24:24 | 11:27:04 | 11:29:44 | 11:32:24 | 11:35:04 | 11:37:44 | 11:40:24 | 11:43:04 | 11:45:44 | 11:48:24 | 11:51:04 | 11:53:44 | 11:56:24 | 11:59:04 | 12:01:44 | 12:04:24 | 12:07:04 | 12:09:44 | 12:12:24 | 12:15:04 | 12:17:44 | 12:20:24 | 12:23:04 | 12:25:44 | 12:28:24 | 12:31:04 | 12:33:44 | 12:36:24 | 12:39:04 | 12:41:44 | 12:44:24 | 12:47:04 | 12:49:44 | 12:52:24 | 12:55:04 | 12:57:44 | 13:00:24 | 13:03:04 | 13:05:44 | 13:08:24 | 13:11:04 | 13:13:44 | 13:16:24 | 13:19:04 | 13:21:44 | 13:24:24 | 13:27:04 | 13:29:44 | 13:32:24 | 13:35:04 | 13:37:44 | 13:40:24 | 13:43:04 | 13:45:44 | 13:48:24 | 13:51:04 | 13:53:44 | 13:56:24 | 13:59:04 | 14:01:44 | 14:04:24 | 14:07:04 | 14:09:44 | 14:12:24 | 14:15:04 | 14:17:44 | 14:20:24 | 14:23:04 | 14:25:44 | 14:28:24 | 14:31:04 | 14:33:44 | 14:36:24 | 14:39:04 | 14:41:44 | 14:44:24 | 14:47:04 | 14:49:44 | 14:52:24 | 14:55:04 | 14:57:44 | 15:00:24 | 15:03:04 | 15:05:44 | 15:08:24 | 15:11:04 | 15:13:44 | 15:16:24 | 15:19:04 | 15:21:44 | 15:24:24 | 15:27:04 | 15:29:44 | 15:32:24 | 15:35:04 | 15:37:44 | 15:40:24 | 15:43:04 | 15:45:44 | 15:48:24 | 15:51:04 | 15:53:44 | 15:56:24 | 15:59:04 | 16:01:44 | 16:04:24 | 16:07:04 | 16:09:44 | 16:12:24 | 16:15:04 | 16:17:44 | 16:20:24 | 16:23:04 | 16:25:44 | 16:28:24 | 16:31:04 | 16:33:44 | 16:36:24 | 16:39:04 | 16:41:44 | 16:44:24 | 16:47:04 | 16:49:44 | 16:52:24 | 16:55:04 | 16:57:44 | 17:00:24 | 17:03:04 | 17:05:44 | 17:08:24 | 17:11:04 | 17:13:44 | 17:16:24 | 17:19:04 | 17:21:44 | 17:24:24 | 17:27:04 | 17:29:44 | 17:32:24 | 17:35:04 | 17:37:44 | 17:40:24 | 17:43:04 | 17:45:44 | 17:48:24 | 17:51:04 | 17:53:44 | 17:56:24 | 17:59:04 | 18:01:44 | 18:04:24 | 18:07:04 | 18:09:44 | 18:12:24 | 18:15:04 | 18:17:44 | 18:20:24 | 18:23:04 | 18:25:44 | 18:28:24 | 18:31:04 | 18:33:44 | 18:36:24 | 18:39:04 | 18:41:44 | 18:44:24 | 18:47:04 | 18:49:34 | 18:51:14 | 18:53:34 | 18:56:14
#REF! | 1
Used SNS RFQ temperature ramping profile & the total braze cycle: is 32 hours; Temperature difference between the part and clamps is within  3 degrees

## Slide 8: Formed Cutter & Full Length Vane
Formed cutter
  Sample part with modulation made by IMP was measured at LBNL  Good profile
A full length vane was machined at IMP

## Slide 9: Module RF Simulations at LBNL
To validate the RF simulation results by Romanov, ANSYS code was used to perform RF simulations on RFQ geometry for Modules 1, 3, & 4 with magnetic BC on one end, not the full RFQ length
  Module 1: Cutbacks (entrance), radial matcher, slug tuners, Pi-rods
  Module 2&3: slug tuners, Pi-rods
  Module 4: Cutbacks (exit), slug tuners, Pi-rods
  For the RF simulations, the model does not have vane modulations
The ANSYS simulations done by Andrew Lambert

## Slide 10: Module 1
Vacuum geometry is one quadrant and contains
  Slug Tuners
  Pi-Rods
  Cutbacks
  Radial Matcher

## Slide 11: Electric Field Flatness of Module 1
Field is flat within 8-9%
Some level of noise due numerical simulation and interpolation
Frequency = 159.5 MHz

## Slide 12: Electric Field Flatness of Module 3
Zoomed in portion of the plot shows noise more clearly
Not considering large peaks, the field is still flat within 3-4%
Frequency = 162.0 MHz
Finer meshes

## Slide 13: Electric Field Flatness of Module 4
Coarse meshes
Field is flat within 8-9%
Frequency = 162.1 MHz