## Slide 1: LFA wire max tension studies
Sotiris Vlachos

## Slide 2: Equipment used
IMADA tension measurement system @ DL (used for qualifying wire spools)
NB : Amateur setup, simple models, gros assumptions !

## Slide 3: Measurement of samples from a single LFA spool
Spool #1 – 26.9N
Spool #5 – 28.5N (less statistics)

## Slide 4: Home made adaptor
To study maximum wire tension
of wires that are not straight

## Slide 5: Wire over board

## Slide 6: Bend wire measurements
Straight wire – 28.5N
Bent 90deg – 27.3N

## Slide 7: Bend wire strength study

## Slide 8: Bend wire strength
Green line is a simple model based on component forces (1/cos(theta))
Red Point : bent over comb
VERY ROUGH angle estimates
NB: not scientific result!
(rigidity of equipment not estimated, point of deflection is not rigid etc)

## Slide 9: Strength of wire with kink
24 ± 0.8 N
Instead of 27 ± 0.5 for straight wire

## Slide 10: Conclusions….
Wire tension of a spool has a std of ~0.2N.
2 to 3 measurements should give a good estimate
Straight or over coverboards etc :
~1N less strength
A few degrees of deflection
do not weaken the wire
Wires with kinks should be replaced