## Slide 1: Measured RRR in MQXFA08b magnet
Maria Baldini

## Slide 2: MQXFA08b cables: RRR estimations
conductor OST 108-127
Both Minor edge extracted sample and rolled samples were used to estimate RRR of the coil
Maximum coil to ground voltage at quench with ordering: 353 V (EDMS 1963398, Us-HiLumi Docdb 879)
COIL | RRR (rolled) | RRR (minor edge)
126 | 252.4 | 324
128 | 210.7 | 286.2
219 | 197.15 | 220
215 | 259.95 | 306.4

## Slide 3: MQXFA08b

## Slide 4: Cold Resistance data

## Slide 5: Measured RRR vs estimated

## Slide 6: Measured RRR in MQXFA14b magnet
Maria Baldini

## Slide 7: MQXFA14b cables: RRR estimations
conductor OST 108-127
Both Minor edge extracted sample and rolled samples were used to estimate RRR of the coil
Maximum coil to ground voltage at quench with ordering: 353 V (EDMS 1963398, Us-HiLumi Docdb 879)
COIL | RRR rolled | RRR minor edge
217 | 261.3 | 273
143 | 192.8 | 236.6
230 | 198.7 | 237.2
231 | 253.2 | 238.4

## Slide 8: MQXFA14b

## Slide 9: Cold Resistance data

## Slide 10: Cold temperature resistance

## Slide 11: Measured RRR vs estimated