## Slide 1: Lessons Learned from MQXFA13 Vertical Test
Paolo Ferracin, G. Ambrosio, Dan Cheng, Laura Garcia Fajardo, Giorgio Vallone
on behalf of the MQXF collaboration
PMG Meeting #54
LBNL, USA
September 19th, 2023

## Slide 2: Outline
A13 Test results
A13 coil dimensions
Finite element analysis of A13
Action items

## Slide 3: A13 test results

## Slide 4: A13 test results

## Slide 5: A13 test results
Many of A13 quenches in the same location (according to quench antenna) as the A07/A08 limiting quenches

## Slide 6: Outline
A13 Test results
A13 coil dimensions
Finite element analysis of A13
Action items

## Slide 7: Arc length excess

## Slide 8: A13 coil size (unshimmed and shimmed)

## Slide 9: A13 coil size (shimmed including ends)
Significant reduction of coil size in the ends
  Visible in all magnets

## Slide 10: Summary Coil radial (shimmed) deviation and key/shim size
In A13, small coils and small loading shim
 | Ave ss | LE min | RE min | Key | Shim | Shim | Ave ss + shim | LE + shim | RE + shim
 | mm | mm | mm | mm | mils | mm | mm | mm | mm
A14b | -0.007 | -0.129 | -0.106 | 13.84 | 43 | 1.092 | 1.085 | 0.963 | 0.986
A13 | -0.004 | -0.146 | -0.094 | 13.72 | 38 | 0.965 | 0.961 | 0.819 | 0.871
A8b | -0.001 | -0.181 | -0.136 | 13.77 | 40 | 1.016 | 1.015 | 0.835 | 0.880
A11 | 0.004 | -0.125 | -0.047 | 13.74 | 39 | 0.991 | 0.995 | 0.866 | 0.944
A10 | -0.092 | -0.222 | -0.199 | 13.82 | 42 | 1.067 | 0.975 | 0.845 | 0.868
A8 | -0.029 | -0.216 | -0.171 | 13.72 | 38 | 0.965 | 0.936 | 0.749 | 0.794
A7 | -0.035 | -0.139 | -0.114 | 13.77 | 40 | 1.016 | 0.981 | 0.877 | 0.902
A6 | -0.046 | -0.138 | -0.178 | 13.72 | 38 | 0.965 | 0.919 | 0.827 | 0.787
A5 | -0.024 | -0.153 | -0.105 | 13.79 | 41 | 1.041 | 1.017 | 0.888 | 0.936

## Slide 11: Outline
A13 Test results
A13 coil dimensions
Finite element analysis of A13
Action items

## Slide 12: Finite element model assumption
Study of the impact of the coil pack size on the coil strain
  in particular in the ‘wedge/end-spacer transition’ region
Contact
Offset

## Slide 13: Peak Strain as a function of the pre-stress
Strain increases reducing the azimuthal prestress at R.T.
Two critical locations:
  Pole turn:
    Real peak might be lower because of some remaining pole turn bonding
  Wedge/endspacer transition
    Peak might be significantly higher due to the discontinuity (after a gap opens), not fully captured by the FE model
A13 - 50 MPa
A13 - 80 MPa
A13 - 100 MPa
Transition
Pole Turn

## Slide 14: Peak Strain as a function of the straight section pre-stress
The peak strain is a function of the applied prestress
Effect on max strain on the transition seems similar:
  A13 requires higher room temperature prestress to keep the strain below the ‘knee’

## Slide 15: Peak Strain as a function of the local pre-stress
Pole stress at cold computed on the same z location of the wedge/end-spacer transition
  Blue/magenta lines represent end-region modifications
  All the points are on the same lines!
The effect seems to be controlled by a local prestress loss

## Slide 16: Conclusions finite element analysis
The size variation of the coil can significantly increase the longitudinal strain in the ends
  This effect is due to a local prestress loss in the end region
Possible solutions:
  Increase the prestress everywhere in the coil
    Might not respect established limits
  Local prestress modifiers (e.g. different keys in the ends)
    Currently under investigation

## Slide 17: Outline
A13 Test results
A13 coil dimensions
Finite element analysis of A13
Action items

## Slide 18: Action items
Before magnet assembly/loading
  Include analysis of coil size in the ends and expected coil pre-stress in the ends to ensure sufficient azimuthal pre-stress everywhere
    Approach validated with A14b
Determine pre-load shim size based on values from A14b and A05 (best performing magnets so far)
During pre-load, target shim size, and monitor SG and fiber optics to ensure that stress limits are not passed
  Maximum allowed peak stress increased from 110 to 120 MPa
In parallel, investigation with FEM of variable size loading shims (thicker in the ends)

## Slide 19: Example from A16 loading and shim review (Aug 24th)

## Slide 20: Appendix

## Slide 21: Possible pre-load criteria
The peak strain is a function of the applied prestress
  The distance between the red and black line will be different for each coil pack shape
We could define an unique criteria on the required minimum prestress at room temperature
  E.g. limit strain = 0.3%
  For MQXFA13, this would require a prestress of ~92 MPa
  Seems reasonable also looking at the transition peak strain
Maximum
Minimum
Nominal
Minimum

## Slide 22: Finite element results
Peak longitudinal strain increases from 2249 µm/m to 2893 µm/m
5 MPa reduction on peak pressure
Slightly larger debonded region

## Slide 23: A13 pre-stress in the ends
A13 prestress is much less uniform
Significant prestress loss in the end region both at room temperature and after cooldown
Measurable difference on the shell stress at warm and at cold
  Could add a sensor….

## Slide 24: A14b quench performance, shimmed coil size, shell size, and loading key size
Loading shim size: 43 mils, 1.092 mm
Total key size: 13.84 mm

## Slide 25: A13 quench performance, shimmed coil size, shell size, and loading key size
Loading shim size: 38 mils, 0.965 mm
Total key size: 13.72 mm

## Slide 26: A05 quench performance, shimmed coil size, shell size, and loading key size
Loading shim size: 41 mils, 1.041 mm
Total key size: 13.79 mm

## Slide 27: Summary A14b, A05, A13
Loading shim size: 43 mils, 1.092 mm
Total key size: 13.84 mm
Loading shim size: 38 mils, 0.965 mm
Total key size: 13.72 mm
Loading shim size: 41 mils, 1.041 mm
Total key size: 13.79 mm