## Slide 1: MQXFA17 & 13b Magnets 302.2.02 and 03 – • Strand Procurement & Testing • Cable Fabrication & Testing
Lance Cooley – NHMFL/ASC (302.2.02 L3)
Vito Lombardo – FNAL (302.2.02 CAM)
Ian Pong – LBNL (302.2.03 L3 & CAM)
Mike Naus – LBNL (302.2.03 L3 Deputy & CAM Deputy)
Elizabeth Lee – LBNL
Jonathan Lee – LBNL Intern Student (now Grad Student at NHMFL)

## Slide 2: Cable & Coil Overview
All cables are 2nd generation QXF cables produced under AUP
Coil # | Cable #
150 | P43OL1186
151 | P43OL1190
152 | P43OL1193
237 | P43OL1182
239 | P43OL1184
242 | P43OL1189

## Slide 3: Cable QC Summary
All cables passed the required quality control testing per US-HiLumi-Doc 74
There were No Critical DRs

## Slide 4: Cable 1186 (Coil 150) DR Detail: 3 DRs

## Slide 5: QXFA-150 / P43OL1186: RRR Heat Treat
DR #12736 (1 of 3)
Issue: Range across all 7 sample TCs outside ±1°C window at 210°C
  Measured Range: 2.3°C Allowed Range: 2.0°C
Cause: TCs calibrated at/between 400°C & 665°C.
  Not expected to be fully accurate at 210°C
Acceptance Justification
  Heat Treatment witness wires’ RRR values were within historical norms (both encapsulated & unencapsulated samples)
  Averaged plateau temperature was within ±1°C of target
  210°C the least impactful to RRR of all plateaus

## Slide 6: QXFA-150 / P43OL1186: Insulation Mfg Data
Issue: Insulation run-log data missing for last 85 m of cable
Cause: Operator unplugged computer; could not restart logging function
Acceptance Justification
  Vision system continued to run normally
    No defects seen
    No automatic process stops
  No visible defects noted by operator(s)
DR #12749 (2 of 3)

## Slide 7: QXFA-150 / P43OL1186: Cabling Machine Stopped
Issue: Cabling machine was momentarily stopped at 7th meter
Cause: Difficulty feeding cable starting end through CME measurement head.
Acceptance Justification
  7th meter will be in the discarded “cable drop” section
DR #12753 (3 of 3)

## Slide 8: Cable 1190 (Coil 151) DR Detail: 3 DRs

## Slide 9: QXFA-151/ P43OL1190: In-Process Thickness
Issue: One in-process thickness measurement above spec (CME) within 1st meter of cable
Cause:
  Cables often started on the thick side in order to be on target for most of run
  Measurement noise is greater close to cut end of cable
Acceptance Justification
  OOS value in to-be-discarded “cable drop” section
DR #12910 (1 of 3)

## Slide 10: QXFA-151/ P43OL1190: Ic Measurement Issue
Issue: 1 of 3 primary Ic strands was not able to be measured.
Cause: Unknown. Believed to be sample mounting issue.
Acceptance Justification
  Back-up sample successfully measured and acceptable, thus meeting the requirement
DR #12922 (2 of 3)

## Slide 11: QXFA-151/ P43OL1190: Bad Accelerometer Data
Issue: Shipping accelerometers had data integrity issues
  Accelerometer-1 only recorded data LBNL-NEWT, not NEWT‑FNAL
  Accelerometer-1 had higher tilt & vibration instances than normal
  Accelerometer-2 didn’t record any data
Cause: Believed to be…
  Memories not cleared before shipment
  Rough handling from shipping company
Acceptance Justification
  Use as-is. Low probability of issues.
  Cables will be inspected during winding
DR #12904 (3 of 3)
[Same issue and DR as Cable 1189]

## Slide 12: Cable 1193 (Coil 152) DR Detail: 2 DRs

## Slide 13: QXFA-152/ P43OL1193: RRR Heat Treat TCs
Issue: Incorrect temperature measurement for first 33 hours of 210°C plateau
Cause:
  Thermocouples plugged into incorrect data logger ports/jacks
Acceptance Justification
  Valid data from last 15 hours was within spec
  No unusual temperature excursions during entirety of 210C run
  Total during confirmed to be 48.2 h [Spec: 48 h ± 2 h]
  Same furnace setpoints from previous run, which was within spec
  210°C plateau the least impactful of the 3 HT plateaus
DR #12896 (1 of 2)

## Slide 14: QXFA-152/ P43OL1193: No Core Detector
Issue: Core detector inoperable during cable manufacture
Cause: PCB failure within core detector box
Acceptance Justification
  Difference in core spool weight pre- and post-run is consistent with that expected
  Core was visually monitored sporadically during the run
DR #12912 (2 of 2)

## Slide 15: Cable 1182 (Coil 237) DR Detail: 4 DRs

## Slide 16: QXFA-237/ P43OL1182: RRR Heat Treatment
Issue: Range across all 7 sample TCs outside ±1°C window at 210°C
  Measured Range: 2.1°C Allowed Range: 2.0°C
Cause: TCs calibrated at/between 400°C & 665°C.
  Not expected to be fully accurate at 210°C
Acceptance Justification
  Heat Treatment witness wires’ RRR values were within historical norms (both encapsulated & unencapsulated samples)
  Averaged plateau temperature was within ±1°C of target
  210°C the least impactful to RRR of all plateaus
DR #12618 (1 of 4)
[Same HT and DR as cable (1184)]

## Slide 17: QXFA-237/ P43OL1182: Thin Insulation
Issue: Insulation verification 10-stack below spec by 1.4µm at 5 MPa
Cause: Suspect excessive verification sample coiling for shipment to LBNL created extra tension on insulation
Acceptance Justification: Vendor’s data is passing
DR #12651 (2 of 4)

## Slide 18: QXFA-237/ P43OL1182: Excess Lubricant
Issue: Excess residual 4BR cabling lubricant within cable
Cause: Changes to lubrication equipment and intentional increased 4BR usage rate
  Attempt to mitigate facet divergence
Acceptance Justification:
  4BR is not known to adversely affect cable quality
  4BR is expected to volatilize away eventually
DR #12564 (3 of 4)

## Slide 19: QXFA-237/ P43OL1182: No Core Detector
Issue: Core detector inoperable during cable manufacture e
Cause: Battery had died. Unable to replace.
Acceptance Justification:
  Difference in core spool weight pre- and post-run is consistent with that expected
  Core was visually monitored sporadically during the run
DR #12608 (4 of 4)

## Slide 20: Cable 1184 (Coil 239) DR Detail: 2 DRs

## Slide 21: QXFA-239/ P43OL1184: In-Process Thickness
DR #12609 (1 of 2)
Issue: One in-process thickness measurement above spec (CME) within first 2 meters of cable
Cause:
  Cables often started on the thick side in order to be on target for most of run
  Measurement noise is greater close to cut end of cable
Acceptance Justification
  OOS value in to-be-discarded “cable drop” section

## Slide 22: QXFA-239/ P43OL1184: RRR Heat Treatment
Issue: Range across all 7 sample TCs outside ±1°C window at 210°C
  Measured Range: 2.1°C Allowed Range: 2.0°C
Cause: TCs calibrated at/between 400°C & 665°C.
  Not expected to be fully accurate at 210°C
Acceptance Justification
  Heat Treatment witness wires’ RRR values were within historical norms (both encapsulated & unencapsulated samples)
  Averaged plateau temperature was within ±1°C of target
  210°C the least impactful to RRR of all plateaus
DR #12618 (2 of 2)
[Same HT and DR as previous cable (1182)]

## Slide 23: Cable 1189 (Coil 242) DR Detail: 1 DR

## Slide 24: QXFA-242/ P43OL1189: Bad Accelerometer Data
Issue: Shipping accelerometers had data integrity issues
  Accelerometer-1 only recorded data LBNL-NEWT, not NEWT‑FNAL.
  Accelerometer-1 had higher tilt & vibration instances than normal
  Accelerometer-2 didn’t record any data.
Cause: Believed to be…
  Memories not cleared before shipment
  Rough handling from shipping company
Acceptance Justification
  Use as-is. Low probability of issues.
  Cables will be inspected during winding
DR #12904 (1 of 1)
[Same issue and DR as previous Cable 1190]

## Slide 25: END [Back-Up Slides Below]

## Slide 26: Strand Summary
All strands ordered per the “HiLumi” specification under the AUP program, per the following POs:
  FNAL PO 646116 SA1 Shipment E
  FNAL PO 667037 Shipments: A, B1, B2, C, and D
Conductor Description:
  Ø0.85 mm, 108/127 stack, Ti-doped, Reduced-Sn core

## Slide 27
Both 665°C/75h
S: 665°C/50h
V: 665°/75h
Both 665°C/50h
Strand Production Data – Ic, 15T
Yellow boxes indicate strand data for these cables

## Slide 28
Both 665°C/75h
S: 665°C/50h
V: 665°/75h
Both 665°C/50h
Strand Production Data – Ic, 12T
Yellow boxes indicate strand data for these cables

## Slide 29: Strand Production Data - RRR
Data for 15% rolled strand predicts the RRR at cable sharp bend
Lab: IEC method, Supplier: 20K method
Inter-lab comparisons have validated approaches (see QP)
Yellow boxes indicate strand data for these cables

## Slide 30: QXFA-150 / P43OL1186

## Slide 31: P43OL1186 – Cable Date, Lengths
Cable Manufacture Date
  03 Feb 2022 (Production run)
Cable Length:
  464 m (LBNL, fabricated, including LBNL samples)

## Slide 32: P43OL1186 – Strand and SS Core ID
Spool:
  PO08S00516A04U x 5 ULs
  PO08S00673A03U x 1 ULs
  PO08S00673A01U x 4 ULs
  PO08S00673A02U x 11 ULs
  PO08S00674A01U x 19 ULs
Core:
  120L37A7400804
    Heat: 850858. Lot: 17-521
    Material: 316L
    Chemical Properties CoT/CoC #172660-1: 0.16 wt% Co
    Core width: 12.0 mm
From 3 billets

## Slide 33: P43OL1186 Respooling Wire Diameter
Below LSL: 0.001%
Above USL: 0.139%

## Slide 34: P43OL1186 – Cable QC Data Summary
CME:
Residual Twist: 145°
10-stack:
  Qualification: 1.537 mm
  Production tail end: 1.528 mm
 | Pressure (MPa) | Angle (°) | Width (mm) | Thickness (mm)
Maximum | 17.0 | 0.394 | 18.177 | 1.533
Average | 17.0 | 0.367 | 18.144 | 1.522
Minimum | 16.9 | 0.328 | 18.138 | 1.517
Sigma | 0.01 | 0.011 | 0.004 | 0.002

## Slide 35
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 36
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 37
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 38: P43OL1186 – Braiding
Fiberglass Lot: #RCV0011562
P/I: 18.9
Spool tension: 10 lbs. @ payoff. 20 lbs. @ takeup (12 lbs min)
Bobbin payoff tension: 0.125 lbs. ≤ T ≤ 0.250 lbs.
Site | Cycle #1 (mm) | Cycle #2 (mm) | Cycle #3 (mm) | Average (mm)
NEWT | 0.147 | 0.145 | 0.144 | 0.145
LBNL Verification | 0.148 | 0.146 | 0.145 | 0.146
Insulation Thickness (at 5 MPa)

## Slide 39: P43OL1186 – Wire Parameters
Properties | Inspected Average
Wire Diameter | 0.8506 ± 0.0006 mm (LBNL)1
Cu ratio a | 54.19% (BOST)
Strand twist pitch a | 18.9 mm (BOST)
RRR (RW) a | 301 (BOST)
RRR (15% rolled) a | 188 (BOST)
IC (4.2 K, 15 T) a | 379 A (BOST)
IC (4.2 K, 14 T) a | 474 A (BOST)
IC (4.2 K, 13 T) a | 580 A (BOST)
IC (4.2 K, 12 T) a | 702 A (BOST)
a First billet averaged, then weighted average according to the spool distribution in the cable
1 As-received. LBNL respooling data. Mean ± 1 sigma

## Slide 40: P43OL1186 – Wire Parameters Supplier (S) and Verification (V) IC Data
Number of spools from that billet used in the cable

## Slide 41: P43OL1186 – Wire Parameters Supplier (S) and Verification (V) RRR Data
Number of spools from that billet used in the cable

## Slide 42: P43OL1186 – Extracted Strand RRR
Cable ID | No. of Units from Billet (spool) | Heat Treat/ Sample ID | Major Edge RRR | Minor Edge RRR | Straight 1 RRR | Straight 2 RRR
PO08S00516A04U P43OL1186AE05E | 5 (5) | LRLK220208ALC1 | 305 | 296 | 390 | 407
PO08S00673A01U P43OL1186AE11E | 16 (4) | LRLK220208ALC1 | 277 | 267 | 331 | 340
PO08S00673A02U P43OL1186AE17E | 16 (11) | LRLK220208ALC1 | 260 | 259 | 330 | 321
PO08S00674A01U P43OL1186AE33E | 19 (19) | LRLK220208ALC1 | 245 | 220 | 295 | 308
PO08S00674A01U P43OL1186AE35E | 19 (19) | LRLK220208ALC1 | 273 | 257 | 321 | 344

## Slide 43: P43OL1186 – Ic, Cable Qual Samples
Wire/ Cable Strand | Ic(A) at Field (T) |  |  | 
 | 12 T | 13 T | 14 T | 15 T
PO08S00674A01U P43OL1186AE33E | 693 | 577 | 474 | 381
PO08S00673A02U P43OL1186AE17E | 679 | 566 | 460 | 367
PO08S00516A04U P43OL1186AE03E | 710 | 591 | 485 | 392

## Slide 44: P43OL1186 – SSL Plot, Cable Qual Samples

## Slide 45: P43OL1186 – SSL Margins, Qual Samples
Strand from which Margin is Calculated: | Strand # 17E @ 1.9 K
Margins | Margin | Operating Point (X)
Load Line Margin (Purple Arrow) | 26.6% | 73.4%
Current Margin (Green Arrow) | 62.6% | 37.4%
Temperature Margin (K) | 5.4 | 7.3
Limits | Strand | Strand x 40
Selected Strand Current (A) at Margin-Calculation Field | 1083.7 | 43348.2
Selected Strand Current (A) at 100% SSL | 553.1 | 22125.0
Selected Strand Field (T) at 100% SSL | 15.04 | 

## Slide 46: QXFA-151 / P43OL1190

## Slide 47: P43OL1190 – Cable Date, Lengths
Cable Manufacture Date
  31 Mar 2022(Production run)
Cable Length:
  468 m (LBNL, fabricated, including LBNL samples)

## Slide 48: P43OL1190 – Strand and SS Core ID
Spool:
  PO08S00657A01U x 6 ULs
  PO08S00657A03U x 5 ULs
  PO08S00660A02U x 11 ULs
  PO08S00661A01U x 2 ULs
  PO08S00661A02U x 7 ULs
  PO08S00661A03U x 9 ULs
Core:
  120L41A7400804
    Heat: 850858. Lot: 17-521
    Material: 316L
    Chemical Properties CoT/CoC #172660-1: 0.16 wt% Co
    Core width: 12.0 mm
From 3 billets

## Slide 49: P43OL1190 Respooling Wire Diameter
Below LSL: 0.001%
Above USL: 0.008%

## Slide 50: P43OL1190 – Cable QC Data Summary
CME:
Residual Twist: 125°
10-stack:
  Qualification: 1.540 mm
  Production tail end: 1.529 mm
 | Pressure (MPa) | Angle (°) | Width (mm) | Thickness (mm)
Maximum | 17.4 | 0.392 | 18.146 | 1.536
Average | 16.7 | 0.359 | 18.133 | 1.524
Minimum | 16.7 | 0.341 | 18.128 | 1.520
Sigma | 0.10 | 0.006 | 0.003 | 0.002

## Slide 51
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 52
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 53
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 54: P43OL1190 – Braiding
Fiberglass Lot: #RCV0011562
P/I: 18.9
Spool tension: 10 lbs. @ payoff. 20 lbs. @ takeup (12 lbs min)
Bobbin payoff tension: 0.125 lbs. ≤ T ≤ 0.250 lbs.
Site | Cycle #1 (mm) | Cycle #2 (mm) | Cycle #3 (mm) | Average (mm)
NEWT | 0.151 | 0.148 | 0.146 | 0.148
LBNL Verification | 0.151 | 0.148 | 0.146 | 0.148
Insulation Thickness (at 5 MPa)

## Slide 55: P43OL1190 – Wire Parameters
Properties | Inspected Average
Wire Diameter | 0.8509 ± 0.001 mm (LBNL)1
Cu ratio a | 54.32% (BOST)
Strand twist pitch a | 19.7 mm (BOST)
RRR (RW) a | 292 (BOST)
RRR (15% rolled) a | 192 (BOST)
IC (4.2 K, 15 T) a | 366 A (BOST)
IC (4.2 K, 14 T) a | 458 A (BOST)
IC (4.2 K, 13 T) a | 563 A (BOST)
IC (4.2 K, 12 T) a | 683 A (BOST)
a First billet averaged, then weighted average according to the spool distribution in the cable
1 As-received. LBNL respooling data. Mean ± 1 sigma

## Slide 56: P43OL1190 – Wire Parameters Supplier (S) and Verification (V) IC Data
Number of spools from that billet used in the cable

## Slide 57: P43OL1190 – Wire Parameters Supplier (S) and Verification (V) RRR Data
Number of spools from that billet used in the cable

## Slide 58: P43OL1190 – Extracted Strand RRR
Cable ID | No. of Units from Billet (spool) | Heat Treat/ Sample ID | Major Edge RRR | Minor Edge RRR | Straight 1 RRR | Straight 2 RRR
PO08S00657A01U P43OL1190AE03E | 11 (6) | LRLK220420ALC1 | 234 | 232 | 296 | 308
PO08S00657A03U P43OL1190AE11E | 11 (5) | LRLK220420ALC1 | 283 | 267 | 328 | 354
PO08S00660A02U P43OL1190AE18E | 11 (11) | LRLK220420ALC1 | 283 | 287 | 353 | 368
PO08S00661A02U P43OL1190AE37E | 18 (7) | LRLK220420ALC1 | 242 | 231 | 271 | 278
PO08S00661A03U P43OL1190AE48E | #N/A | LRLK220420ALC1 | 247 | 245 | 310 | 312

## Slide 59: P43OL1190 – Ic, Cable Qual Samples
Wire/ Cable Strand | Ic(A) at Field (T) |  |  | 
 | 12 T | 13 T | 14 T | 15 T
PO08S00661A03U P43OL1190AE48E | 665 | 552 | 449 | 361
PO08S00661A02U P43OL1190AE37E | 663 | 549 | 447 | 358
PO08S00660A02U P43OL1190AE19E | 639 | 523 | 425 | 338

## Slide 60: P43OL1190 – SSL Plot, Cable Qual Samples

## Slide 61: P43OL1190 – SSL Margins, Qual Samples
Strand from which Margin is Calculated: | Strand # 19E @ 1.9 K
Margins | Margin | Operating Point (X)
Load Line Margin (Purple Arrow) | 25.1% | 74.9%
Current Margin (Green Arrow) | 60.2% | 39.8%
Temperature Margin (K) | 5.2 | 7.1
Limits | Strand | Strand x 40
Selected Strand Current (A) at Margin-Calculation Field | 1020.3 | 40811.6
Selected Strand Current (A) at 100% SSL | 541.7 | 21669.5
Selected Strand Field (T) at 100% SSL | 14.75 | 

## Slide 62: QXFA-152 / P43OL1193

## Slide 63: P43OL1193 – Cable Date, Lengths
Cable Manufacture Date
  03 May 2022(Production run)
Cable Length:
  468 m (LBNL, fabricated, including LBNL samples)

## Slide 64: P43OL1193 – Strand and SS Core ID
Spool:
  PO08S00641A01U x 17 ULs
  PO08S00675A02U x 9 ULs
  PO08S00688A01U x 14 ULs
Core:
  120L44A7400804
    Heat: 850858. Lot: 17-521
    Material: 316L
    Chemical Properties CoT/CoC #187781-1: 0.16 wt% Co
    Core width: 12.0 mm
From 3 billets

## Slide 65: P43OL1193 Respooling Wire Diameter
Below LSL: 0.007%
Above USL: 0.008%

## Slide 66: P43OL1193 – Cable QC Data Summary
CME:
Residual Twist: 140°
10-stack:
  Qualification: 1.541 mm
  Production tail end: 1.527 mm
 | Pressure (MPa) | Angle (°) | Width (mm) | Thickness (mm)
Maximum | 17.2 | 0.388 | 18.160 | 1.532
Average | 16.8 | 0.367 | 18.140 | 1.522
Minimum | 16.7 | 0.339 | 18.136 | 1.518
Sigma | 0.06 | 0.007 | 0.002 | 0.002

## Slide 67
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 68
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 69
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 70: P43OL1193 – Braiding
Fiberglass Lot: #11562
P/I: 18.9
Spool tension: 10 lbs. @ payoff. 20 lbs. @ takeup (12 lbs min)
Bobbin payoff tension: 0.125 lbs. ≤ T ≤ 0.250 lbs.
Site | Cycle #1 (mm) | Cycle #2 (mm) | Cycle #3 (mm) | Average (mm)
NEWT | 0.149 | 0.147 | 0.146 | 0.148
LBNL Verification | 0.150 | 0.147 | 0.145 | 0.147
Insulation Thickness (at 5 MPa)

## Slide 71: P43OL1193 – Wire Parameters
Properties | Inspected Average
Wire Diameter | 0.8506 ± 0.0007 (LBNL)1
Cu ratio a | 53.86% (BOST)
Strand twist pitch a | 19.5mm (BOST)
RRR (RW) a | 306 (BOST)
RRR (15% rolled) a | 229 (BOST)
IC (4.2 K, 15 T) a | 366 A (BOST)
IC (4.2 K, 14 T) a | 459 A (BOST)
IC (4.2 K, 13 T) a | 563 A (BOST)
IC (4.2 K, 12 T) a | 685 A (BOST)
a First billet averaged, then weighted average according to the spool distribution in the cable
1 As-received. LBNL respooling data. Mean ± 1 sigma

## Slide 72: P43OL1193 – Wire Parameters Supplier (S) and Verification (V) IC Data
Number of spools from that billet used in the cable
Some verification data not available

## Slide 73: P43OL1193 – Wire Parameters Supplier (S) and Verification (V) RRR Data
Number of spools from that billet used in the cable
Some verification data not available

## Slide 74: P43OL1193 – Extracted Strand RRR
Cable ID | No. of Units from Billet (spool) | Heat Treat/ Sample ID | Major Edge RRR | Minor Edge RRR | Straight 1 RRR | Straight 2 RRR
PO08S00641A01U P43OL1193AE03E | 17 (17) | LRLK220523ALC1 | 277 | 251 | 315 | 321
PO08S00641A01U P43OL1193AE05E | 17 (17) | LRLK220523ALC1 | 287 | 280 | 347 | 355
PO08S00675A02U P43OL1193AE27E | 9 (9) | LRLK220523ALC1 | 261 | 251 | 320 | 324
PO08S00688A01U P43OL1193AE41E | 14 (14) | LRLK220523ALC1 | 291 | 270 | 338 | 339
PO08S00688A01U P43OL1193AE42E | 14 (14) | LRLK220523ALC1 | 276 | 283 | 341 | 331

## Slide 75: P43OL1193 – Ic, Cable Qual Samples
Wire/ Cable Strand | Ic(A) at Field (T) |  |  | 
 | 12 T | 13 T | 14 T | 15 T
PO08S00641A01U P43OL1193AE01E | 652 | 535 | 430 | 341
PO08S00688A01U P43OL1193AE41E | 669 | 554 | 449 | 363
PO08S00675A02U P43OL1193AE27E | 660 | 549 | 444 | 360
PO08S00641A01U P43OL1193AE03E | 672 | 555 | 451 | 359

## Slide 76: P43OL1193 – SSL Plot, Cable Qual Samples

## Slide 77: P43OL1193 – SSL Margins, Qual Samples
Strand from which Margin is Calculated: | Strand # 27E @ 1.9 K
Margins | Margin | Operating Point (X)
Load Line Margin (Purple Arrow) | 26.0% | 74.0%
Current Margin (Green Arrow) | 61.2% | 38.8%
Temperature Margin (K) | 5.3 | 7.2
Limits | Strand | Strand x 40
Selected Strand Current (A) at Margin-Calculation Field | 1045.4 | 41817.0
Selected Strand Current (A) at 100% SSL | 548.5 | 21941.9
Selected Strand Field (T) at 100% SSL | 14.93 | 

## Slide 78: QXFA-237 / P43OL1182

## Slide 79: P43OL1182 – Cable Date, Lengths
Cable Manufacture Date
  22 Sept 2021 (Production run)
Cable Length:
  467 m (LBNL, fabricated, including LBNL samples)

## Slide 80: P43OL1182 – Strand and SS Core ID
Spool:
  PO08S00649A03U x 9 ULs
  PO08S00656A01U x 2 ULs
  PO08S00656A02U x 15 Uls
  PO08S00659A02U x 14 ULs
Core:
  120L33A7400804
    Heat: 85058. Lot: 17-521
    Material: 316L
    Chemical Properties CoT/CoC #187781-1: 0.158 wt% Co
    Core width: 12.0 mm
From 3 billets

## Slide 81: P43OL1182 Respooling Wire Diameter
Below LSL: 0.000%
Above USL: 0.001%

## Slide 82: P43OL1182 – Cable QC Data Summary
CME:
Residual Twist: 125°
10-stack:
  Qualification: 1.537 mm
  Production tail end: 1.526 mm
 | Pressure (MPa) | Angle (°) | Width (mm) | Thickness (mm)
Maximum | 17.0 | 0.375 | 18.154 | 1.535
Average | 17.0 | 0.359 | 18.144 | 1.523
Minimum | 17.0 | 0.337 | 18.139 | 1.518
Sigma | 0.01 | 0.007 | 0.002 | 0.003

## Slide 83
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 84
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 85
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 86: P43OL1182 – Braiding
Fiberglass Lot: #111154
P/I: 18.9
Spool tension: 10 lbs. @ payoff. 20 lbs. @ takeup (12 lbs min)
Bobbin payoff tension: 0.125 lbs. ≤ T ≤ 0.250 lbs.
Vector #464342
Site | Cycle #1 (mm) | Cycle #2 (mm) | Cycle #3 (mm) | Average (mm)
NEWT | 0.150 | 0.147 | 0.146 | 0.147
LBNL Verification | 0.140 | 0.138 | 0.137 | 0.139
Insulation Thickness (at 5 MPa)

## Slide 87: P43OL1182 – Wire Parameters
Properties | Inspected Average
Wire Diameter | 0.8509 ± 0.0007 mm (LBNL)1
Cu ratio a | 53.59% (BOST)
Strand twist pitch a | 19.8mm (BOST)
RRR (RW) a | 283 (BOST)
RRR (15% rolled) a | 202 (BOST)
IC (4.2 K, 15 T) a | 363 A (BOST)
IC (4.2 K, 14 T) a | 455 A (BOST)
IC (4.2 K, 13 T) a | 561 A (BOST)
IC (4.2 K, 12 T) a | 682 A (BOST)
a First billet averaged, then weighted average according to the spool distribution in the cable
1 As-received. LBNL respooling data. Mean ± 1 sigma

## Slide 88: P43OL1182 – Wire Parameters Supplier (S) and Verification (V) IC Data
Number of spools from that billet used in the cable

## Slide 89: P43OL1182 – Wire Parameters Supplier (S) and Verification (V) RRR Data
Number of spools from that billet used in the cable

## Slide 90: P43OL1182 – Extracted Strand RRR
 | Cable ID | No. of Units from Billet (spool) | HT/sample ID | Major edge RRR | Minor edge RRR | Straight section 1 RRR | Straight section 2 RRR
ID #1 | PO08S00659A02U P43OL1182AE03E | 14 (14) | LRLK211021ALC1 | 268 | 269 | 332 | 358
ID #2 | PO08S00659A02U P43OL1182AE05E | 14 (14) | LRLK211021ALC1 | 252 | 263 | 319 | 348
ID #3 | PO08S00649A03U P43OL1182AE23E | 9 (9) | LRLK211021ALC1 | 217 | 226 | 269 | 292
ID #4 | PO08S00656A02U P43OL1182AE39E | 17 (15) | LRLK211021ALC1 | 236 | 227 | 281 | 324
ID #5 | PO08S00656A02U P43OL1182AE41E | 17 (15) | LRLK211021ALC1 | 235 | 251 | 300 | 326
Vector #464342

## Slide 91: P43OL1182 – Ic , Cable Qual Samples
Wire/ Cable Strand | Ic(A) at Field (T) |  |  | 
 | 12 T | 13 T | 14 T | 15 T
PO08S00656A02U P43OL1182AE39E | 693 | 574 | 470 | 377
PO08S00659A02U P43OL1182AE01E | 666 | 547 | 445 | 355
PO08S00649A03U P43OL1182AE23E | 690 | 573 | 470 | 377

## Slide 92: P43OL1182 – SSL Plot, Cable Qual Samples

## Slide 93: P43OL1182 – SSL Margins, Qual Samples
Strand from which Margin is Calculated: | Strand # 01E @ 1.9 K
Margins | Margin | Operating Point (X)
Load Line Margin (Purple Arrow) | 26.0% | 74.0%
Current Margin (Green Arrow) | 61.8% | 38.2%
Temperature Margin (K) | 5.3 | 7.2
Limits | Strand | Strand x 40
Selected Strand Current (A) at Margin-Calculation Field | 1063.4 | 42534.8
Selected Strand Current (A) at 100% SSL | 548.5 | 21941.8
Selected Strand Field (T) at 100% SSL | 14.93 | 

## Slide 94: QXFA-239 / P43OL1184

## Slide 95: P43OL1184 – Cable Date, Lengths
Cable Manufacture Date
  12 Oct 2021 (Production run)
Cable Length:
  467 m (LBNL, fabricated, including LBNL samples)

## Slide 96: P43OL1184 – Strand and SS Core ID
Spool:
  PO08S00646A02U x 5 ULs
  PO08S00651A01U x 11 ULs
  PO08S00651A02U x 7 ULs
  PO08S00652A01U x 7 ULs
  PO08S00652A02U x 10 ULs
Core:
  120L35A7400804
    Heat: 85058. Lot: 17-521
    Material: 316L
    Chemical Properties CoT/CoC #187781-1: 0.158 wt% Co
    Core width: 12.0 mm
From 3 billets

## Slide 97: P43OL1184 Respooling Wire Diameter
Below LSL: 0.000%
Above USL: 0.006%

## Slide 98: P43OL1184 – Cable QC Data Summary
CME:
Residual Twist: 140°
10-stack:
  Qualification: 1.536 mm
  Production tail end: 1.530 mm
 | Pressure (MPa) | Angle (°) | Width (mm) | Thickness (mm)
Maximum | 17.1 | 0.381 | 18.160 | 1.536
Average | 17.0 | 0.357 | 18.140 | 1.525
Minimum | 17.0 | 0.339 | 18.133 | 1.520
Sigma | 0.01 | 0.007 | 0.002 | 0.002

## Slide 99
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 100
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 101
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 102: P43OL1184 – Braiding
Fiberglass Lot: #111154
P/I: 18.9
Spool tension: 10 lbs. @ payoff. 20 lbs. @ takeup (12 lbs min)
Bobbin payoff tension: 0.125 lbs. ≤ T ≤ 0.250 lbs.
Vector #464342
Site | Cycle #1 (mm) | Cycle #2 (mm) | Cycle #3 (mm) | Average (mm)
NEWT | 0.148 | 0.147 | 0.146 | 0.147
LBNL Verification | 0.143 | 0.141 | 0.140 | 0.141
Insulation Thickness (at 5 MPa)

## Slide 103: P43OL1184 – Wire Parameters
Properties | Inspected Average
Wire Diameter | 0.8520 ± 0.0007 mm (LBNL)1
Cu ratio a | 54.32% (BOST)
Strand twist pitch a | 19.2mm (BOST)
RRR (RW) a | 269 (BOST)
RRR (15% rolled) a | 182 (BOST)
IC (4.2 K, 15 T) a | 356 A (BOST)
IC (4.2 K, 14 T) a | 448 A (BOST)
IC (4.2 K, 13 T) a | 554 A (BOST)
IC (4.2 K, 12 T) a | 673 A (BOST)
a First billet averaged, then weighted average according to the spool distribution in the cable
1 As-received. LBNL respooling data. Mean ± 1 sigma

## Slide 104: P43OL1184 – Wire Parameters Supplier (S) and Verification (V) IC Data
Number of spools from that billet used in the cable

## Slide 105: P43OL1184 – Wire Parameters Supplier (S) and Verification (V) RRR Data
Number of spools from that billet used in the cable

## Slide 106: P43OL1184 – Extracted Strand RRR
 | Cable ID | No. of Units from Billet (spool) | HT/sample ID | Major edge RRR | Minor edge RRR | Straight section 1 RRR | Straight section 2 RRR
ID #1 | PO08S00646A02U P43OL1184AE03E | 5 (5) | LRLK211021ALC1 | 287 | 265 | 324 | 348
ID #2 | PO08S00651A01U P43OL1184AE09E | 18 (11) | LRLK211021ALC1 | 241 | 230 | 285 | 297
ID #3 | PO08S00651A02U P43OL1184AE25E | 18 (7) | LRLK211021ALC1 | 254 | 225 | 293 | 310
ID #4 | PO08S00652A01U P43OL1184AE36E | 17 (7) | LRLK211021ALC1 | 283 | 269 | 310 | 326
ID #5 | PO08S00652A02U P43OL1184AE47E | 17 (10) | LRLK211021ALC1 | 234 | 235 | 302 | 305
Vector #464342

## Slide 107: P43OL1184 – Ic , Cable Qual Samples
Wire/ Cable Strand | Ic(A) at Field (T) |  |  | 
 | 12 T | 13 T | 14 T | 15 T
PO08S00651A01U P43OL1184AE09E | 664 | 551 | 452 | 364
PO08S00652A02U P43OL1184AE47E | 671 | 555 | 453 | 362
PO08S00651A02U P43OL1184AE25E | 651 | 537 | 435 | 347
PO08S00651A01U P43OL1184AE11E | 665 | 552 | 452 | 364

## Slide 108: P43OL1184 – SSL Plot, Cable Qual Samples

## Slide 109: P43OL1184 – SSL Margins, Qual Samples
Strand from which Margin is Calculated: | Strand # 25E @ 1.9 K
Margins | Margin | Operating Point (X)
Load Line Margin (Purple Arrow) | 25.6% | 74.4%
Current Margin (Green Arrow) | 61.0% | 39.0%
Temperature Margin (K) | 5.2 | 7.1
Limits | Strand | Strand x 40
Selected Strand Current (A) at Margin-Calculation Field | 1040.9 | 41636.4
Selected Strand Current (A) at 100% SSL | 545.4 | 21814.5
Selected Strand Field (T) at 100% SSL | 14.84 | 

## Slide 110: QXFA-242 / P43OL1189

## Slide 111: P43OL1189 – Cable Date, Lengths
Cable Manufacture Date
  22 Mar 2022 (Production run)
Cable Length:
  466 m (LBNL, fabricated, including LBNL samples)

## Slide 112: P43OL1189 – Strand and SS Core ID
Spool:
  PO08S00523A03U x 15 ULs
  PO08S00671A02U x 11 ULs
  PO08S00681A01U x 12 ULs
  PO08S00681A02U x 2 ULs
Core:
  120L40A7400804
    Heat: 850858. Lot: 17-521
    Material: 316L
    Chemical Properties CoT/CoC #172660-1: 0.16 wt% Co
    Core width: 12.0 mm
From 3 billets

## Slide 113: P43OL1189 Respooling Wire Diameter
Below LSL: 0.000%
Above USL: 0.004%

## Slide 114: P43OL1189 – Cable QC Data Summary
CME:
Residual Twist: 135°
10-stack:
  Qualification: 1.531 mm
  Production tail end: 1.530 mm
 | Pressure (MPa) | Angle (°) | Width (mm) | Thickness (mm)
Maximum | 17.1 | 0.390 | 18.159 | 1.529
Average | 17.0 | 0.374 | 18.134 | 1.525
Minimum | 16.9 | 0.350 | 18.126 | 1.517
Sigma | 0.02 | 0.007 | 0.004 | 0.002

## Slide 115
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 116
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 117
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 118: P43OL1189 – Braiding
Fiberglass Lot: #RCV0011562
P/I: 18.9
Spool tension: 10 lbs. @ payoff. 20 lbs. @ takeup (12 lbs min)
Bobbin payoff tension: 0.125 lbs. ≤ T ≤ 0.250 lbs.
Site | Cycle #1 (mm) | Cycle #2 (mm) | Cycle #3 (mm) | Average (mm)
NEWT | 0.151 | 0.149 | 0.148 | 0.149
LBNL Verification | 0.146 | 0.144 | 0.142 | 0.144
Insulation Thickness (at 5 MPa)

## Slide 119: P43OL1189 – Wire Parameters
Properties | Inspected Average
Wire Diameter | 0.8503 ± 0.001 mm (LBNL)1
Cu ratio a | 54.15% (BOST)
Strand twist pitch a | 18.7 mm (BOST)
RRR (RW) a | 314 (BOST)
RRR (15% rolled) a | 220 (BOST)
IC (4.2 K, 15 T) a | 380 A (BOST)
IC (4.2 K, 14 T) a | 475 A (BOST)
IC (4.2 K, 13 T) a | 580 A (BOST)
IC (4.2 K, 12 T) a | 703 A (BOST)
a First billet averaged, then weighted average according to the spool distribution in the cable
1 As-received. LBNL respooling data. Mean ± 1 sigma

## Slide 120: P43OL1189 – Wire Parameters Supplier (S) and Verification (V) IC Data
Number of spools from that billet used in the cable

## Slide 121: P43OL1189 – Wire Parameters Supplier (S) and Verification (V) RRR Data
Number of spools from that billet used in the cable

## Slide 122: P43OL1189 – Extracted Strand RRR
Cable ID | No. of Units from Billet (spool) | Heat Treat/ Sample ID | Major Edge RRR | Minor Edge RRR | Straight 1 RRR | Straight 2 RRR
PO08S00523A03U P43OL1189AE03E | 15 (15) | LRLK220420ALC1 | 314 | 238 | 361 | 366
PO08S00523A03U P43OL1189AE05E | 15 (15) | LRLK220420ALC1 | 337 | 270 | 386 | 386
PO08S00671A02U P43OL1189AE24E | 11 (11) | LRLK220420ALC1 | 276 | 246 | 311 | 303
PO08S00681A01U P43OL1189AE41E | 14 (12) | LRLK220420ALC1 | 320 | 266 | 353 | 357
PO08S00681A01U P43OL1189AE42E | 14 (12) | LRLK220420ALC1 | 300 | 270 | 359 | 362

## Slide 123: P43OL1189 – Ic, Cable Qual Samples
Wire/ Cable Strand | Ic(A) at Field (T) |  |  | 
 | 12 T | 13 T | 14 T | 15 T
PO08S00523A03U P43OL1189AE01E | 704 | 587 | 480 | 384
PO08S00681A01U P43OL1189AE41E | 664 | 549 | 449 | 360
PO08S00671A02U P43OL1189AE24E | 665 | 552 | 453 | 365

## Slide 124: P43OL1189 – SSL Plot, Cable Qual Samples

## Slide 125: P43OL1189 – SSL Margins, Qual Samples
Strand from which Margin is Calculated: | Strand # 41E @ 1.9 K
Margins | Margin | Operating Point (X)
Load Line Margin (Purple Arrow) | 26.3% | 73.8%
Current Margin (Green Arrow) | 61.3% | 38.7%
Temperature Margin (K) | 5.3 | 7.2
Limits | Strand | Strand x 40
Selected Strand Current (A) at Margin-Calculation Field | 1047.2 | 41887.8
Selected Strand Current (A) at 100% SSL | 550.1 | 22005.4
Selected Strand Field (T) at 100% SSL | 14.97 |