## Slide 1: 3M 2216 curing time
Sotiris Vlachos

## Slide 2: Handling and Curing time
According to 3M specifications :
Handling after 8– 12 hours
Full strength after 7 days
In various procedures (ex https://edms.cern.ch/document/2616203/3) glued items are handled 5 hours after glue application
This should be increased to ten hours,
Care should be taken not to put strain on them for one week.

## Slide 3: 8760Doc043 V-, U- and G-layer wire combs and comb caps installation
…
9.1.23 Allow at least five hours for the Scotch-Weld 2216 grey epoxy to cure.