**Lessons from the Verification Testing of Nb3Sn Wires Procured Under the High-Luminosity LHC Accelerator Upgrade Project**

Jeremy Levitan1, Jun Lu1, Vito Lombardo2, and Lance Cooley3

1 Magnet science and technology, National High Magnetic Field Laboratory, Tallahassee, FL 32310 USA

2 Technical Division of the Fermi National Accelerator Laboratory, Bata-via, IL 60510 USA.

3 Applied Superconductivity Center, National High Magnetic Field Laboratory, Tallahassee, FL 32310 USA

The High-Luminosity LHC Accelerator Upgrade Project (AUP) in the U.S. delivered the first two quadrupole magnets to CERN in December 2023. A total 13.9 tons, over 2,080 km of highcurrent-density Nb3Sn wires have been procured for AUP program. Programs for quality control (QC) at the supplier and quality verification (QV) at the laboratories were solidified into components of the overall quality plan for strand procurement in 2017. Since then, approximately 1,500 QC samples have been evaluated by the supplier and 400 QV samples by the National High Magnetic Field Laboratory (NHMFL), including measurements of the critical current (*Ic*) and residual resistance ratio (RRR). Several lessons emerge from the testing campaign, which will be discussed in this presentation. While differences between QC and QV samples was within a 2.5% range found by recent inter-laboratory comparisons for 12 T *Ic* data, significant deviations occurred at 15 T with the QC data being conservative relative to the QV data. Since most laboratories have calibrated their test facilities for 12 T measurements, this discrepancy could signal upcoming testing challenges for future colliders where 16 T is a target field.

[[1]](#footnote-1)

**Acknowledgement**

This work is financially supported by DOE through Fermi National Accelerator Laboratory. This work was performed at the National High Magnetic Field Laboratory, which is supported by National Science Foundation Cooperative Agreement No. DMR-1644779 and the State of Florida.

1. This work is financially supported by DOE through Fermi National Accelerator Laboratory. This work was performed at the National High Magnetic Field Laboratory, which is supported by National Science Foundation Cooperative Agreement No. DMR-1644779 and the State of Florida.

J. Levitan and J. Lu are with Magnet Science and Technology, National High Magnetic Field Laboratory, Tallahassee, FL 32310 USA, (Corresponding author: Jun Lu, junlu@magnet.fsu.edu.) L. D. Cooley is with the Applied Superconductivity Center, National High Magnetic Field Laboratory, Tallahassee, FL 32310 USA. Vito Lombardo is with Technical Division of the Fermi National Accelerator Laboratory, Batavia, IL 60510 USA. [↑](#footnote-ref-1)