## Slide 1: MQXFA12b Magnets 302.2.02 and 03 – • Strand Procurement & Testing • Cable Fabrication & Testing
Lance Cooley – NHMFL/ASC (302.2.02 L3)
Vito Lombardo – FNAL (302.2.02 CAM)
Ian Pong – LBNL (302.2.03 L3 & CAM)
Mike Naus – LBNL (302.2.03 L3 Deputy & CAM Deputy)
Elizabeth Lee – LBNL
Jonathan Lee – LBNL Intern Student (now Grad Student at NHMFL)

## Slide 2: Cable & Coil Overview
All cables are 2nd generation QXF cables produced under AUP
Coil # | Cable #
150 | P43OL1186
158 | P43OL1257
159 | P43OL1192
Spare. Already approved. Not reviewed here.

## Slide 3: Cable QC Summary
All cables passed the required quality control testing per US-HiLumi-Doc 74
There were No Critical DRs

## Slide 4: Cable 1192 (Coil 159) DR Detail: 5 DRs

## Slide 5: QXFA-159/ P43OL1192: RRR Reaction Temperatures
Issue: Inaccurate temperatures during first 33 h of 210°C plateau
Cause: Thermocouples plugged into wrong data logger ports
(i.e., calibrations were inaccurate)
Acceptance Justification
  Last ~15 h recorded correctly: Temperatures & range were good
DR #12896 (1 of 5)

## Slide 6: QXFA-159/ P43OL1192: Ic Measurement
Issue: 1 of 3 primary Ic strands was unable to be measured
Cause: Unknown. Believed to be sample mounting issue.
Acceptance Justification
  Back-up sample successfully measured and acceptable, thus meeting the requirement
DR #12931 (2 of 5)

## Slide 7: QXFA-159/ P43OL1192: Accelerometer Data
Issue: 1 of 2 shipment accelerometers had no data
Cause: Battery failure
Acceptance Justification
  Data from working accelerometer was passing
  Preventative Action: Batteries replaced on all accelerometers
DR #12946 (3 of 5)

## Slide 8: QXFA-159/ P43OL1192: Insulation Thickness
Issue: No insulation thickness verification measurement at LBNL
Cause:
Cable instability at braiding vendor 2x when starting at cable’s tail end
  Repaired at LBNL after 1st failure
  Cable sent to FNAL after 2nd failure for respooling in opposite direction to spool from cable’s point end
Instability caused by vendor crossing-over cable during work pauses to temporarily hold cable (No photos. Issue fixed: Clamp implemented.)
To maximize amount of stable conductor for coil winding, insulation verification sample not taken
Acceptance Justification
  Good insulation thickness correlation between LBNL verification and vendor’s data for previous cables
  Original unstable section will be part of ‘cable drops’ after coiling
  Cable successfully braided in presence of L3 (Ian Pong)
DR #13170 & 13348 (4&5 of 5)

## Slide 9: Cable 1257 (Coil 158) DR Detail: 2 DRs

## Slide 10: QXFA-158/ P43OL1257: RRR Reaction Temperatures
Issue 1: Sample reaction TCs outside of calibration window
Issue 2: Range of TC values along the sample length during HT plateaus varied by more than 2 °C.
210C Plateau: Range = 4.2 °C
400C Plateau: Range = 6.0 °C
665C Plateau: Range = 7.0 °C
Cause 1: Unable to calibrate TCs in RRR furnace, as built (fixed)
Cause 2: TC drift coupled with the inability to calibrate.
Acceptance Justification
  Quartz-encapsulated witness wire RRR was within normal range
  Average temperatures within the ±5°C spec
  210C Plateau, Average = 211.9 °C
  400C Plateau, Average = 400.8 °C
  665C Plateau, Average = 667.5 °C
DR #12324 (1 of 2)

## Slide 11: QXFA-158/ P43OL1257: Cable Residual Twist
Issue: Cable residual twist 5° above upper spec (155° vs 150°)
Cause: Unknown. Process variation.
Acceptance Justification
  FNAL had previously stated this is not a hard limit
    Cable at 170° previously allowed without issue (Cable #1161)
DR #12366 (2 of 2)

## Slide 12: END [Back-Up Slides Below]

## Slide 13: Strand Summary
All strands ordered per the “HiLumi” specification under the AUP program, per the following POs:
  FNAL PO 646116 SA1 Shipment E
  FNAL PO 655175 Shipment A
  FNAL PO 667037 Shipment D
Conductor Description:
  Ø0.85 mm, 108/127 stack, Ti-doped, Reduced-Sn core

## Slide 14
Both 665°C/75h
S: 665°C/50h
V: 665°/75h
Both 665°C/50h
Strand Production Data – Ic, 15T
Yellow boxes indicate strand data for this cables

## Slide 15
Both 665°C/75h
S: 665°C/50h
V: 665°/75h
Both 665°C/50h
Strand Production Data – Ic, 12T
Yellow boxes indicate strand data for this cables

## Slide 16: Strand Production Data - RRR
Data for 15% rolled strand predicts the RRR at cable sharp bend
Lab: IEC method, Supplier: 20K method
Inter-lab comparisons have validated approaches (see QP)
Yellow boxes indicate strand data for this cables

## Slide 17: QXFA-159 / P43OL1192

## Slide 18: P43OL1192 – Cable Date, Lengths
Cable Manufacture Date
  14 Apr 2022 (Production run)
Cable Length:
  466 m (LBNL, fabricated, including LBNL samples)

## Slide 19: P43OL1192 – Strand and SS Core ID
Spool:
  PO08S00677A02U x 12 ULs
  PO08S00683A01U x 8 ULs
  PO08S00683A02U x 8 ULs
  PO08S00686A01U x 12 ULs
Core:
  120L43A7400804
    Heat: 850858. Lot: 17-521
    Material: 316L
    Chemical Properties CoT/CoC #187781-1: 0.16 wt% Co
    Core width: 12.0 mm
From 3 billets

## Slide 20: P43OL1192 Respooling Wire Diameter
Below LSL: 0.000%
Above USL: 0.014%

## Slide 21: P43OL1192 – Cable QC Data Summary
CME:
Residual Twist: 150°
10-stack:
  Qualification: 1.533 mm
  Production tail end: 1.532 mm
 | Pressure (MPa) | Angle (°) | Width (mm) | Thickness (mm)
Maximum | 16.9 | 0.398 | 18.160 | 1.529
Average | 16.8 | 0.374 | 18.136 | 1.521
Minimum | 16.8 | 0.357 | 18.129 | 1.518
Sigma | 0.01 | 0.007 | 0.004 | 0.002

## Slide 22
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 23
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 24
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 25: P43OL1192 – Braiding
Fiberglass Lot: #RCV00011562
P/I: 18.9
Spool tension: 10 lbs. @ payoff. 20 lbs. @ takeup (12 lbs min)
Bobbin payoff tension: 0.125 lbs. ≤ T ≤ 0.250 lbs.
Site | Cycle #1 (mm) | Cycle #2 (mm) | Cycle #3 (mm) | Average (mm)
NEWT | 0.150 | 0.148 | 0.147 | 0.148
LBNL Verification* | N/A | N/A | N/A | N/A
Insulation Thickness (at 5 MPa)
*See DRs 13170 & 13348

## Slide 26: P43OL1192 – Wire Parameters
Properties | Inspected Average
Wire Diameter | 0.8509 ± 0.001 mm (LBNL)1
Cu ratio a | 54.31% (BOST)
Strand twist pitch a | 19.5mm (BOST)
RRR (RW) a | 301 (BOST)
RRR (15% rolled) a | 220 (BOST)
IC (4.2 K, 15 T) a | 370 A (BOST)
IC (4.2 K, 14 T) a | 461 A (BOST)
IC (4.2 K, 13 T) a | 567 A (BOST)
IC (4.2 K, 12 T) a | 685 A (BOST)
a First billet averaged, then weighted average according to the spool distribution in the cable
1 As-received. LBNL respooling data. Mean ± 1 sigma

## Slide 27: P43OL1192 – Wire Parameters Supplier (S) and Verification (V) IC Data
Number of spools from that billet used in the cable

## Slide 28: P43OL1192 – Wire Parameters Supplier (S) and Verification (V) RRR Data
Number of spools from that billet used in the cable

## Slide 29: P43OL11192 – Extracted Strand RRR
Cable ID | No. of Units from Billet (spool) | Heat Treat/ Sample ID | Major Edge RRR | Minor Edge RRR | Straight 1 RRR | Straight 2 RRR
PO08S00677A02U P43OL1192AE03E | 12 (12) | LRLK220523ALC1 | 307 | 272 | 326 | 345
PO08S00677A02U P43OL1192AE05E | 12 (12) | LRLK220523ALC1 | 299 | 276 | 331 | 347
PO08S00683A01U P43OL1192AE19E | 16 (8) | LRLK220523ALC1 | 285 | 260 | 328 | 321
PO08S00686A01U P43OL1192AE43E | 12 (12) | LRLK220523ALC1 | 286 | 251 | 325 | 333
PO08S00686A01U P43OL1192AE45E | 12 (12) | LRLK220523ALC1 | 294 | 279 | 342 | 346

## Slide 30: P43OL1192 – Ic, Cable Qual Samples
Wire/ Cable Strand | Ic(A) at Field (T) |  |  | 
 | 12 T | 13 T | 14 T | 15 T
PO08S00686A01U P43OL1192AE43E | 614 | 513 | 422 | 347
PO08S00683A01U P43OL1192AE19E | 653 | 540 | 439 | 352
PO08S00677A02U P43OL1192AE03E | 662 | 543 | 444 | 357

## Slide 31: P43OL1192 – SSL Plot, Cable Qual Samples

## Slide 32: P43OL1192 – SSL Margins, Qual Samples
Strand from which Margin is Calculated: | Strand # 43E @ 1.9 K
Margins | Margin | Operating Point (X)
Load Line Margin (Purple Arrow) | 24.6% | 75.4%
Current Margin (Green Arrow) | 56.9% | 43.1%
Temperature Margin (K) | 5.1 | 7.0
Limits | Strand | Strand x 40
Selected Strand’s Current (A) at Margin-Calculation Field | 942 | 37697
Selected Strand’s Current (A) at 100% SSL | 538 | 21524
Selected Strand’s Field (T) at 100% SSL | 14.7 | 

## Slide 33: QXFA-158 / P43OL1257

## Slide 34: P43OL1257 – Cable Date, Lengths
Cable Manufacture Date
  16 Feb 2021 (Production run)
Cable Length:
  469 m (LBNL, fabricated, including LBNL samples)

## Slide 35: P43OL1257 – Strand and SS Core ID
Spool:
  PO08S00078A04U x 1 ULs
  PO08S00517A02U x 14 ULs
  PO08S00519A01U x 3 ULs
  PO08S00519A02U x 7 ULs
  PO08S00519A03U x 4 ULs
  PO08S00520A03U x 11 Uls
  PO08S00535A02U x 1 ULs
Core:
  120L08A7400804
    Heat: 850858. Lot: 17-521
    Material: 316L
    Chemical Properties CoT/CoC #187781-1: 0.16 wt% Co
    Core width: 12.0 mm
From 5 billets

## Slide 36: P43OL1257 Respooling Wire Diameter
Below LSL: 0.005%
Above USL: 0.008%

## Slide 37: P43OL1257 – Cable QC Data Summary
CME:
Residual Twist: 155°
10-stack:
  Qualification: 1.538 mm
  Production tail end: 1.528 mm
 | Pressure (MPa) | Angle (°) | Width (mm) | Thickness (mm)
Maximum | 17.2 | 0.444 | 18.160 | 1.531
Average | 17.1 | 0.429 | 18.139 | 1.521
Minimum | 16.7 | 0.412 | 18.133 | 1.518
Sigma | 0.03 | 0.006 | 0.003 | 0.002

## Slide 38
Rollers: P-93 (2020 09 02) & P-94 (2020 09 02)

## Slide 39
Rollers: P-93 (2020 09 02) & P-94 (2020 09 02)

## Slide 40
Rollers: P-93 (2020 09 02) & P-94 (2020 09 02)

## Slide 41: P43OL1257 – Braiding
Fiberglass Lot: #111154
P/I: 18.0
Spool tension: 10 lbs. @ payoff. 20 lbs. @ takeup (12 lbs min)
Bobbin payoff tension: 0.125 lbs. ≤ T ≤ 0.250 lbs.
Site | Cycle #1 (mm) | Cycle #2 (mm) | Cycle #3 (mm) | Average (mm)
NEWT | 0.142 | 0.140 | 0.139 | 0.140
LBNL Verification | 0.143 | 0.140 | 0.139 | 0.141
Insulation Thickness (at 5 MPa)

## Slide 42: P43OL1257 – Wire Parameters
Properties | Inspected Average
Wire Diameter | 0.8501 ± 0.001 mm (LBNL)1
Cu ratio a | 53.82% (BOST)
Strand twist pitch a | 19.0mm (BOST)
RRR (RW) a | 324 (BOST)
RRR (15% rolled) a | 241 (BOST)
IC (4.2 K, 15 T) a | 408 A (BOST)
IC (4.2 K, 14 T) a | 505 A (BOST)
IC (4.2 K, 13 T) a | 615 A (BOST)
IC (4.2 K, 12 T) a | 739 A (BOST)
a First billet averaged, then weighted average according to the spool distribution in the cable
1 As-received. LBNL respooling data. Mean ± 1 sigma

## Slide 43: P43OL1257 – Wire Parameters Supplier (S) and Verification (V) IC Data
Number of spools from that billet used in the cable

## Slide 44: P43OL1257 – Wire Parameters Supplier (S) and Verification (V) RRR Data
Number of spools from that billet used in the cable

## Slide 45: P43OL1257 – Extracted Strand RRR
Cable ID | No. of Units from Billet (spool) | Heat Treat/ Sample ID | Major Edge RRR | Minor Edge RRR | Straight 1 RRR | Straight 2 RRR
PO08S00517A02U P43OL1257AE06E | 14 (14) | LRLK210219ALC1 | 357 | 245 | 363 | 341
PO08S00517A02U P43OL1257AE07E | 14 (14) | LRLK210219ALC1 | 322 | 266 | 381 | 372
PO08S00519A02U P43OL1257AE29E | 14 (7) | LRLK210219ALC1 | 353 | 233 | 365 | 358
PO08S00519A03U P43OL1257AE39E | 14 (4) | LRLK210219ALC1 | 289 | 225 | 326 | 314
PO08S00520A03U P43OL1257AE45E | 11 (11) | LRLK210219ALC1 | 371 | 248 | 360 | 349

## Slide 46: P43OL1257 – Ic, Cable Qual Samples
Wire/ Cable Strand | Ic(A) at Field (T) |  |  | 
 | 12 T | 13 T | 14 T | 15 T
PO08S00517A02U P43OL1257AE06E | 710 | 589 | 484 | 389
PO08S00520A03U P43OL1257AE45E | 712 | 592 | 484 | 391
PO08S00519A02U P43OL1257AE29E | 726 | 606 | 498 | 402

## Slide 47: P43OL1257 – SSL Plot, Cable Qual Samples

## Slide 48: P43OL1257 – SSL Margins, Qual Samples
Strand from which Margin is Calculated: | Strand # 06E @ 1.9 K
Margins | Margin | Operating Point (X)
Load Line Margin (Purple Arrow) | 27.6% | 72.5%
Current Margin (Green Arrow) | 63.7% | 36.3%
Temperature Margin (K) | 5.5 | 7.4
Limits | Strand | Strand x 40
Selected Strand’s Current (A) at Margin-Calculation Field | 1118 | 44707
Selected Strand’s Current (A) at 100% SSL | 560 | 22401
Selected Strand’s Field (T) at 100% SSL | 15.2 |