## Slide 1: at
Davide Chiappara, Piero Giubilato, Caterina Pantouvakis, Michele Rignanese
26 Jan 2024
S-curves – Fe55 measurement

## Slide 2: Fe55 measurement
Goal: S-curve measurement using an X-ray monochromatic source instead of performing TP injections
Measurement with Fe55 source scanning over different threshold values
Fe55: kα1 peak at 5.9 keV  1640 e-
With respect to a TP S-curve
the rate does not saturate
per point
Example of a Fe55 measurement done on an array of 16x16 pixels in the central sector of the chip

## Slide 3: Fe55 measurement
Why does the rate keep increasing decreasing the threshold?
Hypothesis:
The electronic cloud generated by the X-ray interaction in Silicon widens by diffusion while drifting towards the electrodes and it can spread over more than one pixel (charge sharing).
Fluctuations of gain, noise, and baseline pixel to pixel are relevant when performing measurements over an array of pixels. Measurable thermal fluctuations.
Comparison of measurements from frontside and backside of the chip + Monte Carlo simulations
200 μm
Measurement on one single pixel in a temperature-controlled environment.
To test:
To comply:

## Slide 4: Single pixel simulation
Simple single pixel Monte Carlo simulation to study geometrical charge sharing effects
Simulation is performed using the following steps:
0
0
1
1
Set two different parameters:
Width of the electrons cloud ()
Front-end electronic noise
3
Generate hit coordinates (x, y) in range [-3, 1 + 3]
Build a 2D gaussian with = (x, y) and
Calculate numerical integral in pixel area
Fill analog histogram
Full charge collection
Partial collection
Noise

## Slide 5: Fe55 simulations: rate vs threshold
Large
Small
Small
 Charge sharing contribution
 Electronic noise
t : threshold
: threshold at which
the s-curve inflection
point is found
Large

## Slide 6: Fe55 frontside measurement vs simulation
Simulation parameters:
Cloud σ = 0.145
El. noise σ = 20 e-
Fit Parameter | Data | Simulation
t0 | 0.98 | 0.98
Cs | 0.19 | 0.22
σ | 0.025 | 0.030

## Slide 7: Fe55 frontside measurement vs simulation
The charge sharing contribution is dominant  Not sensitive on the electronic noise
Fixed electronic noise, charge sharing ±5%
Fixed charge sharing, electronic noise σ ±50%

## Slide 8: Fe55 backside vs frontside
200 μm
Fit Parameter | Frontside | Backside
t0 | 0.98 | 0.98
Cs | 0.19 | 0.54
σ | 0.025 | 0.048

## Slide 9: Ongoing work
Improve statistics with 55Fe source;
Measurements with more pixels;
More realistic simulation;
Larger simulation domain;
Measurements with monochromatic source at a different energy for calibration ?
Electronic cloud simulation with TCAD
Replication on SPICE of the analog front end loading correctly the libraries;
  Quantification of some features of the analog pixels around the array (baseline, noise, gain, …);
  Understanding of the amount of charge injected in the pixel.