## Slide 1: Spike detector data MQXFA07b
1/26/2024
Anis Ben Yahia

## Slide 2
Test cycle 2:
Ramp to 16530 A, 30 minutes hold. NO QUENCH.
Ramp to 16230 A at 30 A/s, QD trip at 14458 A. (threshold were set to 250 mV but an imbalance on QD1 caused the trigger)
Ramp to 16230 A (+30 A/s, -100 A/s), 5 minutes hold. NO QUENCH.
Ramp to 16530 A, 30 minutes hold. NO QUENCH.
Ramp to 16230 A (+30 A/s, -100 A/s), 5 minutes hold. NO QUENCH.
Ramp to 16530 A, 60 minutes hold. NO QUENCH.
Ramp to 16530 A at 4.5 K: Quench #1 IQ = 16482 A, QI = 26.1 MIIts, Coil 114 (Q4)
Ramp to 16230 A at 4.5 K, 30 minutes hold. NO QUENCH.
Ramp to 16530 A, 30 minutes hold. NO QUENCH.
Ramps with spike detector data

## Slide 3
Test cycle 2 ramp | File name | Label | Shortened
Ramp to 16230 A (+30 A/s, -100 A/s), 5 minutes hold. NO QUENCH. | MQXFA07b_fast_ramp_VS | A07b-R1-16230A-1.9K-30A/s-5min-from-VS | A07b-R1
Ramp to 16530 A, 30 minutes hold. NO QUENCH. | MQXFA07b_ramp_20_30_min | A07b-R2-16530A-1.9K-20A/s-30min | A07b-R2
Ramp to 16230 A (+30 A/s, -100 A/s), 5 minutes hold. NO QUENCH. | MQXFA07b_fast_ramp_normalTP | A07b-R3-16230A-1.9K-30A/s-5min-normal-TP | A07b-R3
Ramp to 16530 A, 60 minutes hold. NO QUENCH. | MQXFA07b_one_hour_hold | A07b-R4-16530A-1.9K-20A/s-60min | A07b-R4
Ramp to 16530 A at 4.5 K: Quench #1 IQ = 16482 A, Coil 114 (Q4) | MQXFA07b_4.5k ramp | A07b-R5-16530A-4.5K-20A/s-Quench1 | A07b-R5
Ramp to 16230 A at 4.5 K, 30 minutes hold. NO QUENCH. | MQXFA07b_4.5K ramp repeat | A07b-R6-16230A-4.5K-20A/s-30min | A07b-R6
Ramp to 16530 A, 30 minutes hold. NO QUENCH. | MQXFA07b_1.9K ramp repeat | A07b-R7-16530A-1.9K-20A/s-30min | A07b-R7
A07b – Ramp_# - Target_Current - Temperature- Ramp_rate_up - Hold_time_or_quench
From-VS: fast ramp following a quench
Normal-TP: fast ramp in its typical test plan sequence

## Slide 4
Max captured data: 29 min

## Slide 5: Ramp to 16230 A (+30 A/s, -100 A/s), 5 minutes hold. NO QUENCH.
A07b-R1-16230A-1.9K-30A/s-5min-from-VS

## Slide 6
Full recorded magnet half diff. at 100 kHz

## Slide 7
Max (absolute) value in each recorded spike snapshot

## Slide 19: Ramp to 16530 A, 30 minutes hold. NO QUENCH.
A07b-R2-16530A-1.9K-20A/s-30min

## Slide 30: Ramp to 16230 A (+30 A/s, -100 A/s), 5 minutes hold. NO QUENCH.
A07b-R3-16230A-1.9K-30A/s-5min-normal-TP

## Slide 31
Full recorded magnet half diff. at 100 kHz

## Slide 32
Full recorded magnet half diff. at 100 kHz

## Slide 33
Max (absolute) value in each recorded spike snapshot

## Slide 34
Max (absolute) value in each recorded spike snapshot

## Slide 38
selected_spikes=find(peak_spike>0.05 & current>10000)

## Slide 44: Ramp to 16530 A, 60 minutes hold. NO QUENCH.
A07b-R4-16530A-1.9K-20A/s-60min

## Slide 53: Ramp to 16530 A at 4.5 K: Quench #1 IQ = 16482 A, Coil 114 (Q4)
A07b-R5-16530A-4.5K-20A/s-Quench1

## Slide 60: Ramp to 16230 A at 4.5 K, 30 minutes hold. NO QUENCH.
A07b-R6-16230A-4.5K-20A/s-30min

## Slide 68: Ramp to 16530 A, 30 minutes hold. NO QUENCH.
A07b-R7-16530A-1.9K-20A/s-30min