## Slide 1: Dielectric Laser Acceleration

## Slide 2: Dielectric Laser Acceleration (DLA)
laser-driven microstructures
• lasers: high rep rates, strong field gradients, commercial support
• dielectrics: higher breakdown threshold  higher gradients
(>1 GV/m), leverage industrial fabrication processes
lower cost, more compact, higher gradient
gradient
Wafer is
diced into
individual
samples
for e-beam
tests.
"Accelerator-on-a-chip"
bonded silica phase reset accelerator prototypes fabricated at SLAC/Stanford
Observed electron energy modulation from laser interaction (Dec. 2012)
Notes: Traditional metal cavity accelerators can be scaled to higher frequencies, such as X-band to attempt to get higher gradient. But one is ultimately limited by machining tolerances, the proliferation of transverse wakefields, and the electric field breakdown limit of around 100 MV/m.
Continuing the trend to smaller structures into the optical and IR regime opens up the possibility of driving an accelerator using lasers, which can have peak field gradients of 0.5 GV/m and are more readily and cheaply available commercially than high-power microwave sources. Such structures could also be made of dielectric materials, which have damage thresholds in the GV/m range.
A few of the candidate structures that have been considered are shown here.

## Slide 3: Recently Fabricated Prototypes
SLAC/Stanford E163:
Multi-length gratings
1x 400nm gap
1x 800nm gap
1x1200nm gap
1x test structure
Symmetric process
Alignment channels
- IR reflectors (for laser alignment)
(one half shown only)
400 nm gap
Multi-length
Micro-Accelerator Platform
Enhanced Dual-Grating Silica Structures
UCLA MAP (G.Travish)
- Initial prototypes recently completed and tested at SLAC.

## Slide 4: DLA Results to Date
Fabrication of DLA Accelerators & SubComponents
• Fabrication of first demonstration-ready grating accelerator prototype (Aug 2011).
• Completed the first fully assembled 17-layer silicon woodpile accelerator (June 2012).
Simulation and Theory
• Simulation of high-efficiency (>95%) waveguide coupling technique (June 2012).
• Simulation of particle transport through many-period optical structures (Dec 2012).
• Design of novel DLA-based high-resolution beam position monitor (March 2012).
Benchtop and Electron Beam Testing
• Attosecond microbunching and net acceleration with ITR foil (2008).
• Detailed IR damage studies performed to identify robust materials (2009-2012).
• Demonstration of TM mode excitation in a photonic crystal accelerator (2011).
• First powered acceleration tests of completed DLA prototypes (2011-2012).
• First observation of acceleration in a DLA structure! (Dec 2012).

## Slide 5: Optical structures naturally have sub-fs time scales and favor high repetition rate operation
Pulse Format

## Slide 6: DLA Collider Concept
5 fiber lasers per
6'' wafer module
2 kW per laser
needle emitter and
injector module
final focus and steering wafers
Interaction Point
accelerator wafers
Thulium fiber laser λ=2 µm
tungsten field emission
tip design (P. Hommelhoff)
Loop period=beam repetition rate
Phase control
40 stages per module
1 module = 40 mm long
1 stage = 750 µm long
single 6'' accelerator wafer
5 modules per wafer
5 fiber feeds per wafer
1.5 TeV  3.75 km  62,000 lasers
fiber laser feeds
concept for 1 DLA accelerator structure (E. Peralta)
e-

## Slide 7: Strawman Parameter Table

## Slide 8: DLA Test Facility at SLAC
E163 @ NLCTA: A facility for testing laser-driven accelerator structures.
Beam energy = 60MeV; σt = 1ps; σE = 0.1%; 800nm Ti:Sapph laser
NLCTA Beamline
Class 10,000 Laser Room
Control Room
PI-MAX3
Intensified
CCD
~10 m
Ce:YAG

## Slide 9: Future Test Facility Requirements
e-Beam Requirements
nm-scale emittance
attosecond optical bunching
laser triggered, 1000 e-/bunch
1 MeV energy
Laser Requirements
1-2 um wavelength
Tuneable pulse length (100fs to 5ps)
1-50 MHz rep rates, modelocked
>1uJ pulse energy
Traditional RF electron sources can be used for proof-of-principle experiments, but demonstrating future multi-stage devices will require new capabilities
• adapted TEM source
• needle-tip field emitter
+ low-beta pre-injector
• Thulium-doped fiber laser R&D
• Amplified Erbium-doped lasers
Possible Approaches
• proximity to nanofabrication facilities
• strong university participation & collaboration
• national lab accelerator expertise
Other Desirable
Features:

## Slide 10: Unique testing needs for DLAs
Optical phase synchronization over km-scale lengths
nm-scale structure alignment over km-scale lengths
Laser pulse shaping to compensate for beam loading
Measurement of radiation damage to optical materials
Several m of test beam line for testing optical focusing schemes

## Slide 11: 5-Year Roadmap
Draft of funding profile for a multi-institution research program to develop a scalable DLA design on a 5-year time scale.

## Slide 12: Roadmap Goals by Year

## Slide 13: Risk Assessment
Issue | Risk | Time Scale to Solve
Pulsed e- sources with nm emittance | Medium | 5 years
Pulsed e+ sources with nm emittance | High | Unknown
Technology still in proof of principle stage | Medium | 1-2 years
Sub-micron co-alignment over 7 km | Medium | 5 years (see LIGO)
Developing near 100% efficient power distribution capability | Medium | 5-10 years
Availability of suitable laser sources | Low | 3 years
Combined technology demonstration (e.g. via a scaled-down test facility) | High | 5-10 years depending on funding & effort