## Slide 1
Microwave-optical Quantum Transduction
Changqing Wang and Silvia Zorzetti
Superconducting Quantum Materials and Systems (SQMS) Center, Fermi National Accelerator Laboratory

## Slide 2: Introduction to Quantum Transduction
Optical
Microwave
~200 THz
∼GHz
Cryogenic temperature
Superconducting qubits
Room temperature
Microwave-optical transducers
Optical communication
Han, Xu, et al. Optica 8, 1050-1064 (2021).
Hease, William, et al. PRX Quantum 1, 020315 (2020):.
https://sqms.fnal.gov
https://www.antaira.com/Blog-Four-Advantages-of-Fiber-Optic-Communications
FSR
FSR
Cooperativity:
Efficiency:
Requirement:
Single-photon microwave-optic coupling rate ().
Q factor of the microwave and optical cavities.
Pump power.
Electro-optic material: Lithium Niobate (LiNbO3)
Three-wave mixing:

## Slide 3: 3D electro-optical quantum transduction
3D electro-optical design for transduction
High-Q cavities to boost microwave-optic conversion efficiency in quantum transduction
Bulk electro-optic material embedded in SRF cavity
Estimated conversion efficiency up to 50% at 140
npj Quantum Information 8, 149 (2023)
Characterization of Electro-optic materials
High-Q SRF cavity to characterize microwave properties of electro-optic materials (e.g., LN)
Phys. Rev. B 107, L220302
Fermilab’s 3D Bulk Niobium superconducting cavity ()
Physical Review Applied, 13, 034032 (2020).

## Slide 4: Measurement of LiNbO3’s permittivity and loss tangent at mK
LiNbO3 property at 50mK
Phys. Rev. B 107, L220302
,
Relevant literature: Goryachev et al. Physical Review B 92, 060406(R) (2015)
Wollack et al. Appl. Phys. Lett. 118, 123501 (2021)
Hease et al. PRX Quantum 1, 020315 (2020)

## Slide 5: 3D Design for transduction
npj Quantum Information 8, 149 (2023)
Single-photon microwave-optical coupling rate () | Hz
Microwave quality factor | 
Cooperativity () | 0.58
Conversion efficiency | 50%
Operating bandwidth | 100kHz
Pump power | 140
Microwave quality factor | 
 | 0.58
Conversion efficiency | 50%
Operating bandwidth | 100kHz
Pump power | 
Figures of merit
Ø 2 mm
1 mm
Ø 5 mm
2.25 mm

## Slide 6: Transduction for Remote entanglement
  Entanglement between distant SRF cavities (qubit / qudit encoding) via optical photons
  Entanglement between distant transmon qubits via optical photons
Microwave Bell state generation:
|
Superconducting Transmon Qubit