## Slide 1
U.S. MDP Collaboration Meeting CM8
04/30/2024
Nb3Sn SMCT task overview, main results and next steps
A.V. Zlobin

## Slide 2: Outline
Program goal and milestones
Summary of results achieved
  details by Maria
Next step
  lessons learned by Igor
Long-term plan based on P5 recommendations

## Slide 3: Stress Management Cos-Theta (SMCT) coil concept
The stress-managed cos-theta (SMCT) coil is a new concept being developed at Fermilab for HF and/or LA accelerator magnets based on LTS and HTS.
The SMCT structure is used to reduce large coil deformations under Lorentz forces and, thus, the excessively large strains and stresses in the coil.
A 120-mm aperture two-layer Nb3Sn SMCT dipole coil has been developed at Fermilab to demonstrate the SM concept including coil design, fabrication technology and performance.
Nb3Sn Rutherford cable
Stress management for whole coil using 3D printed stainless steel mandrels

## Slide 4
Cos-theta dipole coils with stress management
ID=60 mm, Bdes~17 T
ID=120 mm, Bdes~11 T
Milestone # | Description | Target
AI-M1a | Development and test of stress management concept using a 2-layer large-aperture and 4-layer small-aperture cos-theta coils and dipole mirror structure. | June-23
AI-M2a | Development, fabrication and test of stress management concept in a 2-layer 120-mm dipole with the field up to 11 T. | June-24
AI-M3a | Assembly and test of stress-management concept in a 4-layer 60-mm 17 T dipole with stress management. | Sept-24
US-MDP Task: Nb3Sn SMCT R&D goals and milestones

## Slide 5
SMCTM1a/b assembly, test steps and configurations
Magnet fabrication and assembly - 2022-2023
Delivered to VMTF - May 2023
Tested in two configurations - Sep 2023-Feb 2024
The first milestone of the MDP SMCT program has been achieved
  The first 2L 123-mm ID cos-theta coil with stress management (SMCT coil) has been developed and fabricated
  The SMCT coil was assembled with 60-mm ID 2L cos-theta coil (previously tested in MDPCT1 dipole) inside the dipole mirror structure SMCTM1 and successfully tested at Fermilab
SMCTM1b
SMCTM1a

## Slide 6: SMCTM1a/b test summary (details in Maria’s talk)
SMCTM1a test with TC:
  relatively short training but no training memory (?)
  Iq degradation wrt coil SSL based on WS data was ~9%
  no performance degradation (!) after TC
  maximum field reached at 1.9 K in the SMCT coil was 12.7 T
SMCTM1b test:
  test was complicated by presence of current and voltage spikes
  maximum field in the SMCT/inner coils was 12.6/14.5 T
  performance limitation due to large degradation of the inner coil
12.7 T
12.6 T
1.9 K
Chart: Magnetic Field, T
| 9.42 | 10.17 | 10.91 | 11.65 | 12.39 | 13.12 | 13.86 | 14.6
2L mirror | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 16.9955
4L mirror (SMCT) | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15
4L mirror (L1) | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15
SMCTM1a | 11.521 | 11.8632 | 12.549 | 12.345 | 12.618 | 13.006 | 12.848 | 13.4 | 13.395 | 13.484 | 13.602 | 13.627 | 13.648 | 13.721 | 13.859 | 13.944 | 13.968 | 14.139 | 13.7 | 13.891 | 14.139 | 14.265 | 14.014 | 14.308 | 14.308 | 14.317 | 14.014 | 13.492 | 11.738 | 10.225 | 9.745 | 7.303 | 14.4201 | 13.8753 | 13.4561 | 12.4084 | 12.9656 | 12.6682 | 13.128 | 12.8426 | 11.433 | 11.3642 | 9.4805 | 8.7107 | 13.2198 | 13.3575 | 11.9927 | 13.3915 | 13.6843 | 13.7953 | 13.6053
SMCTM1b-IC | 10.5324 | 10.7517 | 10.9748 | 10.9123 | 11.1033 | 11.2061 | 11.3061 | 11.3905 | 11.464 | 11.4575 | 11.3024 | 8.7637 | 9.8724 | 10.6342 | 7.7035 | 11.4438 | 10.6884 | 11.3263 | 9.2354 | 10.3883 | 11.1721 | 11.1501 | 10.6388 | 11.1005 | 10.3947 | 9.9514 | 10.4121 | 7.5209 | 8.7884 | 9.9816 | 7.5402 | 10.0367 | 10.79 | 9.285 | 11.4309 | 8.1872 | 8.0064 | 7.7733 | 7.5209
SMCTM1b-OC | 10.5324 | 10.7517 | 10.9748 | 10.9123 | 11.1033 | 11.2061 | 11.3061 | 11.3905 | 11.464 | 11.4575 | 11.3024 | 8.7637 | 9.8724 | 10.6342 | 7.7035 | 11.4438 | 10.6884 | 11.3263 | 9.2354 | 10.3883 | 11.1721 | 11.1501 | 10.6388 | 11.1005 | 10.3947 | 9.9514 | 10.4121 | 7.5209 | 8.7884 | 9.9816 | 7.5402 | 10.0367 | 10.79 | 9.285 | 11.4309 | 8.1872 | 8.0064 | 7.7733 | 7.5209
 | 15 | 12.4887 | 10.4674 | 9.2567 | 7.6273 | 6.6548
The performance of the first large-aperture SMCT coil is inspiring.
The record field of 12.7 T was achieved in 123 mm aperture dipole coil made of brittle Nb3Sn cable.

## Slide 7
Cos-theta dipole coils with stress management
ID=60 mm, Bdes~17 T
ID=120 mm, Bdes~11 T
Milestone # | Description | Target
AI-M1a | Development and test of stress management concept using a 2-layer large-aperture and 4-layer small-aperture cos-theta coils and dipole mirror structure. | June-23
AI-M2a | Development, fabrication and test of stress management concept in a 2-layer 120-mm dipole with the field up to 11 T. | June-24
AI-M3a | Assembly and test of stress-management concept in a 4-layer 60-mm 17 T dipole with stress management. | Sept-24
US-MDP Task: Nb3Sn SMCT R&D next steps

## Slide 8: SMCTD1 design concept (details in Igor’s talk)
New optimized SMCT2 coil + 2 new coils from MDPCT1
Reinforced MDPCT1 mechanical structure
Optimized coil end support
Optimized connection box to provide various test options
Based on lessons learned from MDPCT1 and SMCTM1a/b

## Slide 9: SMCTD1 test configurations and goals
Bo, T | Bmax, T
11.6 | 13.3
12.8 | 14.8
SSL | SSL_deg
14.0 | 12.5
14.2 | 12.7
Bo, T | Bmax, T
14.2 | 15.1
17.2 | 18.4

## Slide 10
Milestone # | Description | Target
AI-M1a | Development and test of stress management concept using a 2-layer large-aperture and 4-layer small-aperture cos-theta coils and dipole mirror structure. | June-23 => Feb 24
AI-M2a | Development, fabrication and test of stress management concept in a 2-layer 120-mm dipole with the field up to 11 T. | June-24
AI-M3a | Assembly and test of stress-management concept in a 4-layer 60-mm 17 T dipole with stress management. | Sept-24
US-MDP Task: Nb3Sn SMCT R&D next steps
AI-M2a+AI-M3a | Development of the SMCT coil technology and test of stress management concept in a 2-layer 120-mm dipole with the field up to 11 T and in a 4-layer 60-mm dipole with the field up to 15 T. | Jan-June 2025
Task progress is limited by the resources available

## Slide 11: Summary
The first milestone AI-M1a of the MDP SMCT task has been achieved
  the 1st SMCT coil has been designed, fabricated and tested showing promising quench performance but revealing also some issues to be addressed by the 2nd coil
Fabrication of the 2nd SMCT coil and its test independently and in two dipole configurations with the 1st SMCT coil and MDPST1 inner coils will allow to further study the potential of the SMCT technology
MDP-1
MDP-2

## Slide 12: MDP phase 3: SMCT concept evolution
Utility structure (LBNL/FNAL)
  Cold mass OD=750 mm
  75 mm thick Al shell
1. Coil conceptual design with stress management
2. Mechanical structures

## Slide 13: Result discussion and publication
Presentations (since CM7):
I. Novitski, “SMCTM1 assembly status,” MSD SCRD group meeting, 03/13/2023
I. Novitski, “SMCT mirror magnet update,” US-MDP general meeting, 05/10/2023
M. Baldini, “SMCTM1 Magnet Instrumentation and Test plan,” 07/17/2023
A.V. Zlobin,“Nb3Sn SMCT program overview and FY24 plan,” US-MDP general meeting, 10/11/2023
M. Baldini, “SMCTM1a test summary and next steps,” US-MDP general meeting, 10/11/2023
I. Novitski, “Development and Test of a Large-Aperture Nb3Sn Cos-Theta Dipole Coil With Stress Management,” MT-28, 10/272023
A.V. Zlobin, “US MDP high-field Nb3Sn cos-theta dipole magnet with stress management,” EU HFM program annual meeting, 11/01/2023
A.V. Zlobin, I. Novitski, M. Baldini, S. Krave, “SMCTM1 - results and discussions”, MSD SCRD group meeting, 03/04/2024
I. Novitski, “SMCT mirror assembly,” US MDP general meeting, 4/10/2024
M. Baldini, “SMCTM1a/b test summary,” US MDP general meeting, 4/10/2024
S. Krave, “Acoustic Sensors for SMCTM1b,” US MDP general meeting, 4/10/2024
Publications:
I. Novitski, A.V. Zlobin, M. Baldini, S. Krave, D. Orris, D. Turrioni, E. Barzi, “Development and test of a large-aperture Nb3Sn cos-theta dipole coil with stress management,” IEEE Trans. on Appl. Supercond., Vol. 3x, Issue x, 2024
IPAC’2024 and ASC’2024 abstracts:
A.V. Zlobin et al., “Development and test of a large-aperture Nb3Sn cos-theta dipole coil with stress management,” IPAC-2024, poster
A.V. Zlobin et al., “Test of a 4-layer Nb3Sn cos-theta dipole coil with stress management,” ASC-2024, invited talk

## Slide 14: MDP 1 and 2 Nb3Sn program at Fermilab
MDP-1
MDP-2