## Slide 1
Lucas Brouwer, Mariusz Juchno, Diego Arbelaez, Paolo Ferracin, Jose Luis Rudeiros Fernandez, and Giorgio Vallone (for the CCT Team)
4/30/2024
CCT6 Design and Prototyping

## Slide 2: Outline
review of nominal CCT6 design
impact of all MQXF cable option (potential for mitigating machining risk)
prototyping results and near-term plans

## Slide 3: CCT6 is a 4-layer, Nb3Sn dipole to provide 12-13 T background fields for HTS insert testing within US-MDP
Targets from MDP program plan
120 mm clear bore diameter for inserts
four layers
12 T at 4.2 K, 13 T at 1.9 K (at ~70% short-sample)
MQXF cable for outer layers (Hi-Lumi Dropouts)
LD1 cable for inner layers (on-hand)
Nominal CCT6 design leverages grading and existing cables
https://doi.org/10.1109/TASC.2022.3151723
2D/3D mechanical design is well-advanced for the nominal case, and employs the utility structure
See next talk by Mariusz for details

## Slide 4: Operational margin for the nominal design is ~30% at MDP target of 12 T at 4.5 K, and 13 T at 1.9 K
1-2% rise of field at conductor
1.5 m physical length, straight-section length of 130 mm based on 1% criteria

## Slide 5: Study impact of switching from LD1 to MQXF cables for the inner layers (possible risk mitigation for machining)
drop in channel aspect ratio from 15.7 to 12
Reduces magnet short-sample (-)
Improves machinability (+)
drop in SC fraction
drop in strand number
drop in Jc

## Slide 6: The margin with the MQXF cable option is to reduced to around 20% for both targets
All four layers MQXF cable
Target | I (kA) | Loadline margin
12 T at 4.5 K | 12.62 | 18%
13 T at 1.9 K | 13.79 | 18%

## Slide 7: Prototyping: where we were at the last CM meeting
Machining
First 7-turn
Second 7-turn
Machining w/new bronze
For nominal design with LD1 cable
demonstrated machining of 7-turn mandrel
demonstrated feasibility of winding
established nominal channel depth and width, including reaction gaps
1st Winding
1st Reaction
Feasibility of fab.
Feasibility of winding
Feedback on gaps/channel
2nd winding
w/spacers
Feedback on updated channel/gaps
Use updated channel/gaps
Epoxy
impregnate
Cut & Inspect
Cable inspection at pole
Wind
React
impregnate
Cut/Inspect
Not yet complete
2nd Reaction
Last Collaboration Meeting
Encountered challenges with machining efficiency and quality (see Jose Luis talk)

## Slide 8: Updated prototyping plan and next steps
Flat plate optimizing both LD1 and MQXF grooves for speed
selection of optimal machining parameters
Procurement of first 1.5 m length tube (defect)
Initial feedback on impact of LD1 vs. MQXF channel for scale up
7 turn testing + 20 turns of final channel in 1.5 m tube
Final feedback on impact of LD1 vs. MQXF channel
+ demonstrate machining of long-length tube
Procurement of final 1.5 m length tube
Full inner layer machining
reaction testing
Final groove parameters based on machining / reaction
Where we are now

## Slide 9: Summary and Next Steps
Summary
graded magnetic design for 12 T at 4.5 K and 13 T at 1.9 K with ~30% margin using existing Nb3Sn cables (LD1 + MQXF)
reminder: this is a 16 T+ short-sample magnet
all MQXF cable option for mitigating machining risk lowers the margin to ~20%
a new prototyping plan seeks to demonstrate an efficient path to long-length layers and will provide feedback on choosing between the nominal design and the all MQXF option
Next Steps
complete prototyping and selection final cable and machining parameters
fabrication of first layer (end of 2024)
further optimization of 3D mechanical structure (ongoing)

## Slide 10
Extra

## Slide 11: A seven-test mandrel to demonstrate feasibility of machining and winding, and to measure reaction gaps of conductor
First seven-turn mandrel matching the inner layer of CCT6 (22.6x2 mm grooves)
Winding of 51 strand LD1 cable into deep grooves is challenging, but feasible
clamps prevent popped strands in the pole region

## Slide 12: Revision of the groove based on position of cable after reaction
Reaction gives first feedback on channel depth and reaction gaps
before reaction
after reaction

## Slide 13: Rewinding + reaction of the mandrel with spacers matching the updated groove

## Slide 14: Cutting showed no popped strands in the pole region
Copper shims simulate updated channel in half of the turns

## Slide 15: Updated structural cross section is optimized to fit in LBNL cryostat (Mariusz Juchno)
Original structure made use of existing LD1 shell (presented at MT27)
New structure reduces the OD by 400 mm to be compatible with testing at LBNL
1260 mm OD
Conductor stress results from the new 2D cross section
Sθ (MPa)
von Mises (MPa)
von Mises (MPa)
Cooldown
13 T
Cooldown
13 T
860 mm OD

## Slide 16: 3D analysis is in progress, with initial results showing no show-stoppers in the conductor, mandrels, and structure
See talk by Mariusz next for details
Von Mises in mandrels: cooldown + 14 T

## Slide 17: Conductor Needs for CCT6 are covered by existing “LD1” cable at LBNL and Hi-Lumi Dropouts (no request to CDP)