## Slide 1
J. L. Rudeiros Fernandez* D. Arbelaez, C. Bird, L. Brouwer, E. Buron, J.F. Croteau, P. Ferracin, S. Prestemon, A. Saravanan, G. Vallone
US Magnet Development Program
Lawrence Berkeley National Laboratory
Progress on Nb3Sn CCT: fabrication and assembly methods
US-MDP Collaboration Meeting 2024

## Slide 2: Table of contents
01
Mandrel fabrication
02
Impregnation materials
03
Assembly progress
J. L. Rudeiros Fernandez et al.
04
Conclusions and next steps

## Slide 3: 1. Mandrel fabrication - Fabrication of mandrels for CCT5-W
J. L. Rudeiros Fernandez et al.
Status update
Layer 1
Layer 2
Finished
Error during the last machining operation.
New mandrel to be produced.
Fabrication time of 1 week.

## Slide 4: 1. Mandrel fabrication - Machining development for mandrels for CCT6
J. L. Rudeiros Fernandez et al.
Test number | Spindle speed (rpm) | Feed (in/min) | Depth of cut (in) | Final depth of cut (in) | Final depth of cut (mm) | Tool manufacturer | Tool ID | Tool cutter diameter | Tool length of cut | Tool overall reach | Flutes | Program configuration | Results
1 | 10000 | 30 | 0.03 | 0.35 | 8.89 | Harvey tool | 41578-c4 | 0.0780" (5/64) | 0.1170" | 0.4060" (13/32) | 3 | Two passes per groove | OK
2 | 10000 | 30 | 0.03 | - | - | Harvey tool | 41778-c4 | 0.0780" (5/64) | 0.1170" | 0.6250" (5/8) | 3 | Two passes per groove | The tool brooke at a depth of 0.43 in
3 | 10000 | 20 | 0.03 | 0.6 | 15.24 | Harvey tool | 41778-c4 | 0.0780" (5/64) | 0.1170" | 0.6250" (5/8) | 3 | Two passes per groove | OK
4 | 10000 | 40 | 0.01 | - | - | Harvey tool | 41978-c4 | 0.0780" (5/64) | 0.1170" | 0.9400" | 3 | Two passes per groove | The tool broke after after a few minutes.
5 | 10000 | 20 | 0.01 | - | - | Harvey tool | 41978-c4 | 0.0780" (5/64) | 0.1170" | 0.9400" | 3 | Two passes per groove | The tool broke after after a few minutes.
6 | 10000 | 20 | 0.005 | 0.94 | 23.876 | Harvey tool | 41978-c4 | 0.0780" (5/64) | 0.1170" | 0.9400" | 3 | Two passes per groove | OK
7 | 10000 | 20 | 0.02 | 0.77 | 19.558 | Harvey tool | 953778-C3 | 0.0780" (5/64) | 0.1170" | 0.8000" | 3 | Two passes per groove | OK
Optimization of parameters for increase of machining speed and reduction in risk of tool breakage

## Slide 5: 1. Mandrel fabrication - Machining development for CCT6 mandrels
J. L. Rudeiros Fernandez et al.
Machining of several 7-turns on a full scale 1.5 m long CCT6 inner layer
Improving the process to reduce potential risks
The next step will be to machine 20-turns on a full scale 1.5 m long CCT6 inner layer
Based on current machining parameters full size mandrel fabrication is estimated between 1 to 2 months

## Slide 6: 1. Mandrel fabrication – Mandrel segmentation development
J. L. Rudeiros Fernandez et al.
As an alternative route to machining mandrels out of a single part, segmented mandrels are in development.
The current design relays on self aligning features. The two parts are locked in the angular direction through a pin or key in the pole region.

## Slide 7: Table of contents
01
Mandrel fabrication
02
Impregnation materials
03
Assembly progress
J. L. Rudeiros Fernandez et al.
04
Conclusions and next steps

## Slide 8: 2. Impregnation materials
J. L. Rudeiros Fernandez et al.
CCT sub2
CCT sub3
CCT sub4
Mix61
CTD-701X*
CCT sub5
Mix61
OL
Paraffin wax
IL
CCT sub6
Paraffin wax
*Haight, A., Haynes, M. M., Krave, S. T., Rudeiros-Fernandez, J. L., & Shen, T. (2021). Characterization of Candidate Insulation Resins for Training Reduction in High Energy Physics Magnets. CEC-ICMC.
*Krave, S., Shen, T., & Haight, A. (2021). Exploring New Resin Systems for Nb3Sn Accelerator Magnets. IEEE Transactions on Applied Superconductivity, 31(5), 1-4.
Magnet
Resin
Resins used for the subscale program
CCT sub7
OL
Filled Paraffin wax
IL
Paraffin wax
Training might be related to interfacial mechanisms (heat dissipation due to frictional motion, debonding, crack propagation…) and therefore the change of resin might play a big role.

## Slide 9: 2. Impregnation materials – Characterization of materials
J. L. Rudeiros Fernandez et al.
The idea was to develop a method to constitute the simplest possible material system that will allow for the fundamental characterization (at various temperatures) of the adhesion and related phenomena between components normally used in superconducting magnets.
Resin
Pull-out frame
Single fiber pull-out (SFP) testing
Strand
Precision machined aluminum plates
Copper wire
a
b
c
d
Sample preparation
Assembly
Resin transfer
The specific resin is transferred to the mold formed by the assembly.
PVC tube
a
b
c
d
Resin
Teflon disc
Silicone O-Ring
Copper wire
Interface characterization
Mix 61
Stycast 2850 MT
Paraffin wax
CTD-101K

## Slide 10: 2. Impregnation materials – Characterization of materials
J. L. Rudeiros Fernandez et al.
Interface characterization
Tensile tester adapter
Load cell
Tensile grips
Pull-out frame
Copper wire
Resin block
Dewar
Wire grips
Copper wire
Liquid nitrogen level
Resin block
Pull-out frame
G10 bars
Mix 61
Paraffin wax
Pull-out frame
Resin block
Sample preparation
Example debonding curves

## Slide 11: 2. Impregnation materials – Characterization of materials
J. L. Rudeiros Fernandez et al.
Interface characterization
For each individual test, and based on a few simplification assumptions, one could compute the apparent interfacial shear strength based on: where is the peak load, is the perimeter of the wire, and is the embedded length.
Initial results
Rudeiros Fernández, J.L., Bird, C., Arbelaez, D., Ferracin, P., Prestemon, S., Shen, T. and Vallone, G., 2024. Interface Characterization for Superconducting Magnets. IEEE Transactions on Applied Superconductivity.

## Slide 12: 2. Impregnation materials – Characterization of materials
J. L. Rudeiros Fernandez et al.
Next steps
Resin
Pull-out frame
Single fiber pull-out (SFP) testing
Strand
Complete the characterization of interfacial properties with the addition of filled systems (i.e. filled paraffin wax and epoxy resins).
Characterize the interfacial properties at 4.2 K as well as energy deposition in the copper strand during debonding (lead by M. Martchevskii).
Characterization of bulk properties of resin systems at various temperatures. This is especially relevant to understand the impact of filled systems (e.g. filled paraffin wax) on the stress on the strands due to Lorentz forces.

## Slide 13: 2. Impregnation materials – Development of filled wax impregnation
J. L. Rudeiros Fernandez et al.
Motivation: No training and increased resilience to high transverse stress
Presented at MT28 by Simon Otten

## Slide 14: 2. Impregnation materials – Development of filled wax impregnation
J. L. Rudeiros Fernandez et al.
Process for uniform mixing
Degassing the preheated paraffin wax + carnauba wax
Mixing particles by hand or light stirring
High shear mixing at 10000 rpm + ultrasonic homogenizer
12 hours of stirring + final filter before transfer to mixer
Normal microscopy techniques have been proven extremely challenging for evaluating particle content.
Due to the very high weight ratio of , density measurements were used as a reliable method to established the quantity of particle through all the development processes.
Material | Weight (g)
Polarit 56/58 (Deffner & Johann GmbH- Germany) | 45.5
Carnauba | 5
PB4 MAR alpha-alumina powder from Baikowski | 180
Mix for 100 ml
Brem, A., Duda, M., Müller, C., Garcia, H., Hug, C., Daly, M., Araujo, D.M., Kosse, J., Otten, S., Kario, A. and Ten Kate, H.H., 2023. From hot to cold: Advanced materials and processes for Nb 3 Sn based magnets. IEEE Transactions on Applied Superconductivity.
Based on

## Slide 15: 2. Impregnation materials – Development of filled wax impregnation
J. L. Rudeiros Fernandez et al.
Development of VPI process for transfer to coil
Phase 1
Phase 2
Phase 3 (Final coil)
Aluminum
Aluminum
Aluminum-bronze
Development
Top reservoir
Coil
Vacuum chamber
Vacuum pump
Resin mixer
Compressed air

## Slide 16: 2. Impregnation materials – Development of filled wax impregnation
J. L. Rudeiros Fernandez et al.
Development of VPI process for transfer to coil
Diagram of the impregnation bag system
Mandrel
Mandrel ID
Mandrel OD
New glass fiber tape
New Peel ply
New Flow media
Cooling by convection
Vacuum bag
External heating elements
Cable
New flow media
New peel ply
PTFE + glass fiber
Nylon based

## Slide 17: 2. Impregnation materials – Development of filled wax impregnation
J. L. Rudeiros Fernandez et al.
Development of VPI process for filled resins
LD1 Nb3Sn cable (plan for CCT6)
Subscale Nb3Sn cable
The impregnation of wide cables in groove (of up to 22 mm wide) with filled resin systems was demonstrated.

## Slide 18: 2. Impregnation materials – Development of filled wax impregnation
J. L. Rudeiros Fernandez et al.
Impregnated coil for CCT sub7: Final surface reveal
After impregnation
Vacuum bag removed
Vacuum bag removed
Final surface after peel ply is removed
Mandrel
Mandrel OD
New glass fiber tape
New Peel ply
New Flow media
Vacuum bag
Cable

## Slide 19: Table of contents
01
Mandrel fabrication
02
Impregnation materials
03
Assembly progress
J. L. Rudeiros Fernandez et al.
04
Conclusions and next steps

## Slide 20: 3. Assembly progress
J. L. Rudeiros Fernandez et al.
Continuous incremental improvements have been made to the fabrication and assembly process of the smartshims.
Compressed air
Smartshim left
Smartshim right
Vacuum pump
Resin mixer
Overflow
Assembly of CCT sub7 is in progress (smartshim
CCT sub7
OL
Filled Paraffin wax
IL
Paraffin wax

## Slide 21: Table of contents
01
Mandrel fabrication
02
Impregnation materials
03
Assembly progress
J. L. Rudeiros Fernandez et al.
04
Conclusions

## Slide 22: 4. Conclusions
J. L. Rudeiros Fernandez et al.
Manufacturing of CC5-W and CCT6 mandrels is in progress, with an emphasis on developing reduced risk manufacturing methods.
The paraffin wax interfacial strength with copper wire has been characterized, showing two orders of magnitude lower adhesion in relation to the epoxy resin used for previous CCT magnets (i.e. Mix61) at RT and 77 K.
The paraffin wax system shows evidence of very low energy deposition in the conductor due to interfacial phenomena.
A method to successfully impregnate CCT magnets with filled resins based on the VPI method has been developed.
The assembly of a subscale with filled wax (IL) is in progress and should be ready for testing in the following months.

## Slide 23: Thanks!
J. L. Rudeiros Fernandez et al.