## Slide 1: Recent Test Results
Diego Arbelaez and Reed Teyber on behalf of LBNL Nb3Sn CCT Team

## Slide 2: Outline
Improved inter-layer quench antenna localization method
Test results from wax CCT subscale

## Slide 3: Quench Localization Analysis
Vtap - turn
Antenna - angle
Extensive analysis was performed by R. Teyber
  Combine Vtap and quench antennas to localize quenches
  Histogram bins to 15, 45 or 75 degrees based on antenna element with largest measured flux
New method was recently introduced to improve the resolution of angle localization by using correlation between antenna segments
Work by R. Teyber

## Slide 4: Improved Quench Localization Method
Define Correlation parameter as
Improve localization by accounting for signals from neighboring antenna elements
  Cross-Correlation between neighboring antennas
  Self-Correlation of neighboring antennas
Use Quench simulations to determine relationship between correlation parameters and quench initiation angle
5⁰ Simulation
0⁰ Simulation
Straight cable simulation performed by Ruben Keijzer & Gerard Willering

## Slide 5: Improved Quench Localization Method (cont.)
Normalized Correlation Matrix
Self-Correlation Neighbor Difference
Cross-Correlation Neighbor Difference
Points are simulation results (deviations near “dead” zones)
Find quench location segment by identifying maximum
Within this segment compare the normalized values of the two neighboring self and cross-correlation values
  Neighbor self-correlation difference:
  Neighbor cross-correlation difference:
Use fit function derived from simulations to determine angle for each case (should be consistent)

## Slide 6: Quench Localization SUB2 and SUB3
SUB2 T1
SUB2 T2
SUB2 T3
CCT Subscale 2
CCT Subscale 3
SUB3 T1
SUB3 T2
Dashed lines represent Vtap segment
Color represents quench number

## Slide 7: Quench Angle Localization Summary and Next Steps
General trends for quench angle on thin and thick spar magnets have been established
Simulations of debonding and training in CCT magnets are being performed by G. Vallone
Will continue to use available information and tools to improve understanding of training mechanisms in these magnets
SUB2 Quench Angle
SUB3 Quench Angle
SUB2
SUB3
Debonding Simulations by G. Vallone

## Slide 8: Subscale 6 Test Results

## Slide 9: Subscale 6 – Thermal 1 + 2
Full wax subscale tested august (T1), october (T2) 2023

## Slide 10: Subscale 6 – Thermal 1 + 2

## Slide 11: Subscale 6 – Thermal 1 + 2

## Slide 12: Subscale 6 – Thermal 1 + 2

## Slide 13: Subscale 6 – Thermal 1 + 2

## Slide 14: Subscale 6 – Thermal 1 + 2

## Slide 15: Subscale 6 – Thermal 1 + 2
The wax subscale test results were just published by Diego, just accepted by Superconductor Science and Technology