## Slide 1: Transverse stress susceptibility of Bi-2212 Rutherford cables at 4.2 K and 11 T
Anna Kario, Simon Otten, Sander Wessel, Jeroen Bijlsma, Mark Smithers, Herman ten Kate, Amalia Ballarino
Tengming Shen (LBNL), Ulf Trociewitz, Daniel Davis, Ernesto Bosque, David Larbalestier (FSU/NHMFL)

## Slide 2: Motivation: stress in Bi-2212 dipole magnets
80 to 105 MPa azimuthal stress present in recent high-field Bi-2212 dipole magnet designs
Apart from one early date test, there are no systematic test data existing on cables
It would be useful to have experimental data on stress limits for recent Rutherford Bi-2212 cables
Zlobin et al. (2023) https://doi.org/10.1109/TASC.2023.3264165
Zlobin et al. (2022) https://doi.org/10.1109/TASC.2022.3158635
104 MPa peak stress
80 MPa peak stress
96 MPa peak stress
Garcia Fajardo et al. (2022) https://doi.org/10.1109/TASC.2023.3264788
Results are also highly relevant for high-field solenoids under high radial compressive load!

## Slide 3: Content
Bi-2212 samples and test setup
Sample preparation
Transverse stress results
Microstructural analysis of cable ross-sections
Conclusion
Bi-2212 Rutherford cable
Cable press in 11 T solenoid

## Slide 4: Bi-2212 Rutherford cable samples
 | Sample 3 | Sample 4
Cable no. | LBNL1109 | LBNL2002
Number of strands | 17 | 
Size excl. insulation | 7.8 mm x 1.4 mm | 
Twist pitch | 58 mm | 
Bi-2212 wire | Nontwisted PMM180207_4, 5, 6 ,7, 55x18, 0.8mm, Engi-mat powder LXB103 | PMM190118, 55x18, 0.8mm, Engi-mat LXB156
Insulation | Mullite sleeve, 150 µm thick | 
Test date at Uni. Twente | December 2022 | June 2023
Zhang et al. (2018), https://doi.org/10.1088/1361-6668/aada2f
Two sample were tested at Uni. Twente in transverse stress set-up
Wire cross-section (Zhang et al.)
0.8 mm
7.8 mm
1.4 mm
Cable cross-section

## Slide 5: Transverse stress setup
50 kA superconducting transformer
11 T solenoid magnet
250 kN press
4.2 K helium bath
50 kA trans-former
Image by Boschman et al.
https://doi.org/10.1109/20.133551
Sample holder
11 T solenoid
Press coils

## Slide 6: Content
Bi-2212 samples and test setup
Sample preparation
Transverse stress results
Microstructural analysis of cable ross-sections
Conclusion
Bi-2212 Rutherford cable
Cable press in 11 T solenoid

## Slide 7: Rutherford cable after heat treatment
The samples were heat treated at NHMFL in 49:1 mixture of argon and oxygen with a total gas pressure of 50 bar (892°C)
Pictures of sample 4 after heat treatment
46 mm
Stainless steel reaction holder
Bi-2212 Rutherford cable in mullite sleeve
Bi-2212 Rutherford cable in mullite sleeve
Removed from the holder

## Slide 8: Epoxy impregnation
Vacuum impregnation with CTD-101k at 60°C, 0.6-0.8 mBar
Cured for 5 hour at 110°C and 16 hour at 125°C in a furnace
Sample holder
Heated resin container
Rod for moving the sample
45 mm pressed section
Impregnation setup
Sample surface after heat treatment
Vacuum chamber
50 cm

## Slide 9: Pushing block positioning
Block glued onto the sample with Stycast 2850FT/23LV and three layers of glass fibre ribbon
Pushed area is 8.1 mm x 45 mm = 3.654 cm2
Pushing block
Alignment plates
(removed when Stycast cured)
Strain gauge (CFLA-6-350-17) on each side of the pushing block
Attached with cyano-acrylate glue (TMI CN)

## Slide 10: Sample connection to the transformer
Transformer
Sample holder
Joints
Pushing block
Soldered over with SnAg. Fixed with Stycast.
Bi2212-Rutherford cable

## Slide 11: Content
Bi-2212 samples and test setup
Sample preparation
Transverse stress results
Microstructural analysis of cable ross-sections
Conclusion
Bi-2212 Rutherford cable
Cable press in 11 T solenoid

## Slide 12: Initial VI curves
T = 4.2 K, Ba = 11 T, σ = 10 MPa
Voltage measured on 6 strands and current leads; they all look smooth and consistent
Voltage criterion of 4.5 µV results from Ec = 10-4 V/m and 45 mm pushing block length
Sample 3: LBNL1109 (Dec 2022)
Ic = 2.70 kA
n = 15
Vc = 4.5 µV
Sample 4: LBNL2002 (June 2023)
Ic = 4.07 kA
n = 15
Vc = 4.5 µV

## Slide 13: Initial Ic(B) curve
Chart: applied magnetic field [T]
| 11.012490892310684 | 9.0104556273376399 | 7.0099622739269121 | 5.0081143440034976
Cable 3 (Ic) | 2695.5 | 2846.8333 | 3063.1667 | 3291.6667
Cable 4 (Ic) | 4069.1667 | 4320.6667 | 4637.8333 | 5068.8333
Cable 3 (n) | 14.65 | 14.5 | 14.6517 | 14.0167
Cable 4 (n) | 14.4833 | 14.6333 | 14.3 | 13.95
Sample 4 Ic (new)
Sample 3 Ic
n-values
Comparison of samples:
Sample 3: LBNL1109, tested Dec 2022
Sample 4: LBNL2002, tested June 2023
Engineering current density at 5 T applied field using 7.8 mm2 cross-sectional area is: 422 A/mm2 for sample 3,
650 A/mm2 for sample 4 (54% increase)
n-values are 14 to 15 for both samples and all applied fields in the range 5 to 11 T.
Critical current and n-values at 10 MPa, 4.2 K

## Slide 14: Critical current versus transverse stress
Chart: average transverse stress [MPa]
| 10.019986663489492 | 19.972634592337041 | 29.903326541877416 | 39.888676028668662 | 50.006113571162103 | 59.949970910804616 | 69.934716131811228 | 79.698056627015262 | 90.003236648046126 | 99.983804599953729 | 109.85769540693157 | 119.93797270893079 | 129.92657964134418 | 139.92524114286164 | 149.85772006985431 | 159.91658125610417 | 169.84619221677559 | 179.92918275056479 | 189.94101747086168 | 199.87366886030671
pressure applied | 1 | 1.0009 | 1.0022 | 1.0021 | 1.0004 | 0.99722 | 0.99586 | 0.9953 | 0.9919 | 0.98757 | 0.9864 | 0.98331 | 0.97966 | 0.97675 | 0.9723 | 0.96593 | 0.96068 | 0.95455 | 0.94707 | 0.93934
unloaded to 10 MPa | 1.001 | 1.0025 | 1.0011 | 0.99536 | 0.99858 | 0.99678 | 0.99277 | 0.99413 | 0.99085 | 0.98429 | 0.98176 | 0.98127 | 0.97879 | 0.97162 | 0.96828 | 0.9637 | 0.95449 | 0.95091 | 0.94336
Chart: average transverse stress [MPa]
| 10.045113099029052 | 20.021794793255058 | 29.975497264251342 | 39.956086136228443 | 49.972307982720253 | 60.002780711478451 | 69.898001660618846 | 79.868671034121576 | 90.024450725337545 | 100.02554545601674 | 110.00583476535391 | 119.98183510271123 | 129.98350510168112 | 139.91418838238221 | 150.00919051663405 | 159.95168952943004 | 169.98168974422381 | 179.95886124762399 | 189.90078556954299 | 199.87760550763213
pressure applied | 1 | 0.99721 | 0.99492 | 0.99353 | 0.99033 | 0.99005 | 0.988 | 0.98161 | 0.97948 | 0.97416 | 0.96682 | 0.96125 | 0.95331 | 0.94499 | 0.94082 | 0.92632 | 0.91534 | 0.90358 | 0.8888 | 0.87463
unloaded to 10 MPa | 0.9973 | 0.99611 | 0.99365 | 0.99078 | 0.99009 | 0.98812 | 0.98407 | 0.98014 | 0.97567 | 0.96785 | 0.9642 | 0.95658 | 0.94684 | 0.93963 | 0.93045 | 0.92087 | 0.90625 | 0.89539 | 0.87598
Applied field 11 T, data normalized to initial Ic of 2.70 kA (sample 3), and 4.07 kA (sample 4)
Measurement sequence:
  10 MPa
  20 MPa
  10 MPa
  30 MPa
  10 MPa
  40 MPa
  etc.
5% degradation reached at: 170-200 MPa in sample 3 and 120-150 MPa in sample 4
Ba = 11 T
Sample 3: LBNL1109 (Dec 2022)
Sample 4: LBNL2002 (June 2023)
Ba = 11 T

## Slide 15: Comparison of the two samples 3 and 4
Sample comparison
Sample 3: LBNL1109, tested Dec 2022
Sample 4: LBNL2002, tested June 2023
Stronger stress dependence observed in sample 4, at 150 MPa:
Sample 3 has 3% degradation, whereas
Sample 4 has 6% degradation
Chart: average transverse stress [MPa]
| 10.019986663489492 | 19.972634592337041 | 29.903326541877416 | 39.888676028668662 | 50.006113571162103 | 59.949970910804616 | 69.934716131811228 | 79.698056627015262 | 90.003236648046126 | 99.983804599953729 | 109.85769540693157 | 119.93797270893079 | 129.92657964134418 | 139.92524114286164 | 149.85772006985431 | 159.91658125610417 | 169.84619221677559 | 179.92918275056479 | 189.94101747086168 | 199.87366886030671
Sample 3 | 1 | 1.0009 | 1.0022 | 1.0021 | 1.0004 | 0.99722 | 0.99586 | 0.9953 | 0.9919 | 0.98757 | 0.9864 | 0.98331 | 0.97966 | 0.97675 | 0.9723 | 0.96593 | 0.96068 | 0.95455 | 0.94707 | 0.93934
Sample 4 | 1 | 0.99721 | 0.99492 | 0.99353 | 0.99033 | 0.99005 | 0.988 | 0.98161 | 0.97948 | 0.97416 | 0.96682 | 0.96125 | 0.95331 | 0.94499 | 0.94082 | 0.92632 | 0.91534 | 0.90358 | 0.8888 | 0.87463
Critical current as function of transverse stress
Ba = 11 T
The difference between the samples at 100 MPa is 1.5% and at 150 MPa is 3% only
Globally, from a magnet application point of view, the samples behave practically the same.

## Slide 16: Ic(B) curves after applying 200 MPa
Sample 3: LBNL1109 (December 2022)
7 to 8% field-independent Ic reduction
n-value dropped by 1 to 2 points
Sample 4: LBNL2002 (June 2023)
12 to 13% field-independent Ic reduction
n-value dropped by 2 to 3 points
σ = 10 MPa
Chart: applied magnetic field [T]
| 11.012490892310684 | 9.0104556273376399 | 7.0099622739269121 | 5.0081143440034976
Ic_mean (begin) | 2695.5 | 2846.8333 | 3063.1667 | 3291.6667
Ic_mean (end) | 2479.6667 | 2640 | 2833.3333 | 3072.8333
n_mean (begin) | 14.65 | 14.5 | 14.6517 | 14.0167
n_mean (end) | 13.2667 | 13.3167 | 13.2833 | 13.0167
σ = 10 MPa
Chart: applied magnetic field [T]
| 11.012634996195011 | 9.0122569258917444 | 7.0106539725716885 | 5.0081143440034976
Ic_mean (begin) | 4069.1667 | 4320.6667 | 4637.8333 | 5068.8333
Ic_mean (end) | 3564.5 | 3788.6667 | 4062.8333 | 4411.5
n_mean (begin) | 14.4833 | 14.6333 | 14.3 | 13.95
n_mean (end) | 12.3 | 12.2 | 12 | 11.6333
σ = 10 MPa

## Slide 17: Effect of mechanical load cycling 10 to 200 MPa
Sample 3: LBNL1109 (December 2022)
2.5% Ic reduction after 50 cycles
No significant change in n-value
Sample 4: LBNL2002 (June 2023)
3.6% reduction after 50 cycles
4.6% reduction after 200 cycles
No significant change in n-value
Chart: number of cycles
| 1 | 10 | 20 | 50
Ic_mean | 2542.8333 | 2503.8333 | 2494.5 | 2479.6667
n_mean | 13.55 | 13.4667 | 13.38 | 13.2667
Ba = 11 T
Chart: number of cycles
| 1 | 10 | 20 | 50 | 100 | 200
Ic_mean | 3564.5 | 3496 | 3471 | 3437.3333 | 3412.6667 | 3402
n_mean | 12.3 | 12.2 | 11.9167 | 11.8167 | 11.8667 | 11.8667
Ba = 11 T
Load cycling Ic reduction at 200 MPa is modest (some 5 %), and saturating (good) .

## Slide 18: Content
Bi-2212 samples and test setup
Sample preparation
Transverse stress results
Microstructural analysis of cable ross-sections
Conclusion
Bi-2212 Rutherford cable
Cable press in 11 T solenoid

## Slide 19: Microstructural analysis cross-sections of sample 3
5 cross-sections examined (200 MPa, 8% Ic decrease)
No obvious damage seen yet, main degrading cause not yet identified
Ic-degradation = broken current path + some residual stress redistribution effect
In Nb3Sn we see filament µm-cracking, current in entire filament interrupted
May be here (hypothesis, for discussion) we brake with nm-cracking current path at grain boundaries mainly on surface of filaments, not leading to global cracking……
Sample 4 has seen 300 MPa and -45%, next to be examined….
Silver matrix removed with NH3OH and H2O2
LBNL1109

## Slide 20: Conclusion
Results obtained on 2 Bi-2212 cable samples, another 2 to be tested
Initial whole cable critical current density at 5 T applied field was 422 A/mm2 in sample 3 (LBNL1109) and 650 A/mm2 in sample 4 (LBNL2002)
5% critical current decrease reached at an average transverse stress of 170 to 200 MPa in sample 3 and at 120 to 150 MPa in sample 4
Progressive Ic reduction (but saturating) observed in both samples when cycling between 10 and 200 MPa
All changes in critical current were irreversible
LBNL1109

## Slide 21
24
Ic(B) curves after applying 250 MPa
Sample 5: LBNL1109 (February 2024)
2 % Ic reduction after 50 cycles
No significant change in n-value
Jc = 782 A/mm2 @ 5 T
Cycling between 10 and 125 MPa
Ba = 11 T
Ba = 11 T

## Slide 22: Curve shape observations for samples 3 and 4
Critical current as function of transverse stress
Chart: average transverse stress [MPa]
| 10.019986663489492 | 19.972634592337041 | 29.903326541877416 | 39.888676028668662 | 50.006113571162103 | 59.949970910804616 | 69.934716131811228 | 79.698056627015262 | 90.003236648046126 | 99.983804599953729 | 109.85769540693157 | 119.93797270893079 | 129.92657964134418 | 139.92524114286164 | 149.85772006985431 | 159.91658125610417 | 169.84619221677559 | 179.92918275056479 | 189.94101747086168 | 199.87366886030671
Sample 3 | 1 | 1.0009 | 1.0022 | 1.0021 | 1.0004 | 0.99722 | 0.99586 | 0.9953 | 0.9919 | 0.98757 | 0.9864 | 0.98331 | 0.97966 | 0.97675 | 0.9723 | 0.96593 | 0.96068 | 0.95455 | 0.94707 | 0.93934
Sample 4 | 1 | 0.99721 | 0.99492 | 0.99353 | 0.99033 | 0.99005 | 0.988 | 0.98161 | 0.97948 | 0.97416 | 0.96682 | 0.96125 | 0.95331 | 0.94499 | 0.94082 | 0.92632 | 0.91534 | 0.90358 | 0.8888 | 0.87463
Sample 4 + 50 MPa | 1 | 0.99721 | 0.99492 | 0.99353 | 0.99033 | 0.99005 | 0.988 | 0.98161 | 0.97948 | 0.97416 | 0.96682 | 0.96125 | 0.95331 | 0.94499 | 0.94082 | 0.92632 | 0.91534 | 0.90358 | 0.8888 | 0.87463
Ba = 11 T
Sample 3 shows negligible degradation up to 50 MPa (no significant initial slope)
Sample 4 shows immediate degradation (clearly visible slope)
But the global shape of the curves is the same…..
When sample 4 curve is moved to the right by 50 MPa they nicely overlap.
Why?
Maybe (an unproven guess) sample 4 has a 50 MPa stress hot spot in the cable (where and how not known)

## Slide 23: Stress level increase to 300 MPa (1st time ever done)
Sample 4 (after load cycling at 200 MPa, so after some 5% extra reduction)!
Loaded at 250 MPa and 300 MPa
For the 1st time ever a Bi-2212 cable was stressed up to this level
Rough indication of the degradation:
  some 20% at 250 MPa, and
  some 45% at 300 MPa
Chart: average transverse stress [MPa]
| 10.019986663489492 | 19.972634592337041 | 29.903326541877416 | 39.888676028668662 | 50.006113571162103 | 59.949970910804616 | 69.934716131811228 | 79.698056627015262 | 90.003236648046126 | 99.983804599953729 | 109.85769540693157 | 119.93797270893079 | 129.92657964134418 | 139.92524114286164 | 149.85772006985431 | 159.91658125610417 | 169.84619221677559 | 179.92918275056479 | 189.94101747086168 | 199.87366886030671
Sample 3 | 1 | 1.0009 | 1.0022 | 1.0021 | 1.0004 | 0.99722 | 0.99586 | 0.9953 | 0.9919 | 0.98757 | 0.9864 | 0.98331 | 0.97966 | 0.97675 | 0.9723 | 0.96593 | 0.96068 | 0.95455 | 0.94707 | 0.93934
Sample 4 | 1 | 0.99721 | 0.99492 | 0.99353 | 0.99033 | 0.99005 | 0.988 | 0.98161 | 0.97948 | 0.97416 | 0.96682 | 0.96125 | 0.95331 | 0.94499 | 0.94082 | 0.92632 | 0.91534 | 0.90358 | 0.8888 | 0.87463 | 0.77944 | 0.56433
Critical current as function of transverse stress
Ba = 11 T
Typical shape of degradation curve maintains
No sudden collapse but gradually increasing degradation effect

## Slide 24
 |  | JE (A/mm^2) | index n-value
Zone 1.25, Top Witness Sample | 231120_TWENTE_Z1_25_PMM160301_I | 1020.2 | 22.69
Zone 3.0, Bottom Witness Sample | 231120_TWENTE_Z3_0_PMM160301_Ic | 914.7 | 18.53
Zone 1.5, "Left" lead sample | 231120_TWENTE_LEFT_Ic | 912.5 | 17.32
Zone 1.5, "Right" lead sample | 231130_TWENTE_RIGHT_Ic | 897.9 | 15.03
25
Heat treatment