## Slide 1: An ARDAP Project - Enhancing Domestic Production of High Temperature Superconducting Bi2Sr2CaCu2Ox/Ag wires for High Field Magnets
Tengming Shen, LBNL
8th US Magnet Development Program Annual collaboration meeting, Fermilab, 04/30/2024-05/03/2024
ARDAP

## Slide 2: Motivations and background – wire front
2 kg billets
10 kg billets
Data by Dr. Jianyi Jiang, NHMFL with Billets from SBIR-STTR, CPRD.

## Slide 3: Motivations and background – cable and magnet fronts
Made from 10 kg billet.
Made from 2 kg billets.
Made from a 2 kg billet.
Conductor science
Cable/coil fab

## Slide 4: Task overview
Task 1: Making precursor powder reproducible and improving production yield
Task 2: Manufacturing (five) 2 kg billets with reproducible plateau JE(4.2 K and 5 T) > 1100 A/mm2
Task 3: Manufacturing (two) 10 kg billets with the target JE(4.2 K and 5 T) > 1100 A/mm2
Task 4: Powder and wire characterization
Task 5: Understanding the science and technology of attaining high JE in Bi-2212 Rutherford cables
Task 6: Demonstrating predictability in Bi-2212 coil heat treatment
Task 7: Insulation and leakage reduction for Rutherford cable coils
Task 8: Contracts to procure powder as a strategic reserve
A lot of new data
and understanding.
New insulation test.
Coil winding in progress.
Two billets produced.

## Slide 5: Project team and management
A virtual knowledge hub formed by private and public businesses, national labs and university
Yibing Huang
Michael Brown
Daniel Bugaris
Claudia Goggin
Daniel Davis, Ulf Trociewitz, Yongjae Kim
Jianyi Jiang, Eric Hellstrom
Tengming Shen*,
Jean-Francois Croteau, Marek Mosat, Chris Escobar
Fast-tempo.
Project-like management with milestones and risk mitigation measures.
Supplemented by DOE-OHEP.

## Slide 6: Task 1-4 – powder, wire manufacturing and characterization
First 2 kg billet produced and received at LBNL.
Second 2 kg billet produced and QA/QC ongoing.
Third billet (10 kg billet) powder in production.
  1st batch with some secondary phase agglomeration.
Enhancing industry ability, product performance, and reproducibility
First cable in May.
ARDAP billet #1
(Potential end effect in this set of samples)
NEW understanding found by J. Jiang
(D. Larbalestier next)

## Slide 7: [Task 5] The science and art of fabricating 2212 Rutherford cables have yet been fully established
7
LBNL 17-strand Rutherford cable
Mullite braided insulation
Bi-2212
LBNL 9-strand Rutherford cable

## Slide 8: Technical progress
Task 5: Understanding the science and technology of attaining high JE in Bi-2212 Rutherford cables
Strands | Powder | Coils
19 x 36, 0.8 mm strands | Nexans | RC1
37 x 18, 0.8 mm strands. | Nexans | RC2/3
55 x 18, 0.8 mm strands. | Engi-Mat | RC5/6/7/8, BIN5c1, BIN5OLa, Bi-CCT1OLa, Bi-CCT1ILb/c.
~13%
After 50 bar OPHT
Shen et al., Scientific Reports Vol. 9, Art. No.: 10170 (2019) ​
Zhang et al Supercond. Sci. Technol. 31 105009 (2018)
Shen et al., Phys. Rev. Accel. Beams 25, 122401 (2022);

## Slide 9: Technical progress
Task 5: Understanding the science and technology of attaining high JE in Bi-2212 Rutherford cables
Wire PMM170725, the wire used in cable 1093 and the magnet CCT BIN5c, 0.8 mm wire, 55 x18
Wire PMM211105, the candidate wire for the magnet Bi-CCT2. 1.0 mm wire, 55x18
Wire PMM220802, used for ARDAP CCT BIN5e magnet, 0.8 mm wire, 37 x18
19 x 36
37 x 18
55 x 18

## Slide 10: Experiments
1. 50 bar OP-PD (830 °C/12 hrs) for measuring cross section area
2. 50 bar-OPHTs: Tmax = 885.5 °C and 890.5 °C
3. Cross sections of OP-PD samples
4. Cross sections of OP-HT samples
5. JE of OP-HT samples
By Jianyi Jiang, FSU

## Slide 11: 50 bar OP-PD (830 °C/12 hrs)
Round
S10
S15
S20
S25
S30
By Jianyi Jiang, FSU

## Slide 12: JE versus rolling reduction – Wire PMM170725, 0.8 mm, 55x18
Reduction in JE (read data points to closest 25 A/mm2)
Tmax = 885.5 C 33%-% (lowest JE)
Tmax = 890.5 C -13% (lowest JE)
By Jianyi Jiang, FSU

## Slide 13: JE versus rolling reduction – Wire PMM211105, 1.0 mm, 55x18
Reduction in JE
Tmax = 885.5 C -14% (plateau)
Tmax = 890.5 C -20% (10% rolling)
Tmax = 890.5 C -12% (plateau)
By Jianyi Jiang, FSU

## Slide 14: Image Analysis of Filaments in Rolled Strands (PMM220802)
Area
Aspect Ratio
Shear bands from rolling
*colormap scales are relative to each image
Chris Escobar, UC Berkeley
engineering, undergraduate
Jean-Francois Croteau

## Slide 15: Task 5 – cable fabrication – a cable that allows easy characterization and a good candidate for commercial applications 4-20 K
First billet, 37x18 wire, drawn to 0.7 mm.
The 0.7 mm strand will be made into a 6-strand Rutherford cable about 2.40 mm x 1.25-1.1.
No. strands | Nominal dimensions | Cable twist pitch (mm) | Strand diameter and design | Projected Ic at 31 T (A)
6 | 2.4 mm x 1.25 mm | 15 - 21.9 | 0.7 mm and 37 x 18 | 1150
Table 2: A Rutherford cable to be fabricated for cable properties evaluation and as a potential solenoid conductor
Cable thickness can be decreased to 1.1 mm to increase the packing factor from ~78.5% to 88.5%.
Cable characterization in ITER barrels at 4K and 31 T@NHMFL.
~80 or 160 m cable will be available for coil tests/developments with ASC’s 15 T, 52 mm bore oxford magnet and 31 T, 39 mm bore magnet.
Magnet time being applied by D. Davis, NHMFL and coil development by Davis, Trociewitz, Kim.

## Slide 16: Task 7 – new insulation and removing leakage
7 m insulation braiding and coil winding trial completed.
24 m pure alumina insulated cable received.
Winding of the first coil completed.
By Youngjae Kim, FSU et al.
CCT ARDAP coil BIN5E:
  Outer layer coil wound. No electrical shorts.
  Have to use TiO2 slurry to “repair, reinforce and lubricate” alumina fibers.
  Possible to replace TiO2 slurry with Al2O3 slurry (courtesy of Dr. Jun Lu, NHMFL)
ARDAP CCT coil BIN5E_OL, after winding, not yet reacted.
CCT ARDAP coil BIN5E:
  Inner layer coil wound. No electrical shorts.
  NEW: Use Al2O3 slurry to “repair, reinforce and lubricate” alumina fibers. (courtesy of Dr. Jun Lu, NHMFL)

## Slide 17: Summary
A virtual knowledge hub formed by private and public businesses, national labs and university, supported by DOE-ARDAP, to improve Bi-2212 conductor and coil technology.
Task 2: Manufacturing (five) 2 kg billets with reproducible plateau JE(4.2 K and 5 T) > 1100 A/mm2
Task 3: Manufacturing (two) 10 kg billets with the target JE(4.2 K and 5 T) > 1100 A/mm2
New data obtained to assist understanding the science and technology of attaining high JE in Bi-2212 Rutherford cables
6-strand Rutherford from 0.7 mm wires enable fast-turn-around tests.
New insulation trial on LBNL CCT coil.

## Slide 18: Thank You

## Slide 19: Image Analysis of Filaments Rolled Strands (PMM211105)
Area
Aspect Ratio
*colormap scales are relative to each image
Chris Escobar, UC Berkeley
engineering, undergraduate
Jean-Francois Croteau