## Slide 1: Distributed Fiber optic strain measurement system for the CORC-based CCT
Linqing Luo
5/2/2024

## Slide 2: Acknowledge
Colleagues: Hugh Higley, Derek Hochvert, Simone Johnson, Bob Memmo, Mike Naus, Matt Reynolds, Tengming Shen, Chet Spencer, Reed Teyber, Marcos Turqueti，Xiaorong Wang.
Funding support from DOE Office of Fusion Energy Sciences and the U.S. MDP from Office of High Energy Physics.

## Slide 3: Outline
Motivation
Introduction of distributed fiber optic sensing
Test Setup
Result and discussion
Conclusion

## Slide 4: Motivation
Distributed temperature sensing may help avoid catastrophic thermal runaway
Fiber optic sensing is an available distributed sensing technology
But a significant gap for applications in cryogenic environment
Burnup due to thermal runaway
Identify the location of local heating in order to understand and improve the CORC magnet and conductor fabrication.
Lu et al. 2019. “Distributed Optical Fiber Sensing: Review
and Perspective.” Applied Physics Reviews 6 (4): 041302.

## Slide 5: Distributed fiber optic sensing
Rayleigh, Raman, and Brillouin scattering
Backscattered spectrum
Buffer
250 µm
Core
9 µm
Cladding
125 µm
Coating
>175
diameter
where is the spectral frequency shift, is the linear coefficient for temperature, is the temperature change, is the strain change, and is the linear coefficient for strain.

## Slide 6: Test setup
Four optical fibers, each installed at:
  Shell
  Layer 1
  Layer 2
  Layer 6
Fiber at each layers are impregnated by Stycast.
Fiber at the outer shell is epoxy with Araldite.
Measurement frequency: 4.17Hz
6 channels fiber are measured at same time
Spatial resolution: 2.6mm.
1
2
6
Shell

## Slide 7: Test Setup
Shell fiber
Optical fiber extension cable

## Slide 8: Test
All tests: 6 Layers are connected in series
Liquid helium test (4.2K)
Room temperature test
  First Ramp: 5A, 0.385V
  After that: Each ramp 10 A, 0.77V
All the plots had baselines as the first data of the same plot
Current input for the liquid helium test

## Slide 9: Liquid Helium test

## Slide 10: Shell fiber response
Compression
Tension
Tension
Compression
2000A
3000A
4000A
5000A
5500A
5500A
6500A
7000A
7500A
8000A
8500A
9000A
9500A
9000A
Special event
Slow ramp 9000A
Unexpected current surge
->
Deformation
Remains for at least 9 hrs

## Slide 11: Shell
Loop 1 Strain
Loop 2 Strain
Shell response in one current input ramp
Fiber response VS current square

## Slide 12: Layer 1
Phase change of the blue line
The residual shows mechanically deformation?
The rising with ramps shows thermal?
But disappearing fast->still mainly strain.
Phase change-> strain then thermal?

## Slide 13: Layer 2

## Slide 14: Layer6

## Slide 15: Layer 1, Layer 2, Layer 6 fiber response VS current square

## Slide 16: Room temperature test after the 4.2 K test

## Slide 17: C3A_3turn_6Layers in Room temperature
Layer 1
As the current power input is low, the Lorentz force leaded mechanical deformation maybe small.
The rising up is mainly contributed by thermal generated inside the 6 layers magnet.
The drift is mainly due to the ambient temperature rise.

## Slide 18: C3A_3turn_6Layers in Room temperature
Layer 2

## Slide 19: C3A_3turn_6Layers in Room temperature
Shell

## Slide 20: C3A_3turn_6Layers in Room temperature
Layer 6
At some locations, there are more heat detected.
These locations are close to the mid-plane of the coil.

## Slide 21: Layer 6 Comparison between Room temperature and liquid helium test
Room temperature test
4.2 K test

## Slide 22: Conclusion
Optical fiber survived in liquid helium and can be used for sensing strain and temperature;
Optical fiber measures the temperature change in the room temperature (<5.5mW/cm);
Optical fiber measures the strain deformation of the shell under Lorentz force;
Optical fiber may measure the thermal change of the magnet if there is temperature change in 4.2 K.

## Slide 23: Next step for C3-40 turn magnet
Cable length range from 10 to 40 m.
Sensitivity and survival rate of the sensor needs to be improved
  Special installation method
  Different optical fiber design
    Signal to noise ratio improvement
    Radiation tolerance
  Customized interrogators
Chart: Raw data STD in GHz along distance
| Bending Insensitive, ZYVAX+Apiezon | Higher Mode, ZYVAX+Apiezon | Bending Insensitive, Apiezon | Higher Mode, Apiezon | Single mode Polyimide fiber, ZYVAX | Single mode Polyimide fiber, ZYVAX2 | Single mode Polyimide fiber, Apiezon
First 0.5m | 0.0999 | 0.0979 | 0.0747 | 0.061 | 0.23 | 0.3185 | 0.0575
Last 0.5m | 0.1152 | 0.0819 | 0.1336 | 0.056 | 0.6297 | 0.2652 | 0.2068
Degredation per meter | 0.004793 | -0.0050123 | 0.037444 | -0.0031786 | 0.16508 | -0.022585 | 0.05317

## Slide 24: C3A_3Turn_6Layer in Room temperature, ambient temperature from night to day
Layer 1

## Slide 25: C3A_3Turn_6Layer in Room temperature, Heating second day
Layer 1

## Slide 26: C3A_3Turn_6Layer in Room temperature, ambient temperature from night to day
Layer 2

## Slide 27: C3A_3Turn_6Layer in Room temperature, Heating second day
Layer 2

## Slide 28: C3A_3Turn_6Layer in Room temperature, ambient temperature from night to day
Shell
Shell is colder at night

## Slide 29: C3A_3Turn_6Layer in Room temperature, Heating second day
Shell

## Slide 30: C3A_3Turn_6Layer in Room temperature, ambient temperature from night to day
Layer 6

## Slide 31: C3A_3Turn_6Layer in Room temperature, Heating second day
Layer 6