## Slide 1: KEK Cryogenics Science Center
High Precision
J-PARC g-2/EDM
High Radiation Hardness
J-PARC COMET
High Field
HL-LHC D1

## Slide 2: Superconducting Magnet R&D for g-2/EDM experiment, MuSEUM experiment
g-2/EDM Superconducting Magnet System
Muon Storage Solenoid with high precision magnetic field extending MRI technologies
  Yoke design modification was just started for kicker coil power line optimization
Precision magnetic field measurement system
NMR magnetic field measurement system with ultra high accuracy of a couple of ppb -> Making new design
  To cancel RF interference btw probes, they should be covered by Al shield box separately.
International collaboration with FNAL and ANL
  Cross calibration of NMR probes, that are individually developed : -> Increase validity
Cross calibration between US and JP probes
New design of field mapping system
Tilted hole
Straight hole
Preparation of MuSEUM experiment
Muonium hyper fine structure measurement in J-PARC
  Experimental area (H1) is ready in Nov. 2023
  Magnet was moved to the area, and ramped up.
  Plan
    Shimming work : Mar. 2024
    Beam run : Apr. - Jun. 2024
Previous prototype
MRI magnet in H1 area

## Slide 3: COMET magnet system
CS coil
COMET Phase-a operation
  Inject J-PARC’s proton beam to the COMET beamline
    Without capture solenoid
  Four excitation runs,
    Three with the dipole negative pole (Negative muons enhanced)
    One at the positive pole (Positive muons).
  Profile on the beam transported by the TS
  Succeeded in observing muon beams transported by the TS
BS 磁石
Capture Solenoid Construction
  Under Assembly at Mitsubishi Electric
  Electric failure of CS coldmass arose has been repaired
  Assembly of CS and TS1 subassemblies is complete
  (Coil connection, piping, radiation shield assembly, vacuum vessel assembly, etc.)
  Final magnet assembly underway
TS1 subassembly
CS subassembly
Notes: For radiation hard technologies, the construction of superconducting magnets for the muon-to-electron conversion search experiment (COMET) is underway and developed into the rad-hard superconducting magnet technology for future large-intensity accelerator applications, including the MLF second target station.
For COMET, the construction of capture solenoid is underway. due to the electric failure found in a coil the schedule is delayed. The construction of transport solenoid is almost completed and cold test was performed. Although there are some issues with mechanical structure was found the issue was resolve with additional supports. Field measurement was also performed and the results were satisfactory,
For rad-hard superconducting magnet technologies, various studies such as studies of radiation hardness of various magnet materials including superconductors, and development of rad-hard insulation technologies are underway in a collaboration with some US and Japanese institutes. (LBNL, BNL, UC Berkeley, and Kyoto Univ.)

## Slide 4: HL-LHC D1 magnet construction
Beam separation dipole (D1) by KEK
  Design study of D1 for HL-LHC within the framework of the CERN-KEK collaboration since 2011.
  150 mm single aperture, 35 Tm (5.6 T x 6.3 m), Nb-Ti technology.
  Development 2-m long model magnets (3 units) at KEK
Deliverables for HL-LHC
  1 full-scale prototype cold mass (LMBXFP)
  6 series cold masses (LMBXF1-6)
So far, 3 magnets have been tested at KEK.
  2 series magnets (MBXF1&5) successfully demonstrated to reach the ultimate current of 13.2 kA (108% of nominal current).
New beam interaction region SC magnet system for HL-LHC
First D1 prototype (MBXFP1) was delivered to CERN (April, 2023) and the cold test is underway in horizontal cryostat.
MBXFP1 was stably operated at the ultimate current for 8 hours.

## Slide 5: R&D of Nb3Sn conductor for future high field accelerator magnet
Nb3Sn conductor development for FCC
in collaboration with CERN
Characterization of Nb3Sn conductors
Compression
Compressive
stress
Nb3Sn wire
with Cu-Nb reinforcement
without reinforcement
Degradation by transverse compressive stress
Neutron diffraction experiments
Achievement in the R&D of the 1st phase (2017~2022)
Phase evolution during HT
In-situ internal strain measurement
under transverse compression
J-PARC/MLF
BL19(TAKUMI)
Stress limit
DT wire with Jc=1100 A/mm2
• Jc improvement by 40% in the Distributed-Tin wire
• Fabrication of short Rutherford cables
Targets in the R&D of the 2nd phase (2024~2027)
• Longer piece length with Jc sufficient for 12T magnet
• Enhancement of Jc towards 1500 A/mm2 at 4.2K, 16 T
• Mechanical reinforcement for transverse compression
Axial
Radial perpendicular
to the loading axis
Radial along
the loading axis
40%
non-Cu Jc>1100 A/mm2
at 4.2 K, 16 T
f1.0 mm
Lattice spacing (Å)

## Slide 6
A collaboration framework to advance high-temperature superconducting magnets for accelerator facilities
Toru Ogitsu1 and Tengming Shen2 for the project team
KEK, 2. Lawrence Berkeley National Laboratory,
Kyoto University, Brookhaven National Laboratory & UC Berkeley
UNIVERSITY OF
CALIFORNIA
A proposal to the U.S.-Japan Science and Technology Cooperation Program in High Energy Physics

## Slide 7
Task 1: Irradiation Test of HTS Conductors
LBNL
88”Cyclotron
UC Berkeley Hot-Lab
FIB-SEM, TEM
Tohoku U. Oharai Center
Hot-Lab 15T Ic Meas. Inst.
Irradiation Sample
JAEA:JRR3
IrSmp
BRR3
Irrad. Samp.
Irrad. Samp
GdBCO
w/wo shield
GdBCO
EuBCO
YBCO
KEK
UC Berkeley
LBNL

## Slide 8
Task 2: Quench Stability and Protection of Spiral conductors
Student and Technology Exchange
Kyoto
Univ.
LBNL
SCSC Cable developed by Kyoto U.
Short sample test stand at Kyoto U.
KEK
Advanced quench protection technologies
BNL
Advanced quench protection technologies
Quench detection
system at BNL

## Slide 9
Task 3: AC Loss and Field Quality of HTS magnet
Kyoto Univ.
LBNL
Nb3Sn coils
REBCO (flat racetrack) coils
Field Simulation of Task 4 coil test
AC Loss computation of SCSC Cable
KEK
Student and Technology Exchange
CT1 Magnet Excitation Test Set Up

## Slide 10
Task 4: HTS/LTS high field hybrid accelerator dipole
KEK
BNL
HTS Racetrack coil with Inorganic Insulation
10T Test Magnet
Bipolar Power Supply
Insert Coil

## Slide 11
Task 4; FY2024-2026
SCSC Cable
Taking advantage of successful achievements with SCSC cable by Kyoto U. in Task 2 and 3 (with external funding)
Develop 2 types of test racetrack coils
1 SCSC coil
2 CORC coil (CORC is SCSC like but without striation)
Test these coils at BNL 10T test stand
Compare field error associated with shielding current
And mechanical properties of cables.
CORC Cable

## Slide 12: Other Developments
J-PARC Hadron E80 Experiment Detector Solenoid
  Construction & Development Support
J-PARC MLF Second Target Muon Capture Solenoid
  Design Study R&D Support
    High-Rad HTS Magnet R&D
Super KEKB QCS Upgrade (FNAL-KEK Collaboration)
  R&D Support
    Quench Protection Study for High Current Density SCM
PF Superconducting Multi-Wiggler
  R&D Support
    Quench Protection Study for High Current Density SCM
And more..
  US-JP with FNAL, TUAT and Tokyo U. : IBS development
  CERN-KEK: Revive Aluminum Stabilized NbTi Conductor
MLF Second Target Muon Capture Solenoid
SuperKEKB QC1P

## Slide 13: Resources and Collaborations
Cryogenics Science Center (CSC)
Researcher: 7
Technical Stuff: 7
iCASA
ARL
RSC
CRC
MEC
ACC(Tsukuba)
SuperKEKB
PF
Multi-Wiggler
QCS
ILC SCM etc
IPNS
ITDC
J-PARC
Cryogenics Section
HL-LHC D1 Detector SCM Rad-Hard SCM
g-2/EDM COMET etc
Collaboration
Concurrent appointments
External Collaborators
Tokyo U.
Kyoto U.
Tohoku U.
TUAT
NIMS
Tokai U.
CERN
LBNL
FNAL
BNL
High Field, Rad-Hard SCM
Detector Solenoid etc
HL-LHC D1 etc

## Slide 14: Summary
User Support
  Cryogen Supply: ~140kL Liq. He (90% recovery rate)
  SCM System Operations at J-PARC: no trouble
  Construction and Development of SCM: HL-LHC D1, COMET, g-2/EDM, E80
  R&D support for SCM: SuperKEKB QCS, PF Multi-wiggler, J-PARC Second Target Capture Solenoid, etc…
R&D for future programs
  High Field Rad-hard SCM: CERN-KEK, US-Japan, JSPS, etc
Resources and Collaborations
  Try to compensate resource shortage by widening collaborations