## Slide 1: MQXFA12b coil dimensions
P. Ferracin, Dan Cheng, Jennifer Doyle, Katherine Ray, Michael Solis
on behalf of the MQXF collaboration
MQXFA13b Coils Acceptance Review
January 23rd, 2024
LBNL, Berkeley, CA, USA

## Slide 2: Outline
Data taking and processing
Impregnated coil dimensional tolerances
Results (straight section)
  Arc length excess
  Outer radius profile deviation
  Inner radial deviations (coil blocks)
  Inner radial deviations (pole)
  Key slot deviations
  Best-fit outer radius
Appendix

## Slide 3: Outline
Data taking and processing
Impregnated coil dimensional tolerances
Results (straight section)
  Arc length excess
  Outer radius profile deviation
  Inner radial deviations (coil blocks)
  Inner radial deviations (pole)
  Key slot deviations
  Best-fit outer radius
Appendix

## Slide 4: Data taking and processing
Leica System
  AT960 with T-Probe
Data processed using
  Spatial Analyzer

## Slide 5: Post processing
Each cross section is treated separately.
  Coils cross-sections are measured in 15 different locations along the coil length, from 70 mm close to the lead end to 4426 mm close to the return end.
  The 12 so-called straight section locations, where the pole key slot is present, are from 465 mm close to the lead end to 4310 mm close to the return end.
  The strain gauge is at location 3965 mm.

## Slide 6: Outline
Data taking and processing
Impregnated coil dimensional tolerances
Results (straight section)
  Arc length excess
  Outer radius profile deviation
  Inner radial deviations (coil blocks)
  Inner radial deviations (pole)
  Key slot deviations
  Best-fit outer radius
Appendix

## Slide 7: Impregnated coil dimensional tolerances (for series coils)

## Slide 8: Impregnated coil dimensional tolerances Arc length excess (straight section)
The impregnated coil is accepted for use in MQXFA if its arc length excesses along the straight section are within the following tolerances: +0.150/-0.250 mm
The arc length excess, which is difference between the measured coil arc length and the nominal one, is determined by fitting outer radius and mid-planes points with the nominal profile, with equal weighting and imposing as symmetrical the two mid-planes offsets. The sum of the two measured mid-plane offsets provides the arc length excess

## Slide 9: Impregnated coil dimensional tolerances Arc length excess (ends)
At 260 and 300 mm (for the lead end) and at 4340 and 4380 mm (for the return end) the absolute value of the coil delta arc-length must not exceed 210 mm.
  The coil delta arc-length is the difference between the coil arc length at each location in the ends and the average coil arc-length in the straight section.

## Slide 10: Impregnated coil dimensional tolerances Outer radius profile deviation
The impregnated coil is accepted for use in MQXFA if its outer radius profile deviations along the straight section are within the following tolerances: +0.200/-0.250 mm
The outer radius profile deviation, which is given by the variation of each point on the outer radius with respect to the nominal outer radius, is determined by fitting outer radius and mid-planes points with the nominal profile, with equal weighting and imposing as symmetrical the two mid-planes offsets. Positive deviation indicates more material than nominal, negative indicates less material than nominal.

## Slide 11: Impregnated coil dimensional tolerances “Coil blocks” inner radius profile deviation
The impregnated coil is accepted for use in MQXFA if its “coil blocks” inner radius profile deviations (E-F in next slide) along the straight section are within the following tolerances: +0.150/-0.250 mm
The “coil blocks” inner radius profile deviations, which is given by the variation of each point on the inner radius with respect to the nominal radius, is determined by fitting outer radius and mid-planes points with the nominal profile, with equal weighting and imposing as symmetrical the two mid-planes offsets. Positive deviation indicates more material than nominal, negative indicates less material than nominal.

## Slide 12: Impregnated coil dimensional tolerances

## Slide 13: Impregnated coil dimensional tolerances “Pole” inner radius profile deviation
The impregnated coil is accepted for use in MQXFA if its “pole” inner radius profile deviations (C-E and D-F in next slide) along the straight section are within the following tolerances: +0.000/-0.250 mm*
The “pole” inner radius profile deviations, which is given by the variation of each point on the inner radius with respect to the nominal radius, is determined by fitting outer radius and mid-planes points with the nominal profile, with equal weighting and imposing as symmetrical the two mid-planes offsets. Positive deviation indicates more material than nominal, negative indicates less material than nominal.

## Slide 14: Impregnated coil dimensional tolerances
* Cross-section measurements shall be taken close to all possible bumper locations. In addition, data shall be taken on the surface surrounding the pole holes where bumpers are inserted and projected on the closest measured cross-section.

## Slide 15: Impregnated coil dimensional tolerances Pole key slot mis-alignment
The impregnated coil is accepted for use in MQXFA if its pole key slot mis-alignment along the straight section are within the following tolerances: +0.250/-0.250 mm
The pole key slot mis-alignment, which is the misalignment of the center of the pole key slot with respect to the nominal position, is determined by fitting outer radius and mid-planes points with the nominal profile, with equal weighting and imposing as symmetrical the two mid-planes offsets.
  View from LE, positive shift towards left

## Slide 16: Best-fit outer radius
The best-fit outer radius is determined by best-fitting only the outer radius points.
No tolerance is specified
  Used to monitor coil-to-collar contact surfaces (“LQ effect”)

## Slide 17: Outline
Data taking and processing
Impregnated coil dimensional tolerances
Results (straight section)
  Arc length excess
  Delta arc length excess straight section - ends
  Outer radius profile deviation
  Inner radial deviations (coil blocks)
  Inner radial deviations (pole)
  Key slot deviations
  Best-fit outer radius
Appendix

## Slide 18: Arc length excess

## Slide 19: Impregnated coil dimensional tolerances Arc length excess (straight section)
The impregnated coil is accepted for use in MQXFA if its arc length excesses along the straight section are within the following tolerances: +0.150/-0.250 mm
The arc length excess, which is difference between the measured coil arc length and the nominal one, is determined by fitting outer radius and mid-planes points with the nominal profile, with equal weighting and imposing as symmetrical the two mid-planes offsets. The sum of the two measured mid-plane offsets provides the arc length excess

## Slide 20: Arc length excess straight section

## Slide 21: Arc length excess straight section

## Slide 22: Arc length excess straight section
Conclusions
  All coils with several points out of spec
Action items
  The coils will be shimmed on the mid-plane to compensate

## Slide 23: Outline
Data taking and processing
Impregnated coil dimensional tolerances
Results (straight section)
  Arc length excess
  Delta arc length excess straight section - ends
  Outer radius profile deviation
  Inner radial deviations (coil blocks)
  Inner radial deviations (pole)
  Key slot deviations
  Best-fit outer radius
Appendix

## Slide 24: Impregnated coil dimensional tolerances Arc length excess (ends)
At 260 and 300 mm (for the lead end) and at 4340 and 4380 mm (for the return end) the absolute value of the coil delta arc-length must not exceed 210 mm.
  The coil delta arc-length is the difference between the coil arc length at each location in the ends and the average coil arc-length in the straight section.

## Slide 25: Arc length excess full length

## Slide 26: Arc length excess LE

## Slide 27: Arc length excess RE

## Slide 28: Delta between arc length excess straight section and spacer-wedge transition

## Slide 29: Delta arc length excess straight section - ends
Conclusions
  All coils except 150 within spec
    225 and 225 both before and after the loading
  150 marginally out of spec
Action items
  No action items

## Slide 30: Outline
Data taking and processing
Impregnated coil dimensional tolerances
Results (straight section)
  Arc length excess
  Delta arc length excess straight section - ends
  Outer radius profile deviation
  Inner radial deviations (coil blocks)
  Inner radial deviations (pole)
  Key slot deviations
  Best-fit outer radius
Appendix

## Slide 31: Outer radius profile deviation

## Slide 32: Impregnated coil dimensional tolerances Outer radius profile deviation
The impregnated coil is accepted for use in MQXFA if its outer radius profile deviations along the straight section are within the following tolerances: +0.200/-0.250 mm
The outer radius profile deviation, which is given by the variation of each point on the outer radius with respect to the nominal outer radius, is determined by fitting outer radius and mid-planes points with the nominal profile, with equal weighting and imposing as symmetrical the two mid-planes offsets. Positive deviation indicates more material than nominal, negative indicates less material than nominal.

## Slide 33: Outer radius profile deviations straight section (min-max)

## Slide 34: Outer radius profile deviations straight section

## Slide 35: Outer radius profile deviations straight section
Conclusions
  All coils within spec
Action items
  No action items

## Slide 36: Outline
Data taking and processing
Impregnated coil dimensional tolerances
Results (straight section)
  Arc length excess
  Delta arc length excess straight section - ends
  Outer radius profile deviation
  Inner radial deviations (coil blocks)
  Inner radial deviations (pole)
  Key slot deviations
  Best-fit outer radius
Appendix

## Slide 37: Inner radial deviations (coil blocks)

## Slide 38: Impregnated coil dimensional tolerances “Coil blocks” inner radius profile deviation
The impregnated coil is accepted for use in MQXFA if its “coil blocks” inner radius profile deviations (E-F in next slide) along the straight section are within the following tolerances: +0.150/-0.250 mm
The “coil blocks” inner radius profile deviations, which is given by the variation of each point on the inner radius with respect to the nominal radius, is determined by fitting outer radius and mid-planes points with the nominal profile, with equal weighting and imposing as symmetrical the two mid-planes offsets. Positive deviation indicates more material than nominal, negative indicates less material than nominal.

## Slide 39: Coil blocks inner radial deviations straight section (min-max)

## Slide 40: Coil blocks inner radial deviations straight section

## Slide 41: Coil blocks inner radial deviations straight section
Conclusions
  Some coils marginally out of spec in few positions
Action items
  Non critical non conformity
    Increase of LHe space between cold bore and inner coil in one location

## Slide 42: Outline
Data taking and processing
Impregnated coil dimensional tolerances
Results (straight section)
  Arc length excess
  Delta arc length excess straight section - ends
  Outer radius profile deviation
  Inner radial deviations (coil blocks)
  Inner radial deviations (pole)
  Key slot deviations
  Best-fit outer radius
Appendix

## Slide 43: Inner radial deviations (pole)

## Slide 44: Impregnated coil dimensional tolerances “Pole” inner radius profile deviation
The impregnated coil is accepted for use in MQXFA if its “pole” inner radius profile deviations (C-E and D-F in next slide) along the straight section are within the following tolerances: +0.000/-0.250 mm*
The “pole” inner radius profile deviations, which is given by the variation of each point on the inner radius with respect to the nominal radius, is determined by fitting outer radius and mid-planes points with the nominal profile, with equal weighting and imposing as symmetrical the two mid-planes offsets. Positive deviation indicates more material than nominal, negative indicates less material than nominal.

## Slide 45: Pole inner radial deviations straight section (min-max)

## Slide 46: Pole inner radial deviations straight section

## Slide 47: Pole inner radial deviations straight section
Conclusions
  Several out of spec positions, in all coils,
    Coil bumper thickness to be corrected to compensate
Action items
    Coil bumper thickness to be corrected to compensate

## Slide 48: Outline
Data taking and processing
Impregnated coil dimensional tolerances
Results (straight section)
  Arc length excess
  Delta arc length excess straight section - ends
  Outer radius profile deviation
  Inner radial deviations (coil blocks)
  Inner radial deviations (pole)
  Key slot deviations
  Best-fit outer radius
Appendix

## Slide 49: Key slot deviations*
  *View from LE, positive shift towards left

## Slide 50: Impregnated coil dimensional tolerances Pole key slot mis-alignment
The impregnated coil is accepted for use in MQXFA if its pole key slot mis-alignment along the straight section are within the following tolerances: +0.250/-0.250 mm
The pole key slot mis-alignment, which is the misalignment of the center of the pole key slot with respect to the nominal position, is determined by fitting outer radius and mid-planes points with the nominal profile, with equal weighting and imposing as symmetrical the two mid-planes offsets.
  View from LE, positive shift towards left

## Slide 51: Key slot deviations

## Slide 52: Key slot deviations

## Slide 53: Key slot deviations
Conclusions
  No data out of spec
*See LBNL note and Record of Decision in Docdb-2844

## Slide 54: Outline
Data taking and processing
Impregnated coil dimensional tolerances
Results (straight section)
  Arc length excess
  Delta arc length excess straight section - ends
  Outer radius profile deviation
  Inner radial deviations (coil blocks)
  Inner radial deviations (pole)
  Key slot deviations
  Best-fit outer radius
Appendix

## Slide 55: Best-fit outer radius
The best-fit outer radius is determined by best-fitting only the outer radius points.
No tolerance is specified
  Used to monitor coil-to-collar contact surfaces (“LQ effect”)

## Slide 56: Best-fit outer radius deviations

## Slide 57: Best-fit outer radius deviations

## Slide 58: Best-fit outer radius deviations
Conclusions
  Data consistent with previous magnets

## Slide 59: Out of specs
Arc length excess
  All coils several points out of spec
    The coils will be shimmed on the mid-plane to compensate
Delta arc length excess straight section – ends
  All coils except 150 within spec
    225 and 225 both before and after the loading
  150 marginally out of spec
Outer radius profile deviation
  All coils within spec
Inner radial deviations (coil blocks)
  Some coils marginally out of spec in few positions
    Non critical non conformity
      Increase of LHe space between cold bore and inner coil in one location
Inner radial deviations (pole)
  Several out of spec positions, in all coils,
    Coil bumper thickness to be corrected to compensate
Key slot deviations
  No data out of spec
Best-fit outer radius deviations
  Data consistent with previous magnets

## Slide 60: Outline
Data taking and processing
Impregnated coil dimensional tolerances
Results (straight section)
  Arc length excess
  Delta arc length excess straight section - ends
  Outer radius profile deviation
  Inner radial deviations (coil blocks)
  Inner radial deviations (pole)
  Key slot deviations
  Best-fit outer radius
Appendix

## Slide 61: Appendix

## Slide 62: Reproducibility
Coil 240, same operator, 2 independent meas.

## Slide 63: CERN coil 140 and 139

## Slide 64: Arc length excess straight section

## Slide 65: Arc length excess straight section (with min/max straight sect and full-length)