## Slide 1: Low radioactivity argon from underground sources
Henning O. Back – Princeton University
LIDINE 2013

## Slide 2: Atmospheric argon limits
Argon-39
  Beta emitter (q = 565 keV, t1/2 = 269 years)
  Produced in the atmosphere through cosmic ray interactions (eg, 40Ar(n, 2n)39Ar)
  Atmospheric abundance
    39Ar/40Ar is 8×10-16 (0.8 ppq)
    Specific activity = 1 Bq/kg
  Is the limiting factor in size and sensitivity for argon detectors
    Limits detector size due to 39Ar event pile-up
    One ton detector
      Electron drift time across 1 ton detector (1m)= order 500μs (minimum time between events, equivalent to 2kHz)
      Atmospheric 39Ar decay rate = 1kHz/ton

## Slide 3: Terrestrial argon sources As I understand them
40Ar comes from 40K decay
Atmosphere
  39Ar produced by cosmic ray neutrons
Crust
  No cosmic ray
  Neutrons from U and Th
Mantle
  Very low U and Th
  Lowest 39Ar levels
Mantle
Low U and Th
(lowest 39Ar)
Crust – 1ppm U and Th (low 39Ar)
Atmosphere (8×10-16 39Ar/40Ar)

## Slide 4: CO2 well is SW Colorado
There are geological formations that trap gases underground
We found CO2 well in SW Colorado (near Cortez)
Contains 600 ppm Argon
39Ar activity < 0.65% of atmospheric argon (arXiv:1204.6011)

## Slide 5: Getting to the argon
Extraction
  In Colorado we extract a crude argon gas mixture (Ar, N2, and He)
Purification
  The gas from Cortez is then sent to Fermilab for further purification

## Slide 6: Absorption of CO2 on 4A zeolite
Siriwardane et al., Energy & Fuels, Vol. 17, No. 3, 2003
VPSA range
0-1.7 bar

## Slide 7: Vacuum Pressure Swing Absorption (VPSA)
Capitalize on pressure dependence of absorption
Absorb CO2 under pressure
Regenerate column under vacuum
Use 2 columns for (near) continuous operation
He, Ar, N2 mixture
Gas from well
Absorbed gas returned to company
Zeolite column
Zeolite column
Gas flows through one column under pressure. CO2, O2, H2O and CH4 are absorbed on zeolite
Simultaneously the other column is pumped on to remove the trapped gases

## Slide 8: Our plant
Gas heaters
First stage
Second stage
Warms gas to avoid liquefaction by to Joule-Thomson cooling
(total ΔP > 750 psi)
Absorbs CO2 and other unwanted gases
Allows Ar, He, and N2 to pass
Reduces N2 content

## Slide 9: VPSA plant
Operated locally by technician Chris Condon – Managed by H. Back

## Slide 10
Chart: Calibration gas versus VPSA stage 2 output
40Ar
36Ar
28N
40Ar
28N
RGA limit

## Slide 11: Production
2010
  Output
    2.5% argon
    70% nitrogen
    27.5% helium
  Production
    23kg argon
2011
  Output
    ~5% argon
  Production
    53kg argon
    Continuous operation:
    May-June & July - October
2012
  Output
    5-7% argon
  Production
    67kg argon
    Duty factor – 57%
2013
  Output
    5-7% argon
  Production (to date)
    ~30kg argon
    Duty factor – 65%
Total underground argon collected to date ~ 173kg

## Slide 12: Purification at Fermilab The Cryogenic Distillation Column
Column is filled with high surface area material
Boiling and condensation happens on the surface of column packing material
Controlling temperature and gas/liquid flows allows for continuous purification
Inject liquefied Ar/N2into column
Waste gas (He and N2)
Product (pure Argon)
Lower boiling point gas preferentially moves up column
Higher boiling point liquid preferentially moves down column
Packed column
Temperature gradient
5.5 cm
Column packing material

## Slide 13: Distillation Column
2 – 600W cryocoolers
  Balanced with 700W heaters for temperature control
Reboiler cooled by liquid from column
  Temperature controlled with 700W heater
Active PID temperature control
Active mass flow control
Pressure and temperature monitoring throughout
Multiple input RGA measures gas at three points
  Input
  Waste
  Product

## Slide 15
Chart: Pure Argon RGA Spectrum
NOTE: Uncorrected pressures
Nitrogen/Argon = 4.3×10-4

## Slide 16
Chart: Distillation product compared to pure argon
Argon peaks
Nitrogen
Nitrogen
H2O background
Other backgrounds
Other backgrounds
Input gas:
5% Ar
40% N2
55% He

## Slide 17
Chart: Nitrogen:Argon ratio in the Product gas
| 40834.4097222222 | 40835.42638888889 | 40835.67638888889 | 40836.26666666664 | 40836.44791666666
N2/Argon | 0.014431 | 0.0036998 | 0.0027391 | 0.0011743 | 0.0010026
Consumed test gas
6 days from start
8.5 days from start
Argon purity = 99.9%

## Slide 18
Chart: Nitrogen:Argon ratio in the product gas

## Slide 19: Tested gas samples
Sample #1
Our RGA measurement:
  N2 = 1000 ppm
Atlantic Analytical:
  N2 = 700 ppm
  O2 = 40 ppm
Pacific Northwest National Lab
  N2 = 920 ppm
  O2 < 10 ppm
Sample #2
Our RGA measurement:
  N2 < 500 ppm
Atlantic Analytical:
  N2 = 4100 ppm
  O2 = 810 ppm
Pacific Northwest National Lab (2 runs)
  N2 = 4250 and 4000 ppm
  O2 = 430 and 600 ppm
We believe there was air contamination

## Slide 20: Argon recovery efficiency
Consumed 24 high pressure cylinders with 262 scf of gas each (7419 liters)
  662g of Argon / cylinder
  14.9 kg of Argon total in 24 cylinders
Accumulated mass (rough estimate)
  Mass lost through product line – 50scc/m for ~10days = 1.2kg
  Mass from liquid level
    16 cm of liquid = 10.8 kg
    Total = 10.8 + 1.2 = 12 kg
  Mass from measuring flow out of reboiler during warm up
    Integral volume out of product – 5521liters = 9.3 kg
    Total = 9.3 + 1.2 = 10.5kg
Collection efficiency
  During continuous distillation = 80%
  Residual loss during cool down, tuning, etc.
  Overall 70-80%

## Slide 21: First Underground Argon purification
Processed 0.5M standard liters of gas
Reached 99.7% pure argon
Issues
  Gas flow abruptly stopped - CLOGGING
  Distillation stalled with different gas mixture – HIGH He CONTENT

## Slide 22: Solidifying impurities
Residual impurities solidified in the Column
Impurities are below the sensitivity of the VPSA RGA
Need to remove impurities before reaching the column
Contaminant | Concentration (v/v) | After 500,000 standard liter of gas |  | 
 |  | contaminants | gas vol. | Liq./solid vol.
H2O | 25 ppm | 61.2 ppm | 30.6 L | >30 mL
CO2 | 30 ppm |  |  | 
CH4 | 1.4 ppm |  |  | 
Isopentane (C5H12) | 3.0 ppm |  |  | 
N-pentane (C5H12) | 1.8 ppm |  |  | 

## Slide 23: CDF cold traps
Originally used to remove alcohol from argon/ethane mix
Repurposed to remove our residual contaminants

## Slide 24: Condenser Booster Helium Separator
Pressurize Booster with Ar-He-N2 mixture
Cool with LN2
Ar and N2 condense
Remaining pressure is He, which is then vented
Pumping on LN2 drives down temperature below 77K

## Slide 25: Argon collection efficiency
Condenser booster pressurized to 2600 psi (175 bar) = ~3500 L @ stp
Operation at 77K
  Ar vapor press. at 77K = 0.3 bar
  Ar concentration in 175 bar He at 77K = 0.17%
  Input gas = 5% argon
  Argon lost = 3.4%
Operation at 65K (subatmospheric LN2 jacket)
  Ar vapor press. @ 65K = .035bar
  Ar concentration in 175 bar He at 65K = 0.02%
  Input gas = 5% Ar
  Ar lost = 0.4%

## Slide 26: Recovering Ar in waste streams
Argon is lost in the waste streams of the Condenser Booster and the Distillation Column
Argon traps readily on charcoal at LAr temps
Pass exhaust from Condenser Booster and Distillation Column to recover argon

## Slide 27: Complete argon purification plants at Fermilab

## Slide 28: Argon purification process
Waste
Condenser Booster Helium Separator
(CB)
Input
Product
Waste
CB
Charcoal Trap
(CBCT)
Input
Product
Waste
CDF Organics Cold Traps
Input
Product
Waste
CDC
Charcoal Trap
Product
Input
Waste
Cryogenic Distillation Column (CDC)
Input
Product
Product
CDC
Charcoal Trap
Input
Waste
Product
Heated Getter
Product
Vent outside
Vent outside
pumped out
pumped out
FROM COLORADO
He 80-90%
Ar 5-7%
N2 5-15%
+ contaminants
(CO2, CH4, C4H10, C5H12, etc.)
Buffer Volume
CB Product
He – 0%
Ar – 30-40%
N2 – 60-70%
+ contaminants
(CO2, CH4, C4H10,
C5H12, etc.)
CB Waste
He >99%
Ar – trace
N2 - trace
CB-CT
He – 0%
Ar – 100%
N2 – 0%
CDF Product
He – 0%
Ar – 30-40%
N2 – 60-70%
CH4 <1%
CDC-CT
Ar – 100%
N2 – 0%
CDC-Waste
N2 - 99%
Ar – 1%
CDC Product
Ar – 100%
N2 < 0.25%
CH4 ~ 2%
CDC-CT
Ar – 100%
N2 < 0.25%
CH4 – 0%
FINAL Product
Ar – 100%
N2 < 10 ppm
CH4 – 0%
Transportation cylinder racks
Same Charcoal Trap performing both operations
Booster

## Slide 29: Conclusions and recap
Argon purification plants are complete and commissioning on going
Underground argon purification begins shortly (2 weeks)
VPSA plant has collected better than 170 kg of argon in Ar/He/N2 mix
Distillation column performed very well with ideal gas mixture
Residual contaminants and high helium concentration required addition of new plants for their removal
Unfortunately I am not available for the discussion section
  I am here for most of the workshop
  Contact info: hback@fnal.gov or +630-840-2218