## Slide 1: MQXFA18 AUP 302.2.02 and 302.2.03 – • Strand Procurement & Testing • Cable Fabrication & Testing
Lance Cooley – NHMFL/ASC (302.2.02 L3)
Vito Lombardo – FNAL (302.2.02 CAM)
Ian Pong – LBNL (302.2.03 L3 & CAM)
Mike Naus – LBNL (302.2.03 L3 Deputy & CAM Deputy)
Elizabeth Lee – LBNL, Manufacturing Engineer (now at LBNL ALS)
Jonathan Lee – LBNL Intern Student (now Grad Student at NHMFL)

## Slide 2: Cable & Coil Overview
All cables are 2nd generation QXF cables produced under AUP
Coil # | Cable #
154 | P43OL1196
160 | P43OL1203
161 | P43OL1209
243 | P43OL1191
244 | P43OL1195
246 | P43OL1199

## Slide 3: Cable QC Summary
All cables passed the required quality control testing per US-HiLumi-Doc 74
There were No Critical DRs

## Slide 4: Cable 1196 (Coil 154) DR Detail: 2 DRs

## Slide 5: QXFA-154 / P43OL1196: Wire Diameter
DR #13013 (1 of 2)
Issue: 1.5% diameter measurements ≥ 0.854 mm (≥ 1µm above USL) from one spool
Internal Spec: <1%
Spool: PO08S00694A01U
AUP Spec: 0.850 mm ± 0.003 mm
Cause: Unknown.
  Possibly incoming product issue (e.g., drawing die wear)
  Spool 03 from same billet had same issue (in Cable 1197)
Acceptance Justification
  Small number of high values should not affect cable viability

## Slide 6: QXFA-154 / P43OL1196: Cable Thickness
DR #13017 (2 of 2)
Issue: Single CME cable thickness point was OOS-Low at 275 m
Cause:
Below target average thickness, plus process & measurement variation
Acceptance Justification:
Single point, < 1 µm below LSL should not affect cable viability

## Slide 7: Cable 1203 (Coil 160) DR Detail: 2 DRs

## Slide 8: QXFA-160 / P43OL1203: Cable Thickness
DR #13062 (1 of 2)
Issue: 3 cable thickness points were OOS-High at cabling start
Cause:
Thickness is started higher than target so that it is on target in steady state. Puts thickness close to USL at start, which sometimes goes over
Acceptance Justification: Will be part of cut-off section at coiling

## Slide 9: QXFA-160 / P43OL1203: Insulation Thickness
DR #13152 (2 of 2)
Issue: LBNL insulation verification measurement 2 µm above spec
152 µm actual vs. 150 µm spec
Cause:
  Insulation at USL (149.8 µm) as measured by vendor (i.e. braided at upper end of spec window)
  Measurement variation between sites
Acceptance Justification:
  Previously accepted coils with similar insulation thickness have been coiled successfully
  When factoring cable thickness (below target) & tolerance, this thicker insulation should be acceptable

## Slide 10: Cable 1209 (Coil 161) DR Detail: 1 DR

## Slide 11: QXFA-161 / P43OL1209: Insulation Thickness
DR #13250 (1 of 1)
Issue: LBNL insulation verification measurement 0.5 µm below spec
139.5 µm actual vs. 140 µm spec
Cause:
  Braided at lower end of spec window
  Measurement differences between sites
    NEWT: 140.3 µm
Acceptance Justification:
        Not expected to cause issue at coiling

## Slide 12: Cable 1191 (Coil 243) DR Detail: 1 DR

## Slide 13: QXFA-243 / P43OL1191: Shipment Accelerometers
DR #12904 (1 of 1)
Issue: Shipping accelerometers had data integrity issues
    Accelerometer-1: Only recorded data LBNL-NEWT, not NEWT‑FNAL
  Accelerometer-1: Higher than normal tilt & vibration instances
    Accelerometer-2: No data recorded
Cause: Uncertain, but believed to be…
  Memories not cleared before shipment
  Rough handling from shipping company
Acceptance Justification:
  Low probability of quality issues with cables
  Cables will be inspected during winding
[Same issue as Coils 151 & 242 reviewed for MQXFA17]

## Slide 14: Cable 1195 (Coil 244) DR Detail: 5 DRs

## Slide 15: QXFA-244 / P43OL1195: RRR HT Temperature Range
DR #12958 (1 of 5)
Issue:
Range of TC values along sample length at 210°C plateau was >2°C
Cause:
Temperature was slightly high at one end of horizontal tube furnace
One of seven TCs caused range to go out
Acceptance Justification:
  Furnace witness wires were within historical norms
  Average temperature on target (209.9°C)
  210°C is least impactful plateau for RRR

## Slide 16: QXFA-244 / P43OL1195: Braiding Data Logger
DR #12999 (2 of 5)
Issue: Automated data logger at braiding vendor only recorded first 34 m of data.
Cause: Improper data logger set-up by braiding operator
Acceptance Justification:
  Vision system operational for full length, catching “one faint oil spot”
  Rest of log retroactively filled-in based on notes from operator
  After this, interlock implemented preventing braiding operation without data logger being on

## Slide 17: QXFA-244 / P43OL1195: Insulation Thickness
DR #13000 (3 of 5)
Issue: Insulation thickness verification 1 µm above specification (151 µm)
Cause: Vendor’s measurement was lower and in spec (148 µm)
Acceptance Justification:
  Previously accepted coils with similar insulation thickness have been coiled successfully
  When factoring cable thickness tolerance, this thicker insulation should be acceptable

## Slide 18: QXFA-244 / P43OL1195: Initial Cable Thickness
DR #13015 (4 of 5)
Issue: 3 cable thickness points were OOS-High at cabling start
Cause:
Thickness is started higher than target so that it is on target in steady state. Puts thickness close to USL at start, which sometimes goes over
Acceptance Justification: Will be part of cut-off section at coiling

## Slide 19: QXFA-244 / P43OL1195: Core Detector
DR #13016 (5 of 5)
Issue: Core detector inoperable during cable manufacturing
Cause: Dead battery. No time to charge or change before run
Acceptance Justification:
  Core spool weighed before and after run to ensure proper amount was incorporated into cable
  Core sporadically monitored during run to ensure it was being incorporated into cable

## Slide 20: Cable 1199 (Coil 246) DR Detail: 2 DRs

## Slide 21: QXFA-246 / P43OL1199: Shipment Accelerometers
DR #13077 (1 of 2)
Issue: Insulation thickness verification 1 µm above spec (151 µm)
Cause: Unknown. Possible measurement differences between sites
    Measurement in spec at vendor (147 µm)
Acceptance Justification:
  Previously accepted coils with similar insulation thickness have been coiled successfully
  When factoring cable thickness & tolerance, this thicker insulation should be acceptable

## Slide 22: QXFA-246 / P43OL1199: Ic Measurement
DR #13088 (2 of 2)
Issue: One of three strands was unable to be measured, requiring measurement of back-up strand
Cause: Believed to be sample handling damage, per FNAL
Acceptance Justification:
  Backup sample successfully measured with passing results

## Slide 23: END [Back-Up Slides Below]

## Slide 24: Strand Summary
All strands ordered per the “HiLumi” specification under the AUP program, per the following POs:
  FNAL PO 655175 Shipment B
  FNAL PO 667037 Shipments D, E, and F
  FNAL PO 683525 Shipment A
  CERN Exchange
Conductor Description:
  Ø0.85 mm, 108/127 stack, Ti-doped, Reduced-Sn core

## Slide 25
Both 665°C/75h
S: 665°C/50h
V: 665°/75h
Both 665°C/50h
Strand Production Data – Ic, 15T
Yellow bands indicate strand data for these cables

## Slide 26
Both 665°C/75h
S: 665°C/50h
V: 665°/75h
Both 665°C/50h
Strand Production Data – Ic, 12T
Yellow bands indicate strand data for these cables

## Slide 27: Strand Production Data - RRR
Data for 15% rolled strand predicts the RRR at cable sharp bend
Lab: IEC method, Supplier: 20K method
Inter-lab comparisons have validated approaches (see QP)
Yellow bands indicate strand data for these cables

## Slide 28: QXFA-243 / P43OL1191

## Slide 29: P43OL1191 – Cable Date, Lengths
Cable Manufacture Date
  12 Apr 2022 (Production run)
Cable Length:
  467 m (LBNL, fabricated, including LBNL samples)

## Slide 30: P43OL1191 – Strand and SS Core ID
Spool: 40 spools from 35 different billets.
  Each spool provided one unit length.
Core:
  120L42A7400804
    Heat: 850858. Lot: 17-521
    Material: 316L
    Chemical Properties CoT/CoC #172660-1: 0.16 wt% Co
    Core width: 12.0 mm
AO08S00092A02U | AO08S00253A01U | AO08S00299A05U | AO08S00384A01U
AO08S00169A02U | AO08S00254A03U | AO08S00301A03U | AO08S00391A03U
AO08S00169A03U | AO08S00256A01U | AO08S00304A02U | AO08S00391A07U
AO08S00226A02U | AO08S00271A04U | AO08S00308A02U | AO08S00392A04U
AO08S00241A04U | AO08S00272A02U | AO08S00309A02U | AO08S00403A04U
AO08S00246A02U | AO08S00282A04U | AO08S00311A03U | AO08S00405A01U
AO08S00246A06U | AO08S00284A03U | AO08S00316A02U | AO08S00437A02U
AO08S00248A05U | AO08S00292A03U | AO08S00321A01U | AO08S00468A02U
AO08S00249A05U | AO08S00297A02U | AO08S00321A03U | AO08S00468A04U
AO08S00250A02U | AO08S00298A03U | AO08S00342A05U | AO08S00570A04U

## Slide 31: P43OL1191 Respooling Wire Diameter
Below LSL: 0.025%
Above USL: 0.175%

## Slide 32: P43OL1191 – Cable QC Data Summary
CME:
Residual Twist: 135°
10-stack:
  Qualification: 1.535 mm
  Production tail end: 1.526 mm
 | Pressure (MPa) | Angle (°) | Width (mm) | Thickness (mm)
Maximum | 17.0 | 0.392 | 18.165 | 1.532
Average | 16.8 | 0.350 | 18.145 | 1.524
Minimum | 16.7 | 0.322 | 18.141 | 1.517
Sigma | 0.04 | 0.009 | 0.002 | 0.002

## Slide 33
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 34
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 35
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 36: P43OL1191 – Braiding
Fiberglass Lot: #RCV0011562
P/I: 18.9
Spool tension: 10 lbs. @ payoff. 20 lbs. @ takeup (12 lbs min)
Bobbin payoff tension: 0.125 lbs. ≤ T ≤ 0.250 lbs.
Site | Cycle #1 (mm) | Cycle #2 (mm) | Cycle #3 (mm) | Average (mm)
NEWT | 0.151 | 0.149 | 0.148 | 0.149
LBNL Verification | 0.148 | 0.146 | 0.144 | 0.146
Insulation Thickness (at 5 MPa)

## Slide 37: P43OL1191 – Wire Parameters
Properties | Inspected Average
Wire Diameter | 0.8504 ± 0.001 mm (LBNL)1
Cu ratio a | 54.11% (BOST)
Strand twist pitch a | 18.6 mm (BOST)
RRR (RW) a | 313 (BOST)
RRR (15% rolled) a | 216 (BOST)
IC (4.2 K, 15 T) a | 380 A (BOST)
IC (4.2 K, 14 T) a | 474 A (BOST)
IC (4.2 K, 13 T) a | 583 A (BOST)
IC (4.2 K, 12 T) a | 705 A (BOST)
a First billet averaged, then weighted average according to the spool distribution in the cable
1 As-received. LBNL respooling data. Mean ± 1 sigma

## Slide 38: P43OL1191 – Wire Parameters Supplier (S) and Verification (V) IC Data
Due to the fact that the source wire came from exchange with CERN, verification data are not available.

## Slide 39: P43OL1191 – Wire Parameters Supplier (S) and Verification (V) RRR Data
Due to the fact that the source wire came from exchange with CERN, verification data are not available.

## Slide 40: P43OL1191 – Extracted Strand RRR
Cable ID | No. of Units from Billet (spool) | Heat Treat/ Sample ID | Major Edge RRR | Minor Edge RRR | Straight 1 RRR | Straight 2 RRR
AO08S00392A04U P43OL1191AE03E | 1 (1) | LRLK220420ALC1 | 283 | 306 | 371 | 401
AO08S00308A02U P43OL1191AE06E | 1 (1) | LRLK220420ALC1 | 327 | 334 | 386 | 408
AO08S00246A02U P43OL1191AE09E | 2 (1) | LRLK220420ALC1 | 319 | 306 | 376 | 400
AO08S00169A03U P43OL1191AE11E | 2 (1) | LRLK220420ALC1 | 263 | 244 | 328 | 353
AO08S00321A03U P43OL1191AE24E | 2 (1) | LRLK220420ALC1 | 353 | 338 | 389 | 409

## Slide 41: P43OL1191 – Ic, Cable Qual Samples
Wire/ Cable Strand | Ic(A) at Field (T) |  |  | 
 | 12 T | 13 T | 14 T | 15 T
AO08S00246A02U P43OL1191AE09E | 667 | 552 | 448 | 357
AO08S00169A02U P43OL1191AE11E | 674 | 554 | 451 | 359
AO08S00321A03U P43OL1191AE24E | 666 | 555 | 454 | 365

## Slide 42: P43OL1191 – SSL Plot, Cable Qual Samples

## Slide 43: P43OL1191 – SSL Margins, Qual Samples
Strand from which Margin is Calculated: | Strand # 24E @ 1.9 K
Margins | Margin | Operating Point (X)
Load Line Margin (Purple Arrow) | 26.2% | 73.8%
Current Margin (Green Arrow) | 61.2% | 38.8%
Temperature Margin (K) | 5.3 | 7.2
Limits | Strand | Strand x 40
Selected Strand’s Current (A) at Margin-Calculation Field | 1045 | 41819
Selected Strand’s Current (A) at 100% SSL | 550 | 22001
Selected Strand’s Field (T) at 100% SSL | 15.0 | 

## Slide 44: QXFA-244 / P43OL1195

## Slide 45: P43OL1195 – Cable Date, Lengths
Cable Manufacture Date
  07 July 2022 (Production run)
Cable Length:
  469 m (LBNL, fabricated, including LBNL samples)

## Slide 46: P43OL1195 – Strand and SS Core ID
Spool:
  PO08S00685A03U x 13 ULs
  PO08S00686A02U x 5 ULs
  PO08S00687A01U x 18 ULs
  PO08S00688A03U x 4 ULs
Core:
  120L46A7400804
    Heat: 850858. Lot: 17-521
    Material: 316L
    Chemical Properties CoT/CoC #187781-1: 0.16 wt% Co
    Core width: 12.0 mm
From 4 billets

## Slide 47: P43OL1195 Respooling Wire Diameter
Below LSL: 0.000%
Above USL: 0.021%

## Slide 48: P43OL1195 – Cable QC Data Summary
CME:
Residual Twist: 130°
10-stack:
  Qualification: 1.538 mm
  Production tail end: 1.529 mm
 | Pressure (MPa) | Angle (°) | Width (mm) | Thickness (mm)
Maximum | 17.1 | 0.393 | 18.154 | 1.536
Average | 16.9 | 0.365 | 18.139 | 1.526
Minimum | 16.6 | 0.327 | 18.133 | 1.522
Sigma | 0.03 | 0.012 | 0.003 | 0.002

## Slide 49
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 50
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 51
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 52: P43OL1195 – Braiding
Fiberglass Lot: #RCV00011562
P/I: 18.9
Spool tension: 10 lbs. @ payoff. 20 lbs. @ takeup (12 lbs min)
Bobbin payoff tension: 0.125 lbs. ≤ T ≤ 0.250 lbs.
Site | Cycle #1 (mm) | Cycle #2 (mm) | Cycle #3 (mm) | Average (mm)
NEWT | 0.149 | 0.148 | 0.147 | 0.148
LBNL Verification | 0.154 | 0.151 | 0.150 | 0.151
Insulation Thickness (at 5 MPa)

## Slide 53: P43OL1195 – Wire Parameters
Properties | Inspected Average
Wire Diameter | 0.8509 ± 0.001 mm (LBNL)1
Cu ratio a | 53.97% (BOST)
Strand twist pitch a | 19.4mm (BOST)
RRR (RW) a | 296 (BOST)
RRR (15% rolled) a | 229 (BOST)
IC (4.2 K, 15 T) a | 374 A (BOST)
IC (4.2 K, 14 T) a | 468 A (BOST)
IC (4.2 K, 13 T) a | 576 A (BOST)
IC (4.2 K, 12 T) a | 697 A (BOST)
a First billet averaged, then weighted average according to the spool distribution in the cable
1 As-received. LBNL respooling data. Mean ± 1 sigma

## Slide 54: P43OL1195 – Wire Parameters Supplier (S) and Verification (V) IC Data
Number of spools from that billet used in the cable

## Slide 55: P43OL1195 – Wire Parameters Supplier (S) and Verification (V) RRR Data
Number of spools from that billet used in the cable

## Slide 56: P43OL1195 – Extracted Strand RRR
Cable ID | No. of Units from Billet (spool) | Heat Treat/ Sample ID | Major Edge RRR | Minor Edge RRR | Straight 1 RRR | Straight 2 RRR
PO08S00685A03U P43OL1195AE03E | 13 (13) | LRLK220804ALC1 | 326 | 273 | 348 | 349
PO08S00685A03U P43OL1195AE06E | 13 (13) | LRLK220804ALC1 | 336 | 264 | 349 | 355
PO08S00686A02U P43OL1195AE21E | 5 (5) | LRLK220804ALC1 | 272 | 240 | 311 | 298
PO08S00687A01U P43OL1195AE29E | 18 (18) | LRLK220804ALC1 | 282 | 231 | 307 | 318
PO08S00687A01U P43OL1195AE30E | 18 (18) | LRLK220804ALC1 | 326 | 253 | 330 | 343

## Slide 57: P43OL1195 – Ic, Cable Qual Samples
Wire/ Cable Strand | Ic(A) at Field (T) |  |  | 
 | 12 T | 13 T | 14 T | 15 T
PO08S00687A01U P43OL1195AE29E | 671 | 553 | 451 | 359
PO08S00685A03U P43OL1195AE01E | 666 | 552 | 449 | 359
PO08S00686A02U P43OL1195AE21E | 676 | 560 | 458 | 367

## Slide 58: P43OL1195 – SSL Plot, Cable Qual Samples

## Slide 59: P43OL1195 – SSL Margins, Qual Samples
Strand from which Margin is Calculated: | Strand # 01E @ 1.9 K
Margins | Margin | Operating Point (X)
Load Line Margin (Purple Arrow) | 26.1% | 73.9%
Current Margin (Green Arrow) | 61.6% | 38.4%
Temperature Margin (K) | 5.3 | 7.2
Limits | Strand | Strand x 40
Selected Strand’s Current (A) at Margin-Calculation Field | 1056 | 42221
Selected Strand’s Current (A) at 100% SSL | 549 | 21964
Selected Strand’s Field (T) at 100% SSL | 15.0 | 

## Slide 60: QXFA-154 / P43OL1196

## Slide 61: P43OL1196 – Cable Date, Lengths
Cable Manufacture Date
  11 Aug 2022 (Production run)
Cable Length:
  470 m (LBNL, fabricated, including LBNL samples)

## Slide 62: P43OL1196 – Strand and SS Core ID
Spool:
Core:
  120L47A7400804
    Heat: 850858 Lot: 17-521
    Material: 316L
    Chemical Properties CoT/CoC #187781-1: 0.16 wt% Co
    Core width: 12.0 mm
From 15 billets
PO08S00596A01U x 1 ULs | PO08S00631A07U x 3 ULs
PO08S00598A02U x 1 ULs | PO08S00632A01U x 1 ULs
PO08S00602A03U x 1 ULs | PO08S00632A02U x 1 ULs
PO08S00621A05U x 1 ULs | PO08S00636A02U x 1 ULs
PO08S00622A01U x 1 ULs | PO08S00638A05U x 1 ULs
PO08S00622A03U x 1 ULs | PO08S00685A01U x 2 ULs
PO08S00625A01U x 1 ULs | PO08S00685A02U x 2 ULs
PO08S00625A03U x 1 ULs | PO08S00689A01U x 6 ULs
PO08S00630A03U x 1 ULs | PO08S00689A02U x 1 ULs
PO08S00631A01U x 1 ULs | PO08S00689A05U x 2 ULs
PO08S00631A02U x 3 ULs | PO08S00690A02U x 2 ULs
PO08S00631A03U x 1 ULs | PO08S00694A01U x 1 ULs
PO08S00631A06U x 3 ULs | 

## Slide 63: P43OL1196 Respooling Wire Diameter
Below LSL: 0.000%
Above USL: 0.075%

## Slide 64: P43OL1196 – Cable QC Data Summary
CME:
Residual Twist: 145°
10-stack:
  Qualification: 1.534 mm
  Production tail end: 1.527 mm
 | Pressure (MPa) | Angle (°) | Width (mm) | Thickness (mm)
Maximum | 17.0 | 0.394 | 18.142 | 1.531
Average | 16.9 | 0.368 | 18.131 | 1.519
Minimum | 16.8 | 0.343 | 18.126 | 1.514
Sigma | 0.02 | 0.009 | 0.002 | 0.002

## Slide 65
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 66
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 67
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 68: P43OL1196 – Braiding
Fiberglass Lot: #RCV00011562
P/I: 18.9
Spool tension: 10 lbs. @ payoff. 20 lbs. @ takeup (12 lbs min)
Bobbin payoff tension: 0.125 lbs. ≤ T ≤ 0.250 lbs.
Site | Cycle #1 (mm) | Cycle #2 (mm) | Cycle #3 (mm) | Average (mm)
NEWT | 0.149 | 0.147 | 0.146 | 0.147
LBNL Verification | 0.149 | 0.146 | 0.146 | 0.147
Insulation Thickness (at 5 MPa)

## Slide 69: P43OL1196 – Wire Parameters
Properties | Inspected Average
Wire Diameter | 0.8510 ± 0.001 mm (LBNL)1
Cu ratio a | 54.27% (BOST)
Strand twist pitch a | 19.4mm (BOST)
RRR (RW) a | 288 (BOST)
RRR (15% rolled) a | 203 (BOST)
IC (4.2 K, 15 T) a | 375 A (BOST)
IC (4.2 K, 14 T) a | 469 A (BOST)
IC (4.2 K, 13 T) a | 575 A (BOST)
IC (4.2 K, 12 T) a | 697 A (BOST)
a First billet averaged, then weighted average according to the spool distribution in the cable
1 As-received. LBNL respooling data. Mean ± 1 sigma

## Slide 70: P43OL1196 – Wire Parameters Supplier (S) and Verification (V) IC Data
Number of spools from that billet used in the cable
Verification samples only sent to CERN, so Verification data is not available for several billets

## Slide 71: P43OL1196 – Wire Parameters Supplier (S) and Verification (V) RRR Data
Number of spools from that billet used in the cable
Verification samples only sent to CERN, so Verification data is not available for several billets

## Slide 72: P43OL1196 – Extracted Strand RRR
Cable ID | No. of Units from Billet (spool) | Heat Treat/ Sample ID | Major Edge RRR | Minor Edge RRR | Straight 1 RRR | Straight 2 RRR
PO08S00689A01U P43OL1196AE03E | 9 (6) | LRLK220825ALC1 | 332 | 275 | 338 | 337
PO08S00685A02U P43OL1196AE11E | 4 (2) | LRLK220825ALC1 | 259 | 218 | 286 | 279
PO08S00631A02U P43OL1196AE19E | 11 (3) | LRLK220825ALC1 | 303 | 275 | 353 | 360
PO08S00631A06U P43OL1196AE30E | 11 (3) | LRLK220825ALC1 | 303 | 271 | 335 | 344
PO08S00631A07U P43OL1196AE48E | 11 (3) | LRLK220825ALC1 | 304 | 270 | 339 | 350

## Slide 73: P43OL1196 – Ic, Cable Qual Samples
Wire/ Cable Strand | Ic(A) at Field (T) |  |  | 
 | 12 T | 13 T | 14 T | 15 T
PO08S00689A01U P43OL1196AE01E | 662 | 549 | 448 | 362
PO08S00631A02U P43OL1196AE19E | 690 | 575 | 470 | 378
PO08S00631A06U P43OL1196AE30E | 669 | 565 | 460 | 361

## Slide 74: P43OL1196 – SSL Plot, Cable Qual Samples

## Slide 75: P43OL1196 – SSL Margins, Qual Samples
Strand from which Margin is Calculated: | Strand # 01E @ 1.9 K
Margins | Margin | Operating Point (X)
Load Line Margin (Purple Arrow) | 26.0% | 74.0%
Current Margin (Green Arrow) | 60.9% | 39.1%
Temperature Margin (K) | 5.3 | 7.2
Limits | Strand | Strand x 40
Selected Strand’s Current (A) at Margin-Calculation Field | 1039 | 41544
Selected Strand’s Current (A) at 100% SSL | 549 | 21942
Selected Strand’s Field (T) at 100% SSL | 14.9 | 

## Slide 76: QXFA-246 / P43OL1199

## Slide 77: P43OL1199 – Cable Date, Lengths
Cable Manufacture Date
  10 Nov 2022 (Production run)
Cable Length:
  471 m (LBNL, fabricated, including LBNL samples)

## Slide 78: P43OL1199 – Strand and SS Core ID
Spool:
  PO08S00538A01U x 2 ULs
  PO08S00538A02U x 8 ULs
  PO08S00538A03U x 3 ULs
  PO08S00538A04U x 3 ULs
  PO08S00690A01U x 11 ULs
  PO08S00690A03U x 4 ULs
  PO08S00692A01U x 7 ULs
  PO08S00695A01U x 2 ULs
Core:
  120L50A7400804
    Heat: 850858 Lot: 17-521
    Material: 316L
    Chemical Properties CoT/CoC #187781-1: 0.16 wt% Co
    Core width: 12.0 mm
From 4 billets

## Slide 79: P43OL1199 Respooling Wire Diameter
Below LSL: 0.005%
Above USL: 0.105%

## Slide 80: P43OL1199 – Cable QC Data Summary
CME:
Residual Twist: 145°
10-stack:
  Qualification: 1.532 mm
  Production tail end: 1.527 mm
 | Pressure (MPa) | Angle (°) | Width (mm) | Thickness (mm)
Maximum | 17.1 | 0.406 | 18.159 | 1.531
Average | 17.0 | 0.386 | 18.134 | 1.521
Minimum | 16.9 | 0.349 | 18.129 | 1.517
Sigma | 0.03 | 0.008 | 0.003 | 0.002

## Slide 81
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 82
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 83
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 84: P43OL1199 – Braiding
Site | Cycle #1 (mm) | Cycle #2 (mm) | Cycle #3 (mm) | Average (mm)
NEWT | 0.151 | 0.148 | 0.147 | 0.149
LBNL Verification | 0.153 | 0.151 | 0.150 | 0.151
Insulation Thickness (at 5 MPa)
Fiberglass Lot: #RCV00011562
P/I: 18.9
Spool tension: 10 lbs. @ payoff. 20 lbs. @ takeup (12 lbs min)
Bobbin payoff tension: 0.125 lbs. ≤ T ≤ 0.250 lbs.

## Slide 85: P43OL1199 – Wire Parameters
Properties | Inspected Average
Wire Diameter | 0.8509 ± 0.001 mm (LBNL)1
Cu ratio a | 53.86% (BOST)
Strand twist pitch a | 19.4mm (BOST)
RRR (RW) a | 275 (BOST)
RRR (15% rolled) a | 188 (BOST)
IC (4.2 K, 15 T) a | 392 A (BOST)
IC (4.2 K, 14 T) a | 487 A (BOST)
IC (4.2 K, 13 T) a | 596 A (BOST)
IC (4.2 K, 12 T) a | 719 A (BOST)
a First billet averaged, then weighted average according to the spool distribution in the cable
1 As-received. LBNL respooling data. Mean ± 1 sigma

## Slide 86: P43OL1199 – Wire Parameters Supplier (S) and Verification (V) IC Data
Number of spools from that billet used in the cable

## Slide 87: P43OL1199 – Wire Parameters Supplier (S) and Verification (V) RRR Data
Number of spools from that billet used in the cable

## Slide 88: P43OL1199 – Extracted Strand RRR
Cable ID | No. of Units from Billet (spool) | Heat Treat/ Sample ID | Major Edge RRR | Minor Edge RRR | Straight 1 RRR | Straight 2 RRR
PO08S00690A01U P43OL1199AE03E | 15 (11) | LRLK221212ALC1 | 342 | 283 | 363 | 363
PO08S00538A02U P43OL1199AE07E | 16 (8) | LRLK221212ALC1 | 244 | 212 | 298 | 300
PO08S00538A03U P43OL1199AE31E | 16 (3) | LRLK221212ALC1 | 323 | 262 | 348 | 352
PO08S00692A01U P43OL1199AE36E | 7 (7) | LRLK221212ALC1 | 266 | 210 | 291 | 310
PO08S00690A03U P43OL1199AE55E | 15 (4) | LRLK221212ALC1 | 303 | 246 | 323 | 328

## Slide 89: P43OL1199 – Ic, Cable Qual Samples
Wire/ Cable Strand | Ic(A) at Field (T) |  |  | 
 | 12 T | 13 T | 14 T | 15 T
PO08S00538A02U P43OL1199AE07E | 731 | 612 | 503 | 409
PO08S00692A01U P43OL1199AE36E | 679 | 565 | 463 | 375
PO08S00538A03U P43OL1199AE31E | 734 | 610 | 501 | 404

## Slide 90: P43OL1199 – SSL Plot, Cable Qual Samples

## Slide 91: P43OL1199 – SSL Margins, Qual Samples
Strand from which Margin is Calculated: | Strand # 36E @ 1.9 K
Margins | Margin | Operating Point (X)
Load Line Margin (Purple Arrow) | 26.7% | 73.3%
Current Margin (Green Arrow) | 61.8% | 38.2%
Temperature Margin (K) | 5.4 | 7.3
Limits | Strand | Strand x 40
Selected Strand’s Current (A) at Margin-Calculation Field | 1062 | 42495
Selected Strand’s Current (A) at 100% SSL | 553 | 22136
Selected Strand’s Field (T) at 100% SSL | 15.1 | 

## Slide 92: QXFA-260 / P43OL1203

## Slide 93: P43OL1203 – Cable Date, Lengths
Cable Manufacture Date
  12 Dec 2022 (Production run)
Cable Length:
  469 m (LBNL, fabricated, including LBNL samples)

## Slide 94: P43OL1203 – Strand and SS Core ID
Spool:
  PO08S00078A04U x 1 ULs
  PO08S00697A01U x 1 ULs
  PO08S00700A01U x 7 ULs
  PO08S00701A01U x 8 ULs
  PO08S00705A03U x 7 ULs
  PO08S00706A03U x 4 ULs
  PO08S00710A04U x 11 ULs
  PO08S00712A03U x 2 ULs
Core:
  120L54A7400804
    Heat: 850858 Lot: 17-521
    Material: 316L
    Chemical Properties CoT/CoC #187781-1: 0.16 wt% Co
    Core width: 12.0 mm
From 8 billets

## Slide 95: P43OL1203 Respooling Wire Diameter
Below LSL: 0.002%
Above USL: 0.103%

## Slide 96: P43OL1203 – Cable QC Data Summary
CME:
Residual Twist: 135°
10-stack:
  Qualification: 1.539 mm
  Production tail end: 1.528 mm
 | Pressure (MPa) | Angle (°) | Width (mm) | Thickness (mm)
Maximum | 16.9 | 0.413 | 18.165 | 1.537
Average | 16.9 | 0.379 | 18.135 | 1.523
Minimum | 16.8 | 0.345 | 18.128 | 1.518
Sigma | 0.01 | 0.012 | 0.006 | 0.004

## Slide 97
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 98
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 99
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 100: P43OL1203 – Braiding
Site | Cycle #1 (mm) | Cycle #2 (mm) | Cycle #3 (mm) | Average (mm)
NEWT | 0.152 | 0.149 | 0.148 | 0.150
LBNL Verification | 0.154 | 0.151 | 0.150 | 0.152
Insulation Thickness (at 5 MPa)
Fiberglass Lot: #RCV00011562
P/I: 18.9
Spool tension: 10 lbs. @ payoff. 20 lbs. @ takeup (12 lbs min)
Bobbin payoff tension: 0.125 lbs. ≤ T ≤ 0.250 lbs.

## Slide 101: P43OL1203 – Wire Parameters
Properties | Inspected Average
Wire Diameter | 0.8509 ± 0.001 mm (LBNL)1
Cu ratio a | 54.33% (BOST)
Strand twist pitch a | 20.0 mm (BOST)
RRR (RW) a | 315 (BOST)
RRR (15% rolled) a | 217 (BOST)
IC (4.2 K, 15 T) a | 368 A (BOST)
IC (4.2 K, 14 T) a | 458 A (BOST)
IC (4.2 K, 13 T) a | 563 A (BOST)
IC (4.2 K, 12 T) a | 680 A (BOST)
a First billet averaged, then weighted average according to the spool distribution in the cable
1 As-received. LBNL respooling data. Mean ± 1 sigma

## Slide 102: P43OL1203 – Wire Parameters Supplier (S) and Verification (V) IC Data
Number of spools from that billet used in the cable

## Slide 103: P43OL1203 – Wire Parameters Supplier (S) and Verification (V) RRR Data
Number of spools from that billet used in the cable

## Slide 104: P43OL1203 – Extracted Strand RRR
Cable ID | No. of Units from Billet (spool) | Heat Treat/ Sample ID | Major Edge RRR | Minor Edge RRR | Straight 1 RRR | Straight 2 RRR
PO08S00710A04U P43OL1203AE05E | 11 (11) | LRLK230109ALC1 | 294 | 262 | 325 | 324
PO08S00706A03U P43OL1203AE18E | 4 (4) | LRLK230109ALC1 | 299 | 252 | 330 | 333
PO08S00705A03U P43OL1203AE24E | 7 (7) | LRLK230109ALC1 | 287 | 228 | 312 | 309
PO08S00700A01U P43OL1203AE35E | 7 (7) | LRLK230109ALC1 | 297 | 269 | 333 | 348
PO08S00701A01U P43OL1203AE45E | 8 (8) | LRLK230109ALC1 | 329 | 303 | 359 | 365

## Slide 105: P43OL1203 – Ic, Cable Qual Samples
Wire/ Cable Strand | Ic(A) at Field (T) |  |  | 
 | 12 T | 13 T | 14 T | 15 T
PO08S00710A04U P43OL1203AE01E | 642 | 526 | 430 | 340
PO08S00701A01U P43OL1203AE45E | 659 | 544 | 448 | 362
PO08S00705A03U P43OL1203AE24E | 651 | 541 | 437 | 349

## Slide 106: P43OL1203 – SSL Plot, Cable Qual Samples

## Slide 107: P43OL1203 – SSL Margins, Qual Samples
Strand from which Margin is Calculated: | Strand # 01E @ 1.9 K
Margins | Margin | Operating Point (X)
Load Line Margin (Purple Arrow) | 25.2% | 74.8%
Current Margin (Green Arrow) | 60.2% | 39.8%
Temperature Margin (K) | 5.1 | 7.0
Limits | Strand | Strand x 40
Selected Strand’s Current (A) at Margin-Calculation Field | 1018 | 40731
Selected Strand’s Current (A) at 100% SSL | 542 | 21688
Selected Strand’s Field (T) at 100% SSL | 14.8 | 

## Slide 108: QXFA-161 / P43OL1209

## Slide 109: P43OL1209 – Cable Date, Lengths
Cable Manufacture Date
  02 Mar 2023 (Production run)
Cable Length:
  469 m (LBNL, fabricated, including LBNL samples)

## Slide 110: P43OL1209 – Strand and SS Core ID
Spool:
  PO08S00665A01U x 19 ULs
  PO08S00667A02U x 3 ULs
  PO08S00667A04U x 2 ULs
  PO08S00696A02U x 16 ULs
Core:
  120L60A7400804
    Heat: 850858 Lot: 17-521
    Material: 316L
    Chemical Properties CoT/CoC #187781-1: 0.16 wt% Co
    Core width: 12.0 mm
From 3 billets

## Slide 111: P43OL1209 Respooling Wire Diameter
Below LSL: 0.000%
Above USL: 0.013%

## Slide 112: P43OL1209 – Cable QC Data Summary
CME:
Residual Twist: 140°
10-stack:
  Qualification: 1.533 mm
  Production tail end: 1.525 mm
 | Pressure (MPa) | Angle (°) | Width (mm) | Thickness (mm)
Maximum | 17.1 | 0.427 | 18.148 | 1.531
Average | 17.0 | 0.388 | 18.140 | 1.522
Minimum | 16.7 | 0.358 | 18.134 | 1.518
Sigma | 0.03 | 0.013 | 0.003 | 0.002

## Slide 113
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 114
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 115
Rollers: P-93 (2021-08-09) & P-94 (2021-08-09)

## Slide 116: P43OL1209 – Braiding
Site | Cycle #1 (mm) | Cycle #2 (mm) | Cycle #3 (mm) | Average (mm)
NEWT | 0.142 | 0.140 | 0.139 | 0.140
LBNL Verification | 0.142 | 0.139 | 0.138 | 0.140
Insulation Thickness (at 5 MPa)
Fiberglass Lot: #RCV00011562
P/I: 18.9
Spool tension: 10 lbs. @ payoff. 20 lbs. @ takeup (12 lbs min)
Bobbin payoff tension: 0.125 lbs. ≤ T ≤ 0.250 lbs.

## Slide 117: P43OL1209 – Wire Parameters
Properties | Inspected Average
Wire Diameter | 0.8507 ± 0.001 mm (LBNL)1
Cu ratio a | 53.74% (BOST)
Strand twist pitch a | 18.9 mm (BOST)
RRR (RW) a | 293 (BOST)
RRR (15% rolled) a | 186 (BOST)
IC (4.2 K, 15 T) a | 379 A (BOST)
IC (4.2 K, 14 T) a | 473 A (BOST)
IC (4.2 K, 13 T) a | 579 A (BOST)
IC (4.2 K, 12 T) a | 700 A (BOST)
a First billet averaged, then weighted average according to the spool distribution in the cable
1 As-received. LBNL respooling data. Mean ± 1 sigma

## Slide 118: P43OL1209 – Wire Parameters Supplier (S) and Verification (V) IC Data
Number of spools from that billet used in the cable

## Slide 119: P43OL1209 – Wire Parameters Supplier (S) and Verification (V) RRR Data
Number of spools from that billet used in the cable

## Slide 120: P43OL1209 – Extracted Strand RRR
Cable ID | No. of Units from Billet (spool) | Heat Treat/ Sample ID | Major Edge RRR | Minor Edge RRR | Straight 1 RRR | Straight 2 RRR
PO08S00667A02U P43OL1209AE05E | #N/A | LRLK230411ALC1 | 296 | 257 | 335 | 339
PO08S00696A02U P43OL1209AE09E | #N/A | LRLK230411ALC1 | 316 | 282 | 344 | 347
PO08S00696A02U P43OL1209AE11E | #N/A | LRLK230411ALC1 | 337 | 291 | 357 | 361
PO08S00665A01U P43OL1209AE33E | #N/A | LRLK230411ALC1 | 274 | 235 | 282 | 295
PO08S00665A01U P43OL1209AE35E | #N/A | LRLK230411ALC1 | 286 | 266 | 324 | 333

## Slide 121: P43OL1209 – Ic, Cable Qual Samples
Wire/ Cable Strand | Ic(A) at Field (T) |  |  | 
 | 12 T | 13 T | 14 T | 15 T
PO08S00665A01U P43OL1209AE33E | 679 | 562 | 459 | 370
PO08S00696A02U P43OL1209AE09E | 664 | 552 | 457 | 366
PO08S00667A02U P43OL1209AE05E | 653 | 539 | 439 | 351

## Slide 122: P43OL1209 – SSL Plot, Cable Qual Samples

## Slide 123: P43OL1209 – SSL Margins, Qual Samples
Strand from which Margin is Calculated: | Strand # 05E @ 1.9 K
Margins | Margin | Operating Point (X)
Load Line Margin (Purple Arrow) | 25.6% | 74.4%
Current Margin (Green Arrow) | 60.7% | 39.3%
Temperature Margin (K) | 5.2 | 7.1
Limits | Strand | Strand x 40
Selected Strand’s Current (A) at Margin-Calculation Field | 1031 | 41254
Selected Strand’s Current (A) at 100% SSL | 546 | 21826
Selected Strand’s Field (T) at 100% SSL | 14.9 |