## Slide 1: Tapered Key Load Test Using MQXFA12b
G. Vallone, G. Ambrosio, D. Cheng, P. Ferracin, L. Garcia Fajardo, J. Herrera
May 23, 2024
MQXF Structural Working Group Meeting

## Slide 2: Introduction
An investigation started after MQXFA07 test discovered that localized strain spikes at the inner layer wedge/end-spacer interface can cause filament failures
  The analysis suggested that this was due to the low azimuthal prestress experienced by the failed coil (closed pole key ‘gaps’)
  More details here: G. Ambrosio et al., 10.1109/TASC.2023.3261842
Similar damages were found in MQXFA13 coils
  This time, the azimuthal prestress reduction was only local, and due to the small coil ends
This suggests that we should avoid using coils with ‘small’ ends
  Here we explore a potential shimming strategy to avoid wasting these coils

## Slide 3: Modeling - Summary
MQXFS octant model
  Contact offset on the coil/filler contact
  All coil components bonded but:
    Separation allowed between the wedge and the spacer
    and the coil and the winding pole
  Model shows strain spikes at the wedge/end-spacer interface under certain conditions…

## Slide 4: Why the strain increases?
Pole stress at cold computed on the same z location of the wedge/end-spacer transition
  Blue/magenta lines represent end-region modifications
  All the points are on the same lines!
The effect seems to be controlled by a local prestress loss

## Slide 5: Local Prestress Modifiers - Results
Increasing the ‘global’ prestress might ‘push’ the coil stress over the project-defined limits
Alternatively, we could act on ‘local’ modifiers. Two strategies were explored:
  Radial shimming of the coil pack
    Available shimming region relatively small, as we do not want steps close to the cable
    Goes in the wrong direction - LQ effect, decreases the prestress locally
  Increasing the key size in the coil end region
    Key size increased (100 µm) along the whole ‘short’ shell
    Can remove completely the effect of the undersized coil ends (considering the A13 case)
Coil/Collar Shimming
Key Shimming

## Slide 6: Load Key Configuration - Proposal
The key solution works, but introduces a sharp transition in the key size
We can create a ‘tapered’ key using 2 mils shim
  Assuming an additional interference of ~100 µm, we can stagger two shims
  Not clear how long they should be to reach the desired effect: lowering the max strain and the strain in the transition region during magnet powering
Shim 2
Shim 1
Full Load Key
Lshim
Wedge
Transition
Magnet
Center
Lshim

## Slide 7: Load Key Configuration - Proposal
Parametric study changing the length of the shim and its distance from the wedge transition
For a ‘MQXFA13’ coil pack, we need to extend the key for at least 3 inches after the transition (total length 6 inches)
  For lower values, the peak strain decreases, but the one at the transition increases!
  The effect should be visible on shell and/or pole gauges: ~20 MPa stress increase on both
Additional Key | Staggering Distance | Shell Center | Shell End | Pole Center | Pole Transition | Strain Max | Strain Transition
um | Inches | MPa | MPa | MPa | MPa | um/m | um/m
0 | / | 100.7 | 103.7 | 101 | 40.6 | 5164 | 2742
100 | 1 | 100 | 119 | 101.9 | 64.4 | 4378 | 3380
100 | 1.5 | 99.7 | 119.7 | 102 | 61.4 | 3300 | 4044
100 | 2 | 99.9 | 120 | 102 | 60.9 | 3820 | 2981
100 | 3 | 99.9 | 120.4 | 101.8 | 59 | 3553 | 2141
100 | 4 | 100.1 | 120.6 | 101.3 | 57.4 | 3577 | 1874

## Slide 8: MQXFA12b – Assembly Test
We wanted to test the shimming strategy during MQXFA12b assembly
However, we first checked that the test will not put in danger the coil/structure
Simulation steps
  Complete the first half of the loading
  Insert the ‘custom’ key
  Remove the custom key
  Complete loading
Simulated
Non-simulated

## Slide 9: MQXFA12b Testing – Coil Stress
Model target interference 300 um
Peak stress during ‘special key’ step is not larger than after full loading
Slight stress redistribution in the ends after special key unloading
  Peak stress not higher
  Frictional effects, difficult to predict and probably dependent on bladder operation sequence (e.g. if a bladder operation is interrupted we would also see a small stress redistribution)
  MQXFB experience suggests that these effects disappear during cooldown

## Slide 10: MQXFA12b Testing – Coil Strain
Longitudinal strain in the coil:
  Same considerations as for the peak stress
Structure checks in the back up slides

## Slide 11: Assembly Test – Chronology
Standard loading operations up to a 30 mils shim stack (12.75 mm + 0.762 mm)
  Operations stopped for one week – MPD collab. Meeting
Tapered key test:
  Insert the tapered keys on the lead end side
  Return to the constant thickness keys
Complete loading (41 mils) (same day)
Additional measurement stations installed on the LE shell (center) and on the pole, at the transition longitudinal location

## Slide 12: Assembly Test – Results - Center
Transfer function agreement ok overall
  Small variation of center TF after tapered key test
    Frictional effect? Stress relaxation?
  Offset with respect to key size in the ends
    Initial impact of radial size error seems lower than expected in this region
  Slope similar

## Slide 13: Assembly Test - Results
Looking only at the delta during tapered key test:
  Slight unloading in the center
  Load variation at the lead end gauge close to predictions (expected/measured):
    12/11 MPa on the shell
    -16/-19 MPa on the pole

## Slide 14: Conclusion
Local size variations can cause filament failure in the coil ends
  This means that we need a solution to use the coils with ‘small’ ends
Local prestress modifiers were investigated
  Increasing the key thickness in the ends decreases the strain
A ‘practical’ tapered load key shim configuration has been proposed
  Simulation results suggest that, with adequate staggering distances, the configuration can reduce the peak strain in the transition region
  Introducing the key during MQXFA12b loading operations is not of any danger to the coil (lower strain and stresses than after loading is complete)
We have tested the shimming strategy during MQXFA12b assembly:
  Measured prestress increase due to the tapered key close to prediction
  However, the measured stress at that location was higher than expected

## Slide 15: Extra

## Slide 16: Structure Verification
Structural checks performed comparing stress levels with A13 model results
  Quicker, avoids submodeling
  We can still check more in detail the magnets when we know coil dimensions and target key shape and size

## Slide 17: Structure Verification (1)
Special key solution has lower structure stress (~20%) w.r.t. full loading

## Slide 18: Structure Verification (2)
Yoke/pad stress slightly higher but still with very large margin over yield

## Slide 19: Prestress Modifiers – MT28 Key
Tapered key solution as efficient as the longer key shimming with no tapering