## Slide 1: Analysis of MQXFA17 Vertical Test NCR
Summary of contributions from all MQXF team members
MQXFA Mtg
June 4, 2024

## Slide 2: Outline
Quench History
Quench Start location
Voltage Signals analysis
Strain Gauges analysis
Quench Antenna analysis
Coil 239 DRs and Fabrication data
MQXFA17 Assembly data and NCRs

## Slide 3: Quench History

## Slide 4: Quench History

## Slide 7: MQXFA17 Quench Location

## Slide 8: Quench Location from Quench Antenna

## Slide 9: MQXFA17 Voltage Signals
(Vittorio)

## Slide 10: MQXFA13 Voltage Signals
(Vittorio)

## Slide 11
(Anis)

## Slide 12
Quench 15
(Anis)

## Slide 13
MQXFA07
MQXFA13

## Slide 14: Locations on Coil 227
Coil CAD model with quench locations
  “Calibration” is in progress
(Miao)

## Slide 15: Coil 239 Fabrication Data
Coil 239 Travelers and DRs are in FNAL Vector and BNL system:
  Vector link to Coil 239 Interface Travelers and DRs:
  https://vector-onsite.fnal.gov/GenerateTravelerRequest.asp?qsDocID=34203
Presented at MQXFA17 and MQXFA13b Coils Acceptance Review:
  MQXFA17 and MQXFA13b Coils Acceptance Review (October 6, 2023) · INDICO-FNAL (Indico)

## Slide 16: Cable QC Summary
All cables passed the required quality control testing per US-HiLumi-Doc 74
There were No Critical DRs
No impact on coil 239

## Slide 17: QXFA239 - DRs
DRs posted to interface traveler.
Critical = Affecting Form, Fit or Function
(as found)

## Slide 19: MQXFA17 Assembly Data and NCRs
MQXFA17 Structure and Shims Review:
  MQXFA17 Structure & Shims Review (October 18, 2023) · INDICO-FNAL (Indico)
  MQXFA17 NCRs:
    #593 – Coil 239 accelerometer issues upon arrival
    #601 – Proud pin on Coil 239 at 1365 mm from LE (modified alignment key)
MQXFA17 Specs Mtg:
  MQXFA17 Spec Meeting (March 15, 2024) · INDICO-FNAL (Indico)
  “MQXFA17 load keys are smaller than target because a coil reached 120 MPa” (Paolo)
MQXFA17 Fabrication Report:
  US-HiLumi-doc-5151
  Critical NCR for Overheated splice
  Critical NCR caused axial-preload unloading twice

## Slide 20: MQXFA17 Critical NCRs

## Slide 21: Magnet assembly and loading Specifications (shells)

## Slide 22: Magnet assembly and loading Specifications (coils)
SG
FBG @ 700 mm
FBG @ 1900 mm
FBG @ 3800 mm

## Slide 23: Delta between arc length excess straight section and spacer-wedge transition
Red & dark blue markers: measured at 207 mm and 4426 mm
Orange & light blue markers: measured at 260-300 mm and 4340-4380 mm

## Slide 24: Target loading key shim
For final loading key shim size reached during the pre-load operations, the following target is set:
At the end of the pre-loading operation, the sum of the loading shim size and the coil-pack radial dimension deviations in straight section, LE and RE shall be within the range achieved in magnets MQXFA14b and MQXFA05
  If, with such load key shim, the coil stress measured in 2+ strain gauges at the end of the loading or during bladder inflation is above the coil stress spec., priority should be given to keeping the coil stress within the specs.

## Slide 25: Summary and proposal
Proposed target
  Aiming at a shim of 42 mils, with the possibility of going to 42-44 mils depending on SG data
 | Ave ss | Key | Shim | Shim | Ave ss + shim
 | mm | mm | mils | mm | mm
A17 up | -0.004 | 13.84 | 43 | 1.092 | 1.088
A17 low | -0.004 | 13.77 | 40 | 1.016 | 1.012
 | LE | Key | Shim | Shim | LE + shim
 | mm | mm | mils | mm | mm
A17 up | -0.134 | 13.84 | 43 | 1.092 | 0.959
A17 low | -0.134 | 13.77 | 40 | 1.016 | 0.882
 | RE | Key | Shim | Shim | RE + shim
 | mm | mm | mils | mm | mm
A17 up | -0.125 | 13.87 | 44 | 1.118 | 0.992
A17 low | -0.125 | 13.82 | 42 | 1.067 | 0.941

## Slide 26: Key-shim size vs. bladder pressure

## Slide 27: Magnet assembly and loading Specifications (coils)
For the maximum stress reached during the pre-load operations:
  During the entire pre-load operation, the maximum compression measured on each coil shall never exceed -120 MPa
Peak stress on coils (MPa)
CQ1 | CQ2 | CQ3 | CQ4
-110 | -91 | -120 | -100
CQ1-700 | CQ2-700 | CQ3-700 | CQ4-700 | CQ1-1900 | CQ2-1900 | CQ3-1900 | CQ4-1900 | CQ1-3800 | CQ2-3800 | CQ3-3800 | CQ4-3800
-86 | -89 | -98 | -83 | -88 | -129 | -121 | -103 | -83 | -93 | -94 | -70
Electrical SGs
FBGs

## Slide 28: Magnet assembly and loading Specifications (shells)
For the pre-load targets at the end of the pre-load:
  The target average measured stress on coils, shells and rods at the end of the loading (after at least 24 h) shall be
    Shell average azimuthal stress: +58 ±6 MPa
Channel | SC02TT | SC02RT | SC02BT | SC02LT | Average
Preload (end) | 64 | 65 | 47 | 66 | 61
Overnight (end) | 63 | 65 | 45 | 66 | 60
Channel | SC04TT | SC04RT | SC04BT | SC04LT | Average
Preload (end) | 65 | 50 | 69 | 66 | 63
Overnight (end) | 65 | 50 | 68 | 65 | 62
Channel | SC07TT | SC07RT | SC07BT | SC02LT | Average
Preload (end) | 61 | 67 | 71 | 66 | 66
Overnight (end) | 60 | 67 | 71 | 65 | 66

## Slide 29: Magnet assembly and loading Specifications (coils)
For the pre-load targets at the end of the pre-load:
  The target average measured stress on coils, shells and rods at the end of the loading (after at least 24 h) shall be
    Coil (winding pole) average azimuthal stress: -80 ±8 MPa
Channel | CQ1T | CQ2T | CQ3T | CQ4T | Average
Preload (end) | -92 | -73 | -98 | -79 | -86
Overnight (end) | -93 | -72 | -98 | -80 | -86

## Slide 30: A17 Coil arc length and coil stress measurements
Computed on SG loc = SG data
Av straight section = -0.006 mm (465-4310 mm)
Min LE = -0.210 mm (260-300 mm)
Min RE = -0.197 (4426 mm)

## Slide 31: Coil arc length shimmed A13

## Slide 32: Coil and shell stress A13 Measured and computed (based on arc length shimmed)
SG at 3965 mm
FPG at 700 mm
FPG at 1900 mm
FPG at 3800 mm

## Slide 33: MQXFA17 Strain Gauge Data
Strain Gauge data analyzed by Dan
Small anomaly: Kink in axial rod (Q1) at low current

## Slide 34: Lead End vs Return End

## Slide 35: Iron to Stainless Steel

## Slide 37: CLIQ
CLIQ add current to coils in Q2 and Q4
   shorter training in these coils
  Possible higher risk of damage in these coils during quench above nominal current?
  (Stoyan and Sandor)
Magnet 13, quench 22, current in Q2/Q4:
CLIQ boost based on 14126 A (quench 1 current) and peak current of 15000 A : 874 A
CLIQ boost based on 16362 A (quench 22 current) and peak current of 17106 A : 744 A

## Slide 38
Delta I = - 283 A
Q4 coil

## Slide 39
Delta I = - 7 A
Q3 coil

## Slide 40
Delta I = - 80 A
Q3 coil

## Slide 41
Delta I = - 45 A
Q1 coil

## Slide 42
Magnet | Quadrant | # previous quenchs at higher current | Delta current wrt last previous quench (A) | Previous quenches in same coil & close-by position | All previous quenches in same coil
MQXFA17 | Q4 | 4 | -283 | 0 | 0
MQXFA07 | Q3 | 0 | -7 | 0 | 1
MQXFA08 | Q3 | 1 | -80 | 1 | 2
MQXFA13 | Q1 | 1 | -45 | 1 | 4

## Slide 43
Coils in MQXFA magnets |  |  |  |  |  |  |  |  |  |  | 
 |  | CLIQ + |  | CLIQ + |  |  | Lead End arc length + loading shim |  |  |  | 
Magnet | Q1 | Q2 | Q3 | Q4 |  |  | mm |  |  |  | 
MQXFA03 | 204 | 110 | 202 | 111 |  |  |  |  |  |  | 
MQXFA04 | 203 | 113 | 206 | 112 |  |  |  |  |  |  | 
MQXFA05 | 207 | 116 | 209 | 115 |  |  | 0.862 | Passed endurance test |  |  | 
MQXFA06 | 122 | 119 | 211 | 123 |  |  |  |  |  |  | 
MQXFA07 | 212 | 124 | 214 | 114 |  |  | Closed pole-key gaps |  |  |  | 
MQXFA07b | 212 | 124 | 218 | 114 |  |  | 0.932 |  |  |  | 
MQXFA08 | 215 | 126 | 213 | 128 |  |  | Closed pole-key gaps |  |  |  | 
MQXFA08b | 215 | 126 | 219 | 128 |  |  | 0.768 | 750-800 range |  |  | 
MQXFA10 | 132 | 221 | 131 | 129 |  |  | 0.799 | 750-800 range |  |  | 
MQXFA11 | 223 | 222 | 134 | 135 |  |  | 0.937 |  |  |  | 
MQXFA13 | 227 | 139 | 229 | 141 |  |  | 0.662 | lower than 700 |  |  | 
MQXFA14b | 217 | 230 | 143 | 231 |  |  | 0.907 |  |  |  | 
MQXFA15 | 233 | 226 | 220 | 117 |  |  | 0.922 |  |  |  | 
MQXFA17 | 151 | 237 | 152 | 239 |  |  | 0.791 | 750-800 range |  |  | 
MQXFA13b | 150 | 139 | 229 | 141 |  | NOT tested yet |  |  |  |  | 
MQXFA16 | 144 | 235 | 145 | 236 |  | NOT tested yet |  |  |  |  | 
MQXFA12b | 224 | 159 | 225 | 148 |  | NOT tested yet |  |  |  |  | 

## Slide 44: Back-up Slides

## Slide 45: Summary for MQXFA13
No major DRs/NCRs
Coil 227 has the smallest arc length among tested coils, although it was shimmed
It has also a small arc length in the lead end, similarly to other coils that met requirements
MQXFA13 had small key shims, similarly to other magnets that met requirements

## Slide 46: Change to MQXFA Series Magnet Production Specification (-110 MPa peak stress during loading)
Paolo Ferracin, G. Ambrosio, Dan Cheng, Laura Garcia Fajardo, Giorgio Vallone
on behalf of the MQXF collaboration
AUP Meeting
LBNL, USA
July 21st, 2023

## Slide 47: Arc length excess

## Slide 48: A13 coil size: unshimmed vs shimmed

## Slide 49: A13 coil size: unshimmed vs shimmed Including ends

## Slide 50: Finite element analysis
Impact of the coil pack size on the coil strain, in particular in the ‘wedge/end-spacer transition’ region

## Slide 51: Maximum Long. Strain
The peak strain is a function of the applied prestress
  Clearly the distance between the red and black line will be different for each coil pack shape

## Slide 52: Increase pre-load proposal
We could define an unique criteria on the required minimum prestress at room temperature
  E.g. limit strain = 0.3%
  For MQXFA13, this would require a prestress of ~90 MPa
Maximum
Minimum
Nominal

## Slide 53: Proposal: max allowable stress during pre-load from 110 to 120 MPa
-120

## Slide 54: Comparison with previous magnets: Delta coil arc length and key size
Magnet | Average ss | LE min | RE min | LE delta | RE delta | Key
 | mm | mm | mm | mm | mm | mm
A15 | 0.001 | -0.156 | -0.070 | -0.157 | -0.071 | 13.72
A14b | -0.011 | -0.203 | -0.167 | -0.192 | -0.156 | 13.84
A13 | -0.007 | -0.230 | -0.148 | -0.223 | -0.141 | 13.72
A8b | -0.001 | -0.285 | -0.214 | -0.284 | -0.213 | 13.77
A11 | 0.006 | -0.196 | -0.074 | -0.201 | -0.079 | 13.74
A10 | -0.145 | -0.348 | -0.313 | -0.203 | -0.168 | 13.82
A8 | -0.046 | -0.340 | -0.269 | -0.294 | -0.223 | 13.72
A7 | -0.055 | -0.218 | -0.179 | -0.164 | -0.125 | 13.77
A6 | -0.072 | -0.217 | -0.279 | -0.145 | -0.207 | 13.72
A5 | -0.037 | -0.241 | -0.165 | -0.205 | -0.129 | 13.79

## Slide 55: Delta stress due to coil arc length and key size
Computation of the delta stress in the LE of each magnet with respect to a “nominal magnet” with
  Coil end with nominal dimensions
  Loading keys of 13.76 mm (average of all magnets)
Based on sensitivity analysis (computation and measurements)
  +0.100 mm of coil outer radius increase
    -20 MPa of coil stress variation
    +12 MPa of shell stress variation

## Slide 56: Delta stress due to coil arc length and key size
Magnet | LE min | r LE | Key | key (wrt 13.76 mm) | r+key | 
 | mm | mm | mm | mm | mm | MPa
A15 | -0.156 | -0.099 | 13.72 | -0.041 | -0.140 | 28
A14b | -0.203 | -0.129 | 13.84 | 0.079 | -0.050 | 10
A13 | -0.230 | -0.146 | 13.72 | -0.041 | -0.187 | 37
A8b | -0.285 | -0.181 | 13.77 | 0.009 | -0.172 | 34
A11 | -0.196 | -0.125 | 13.74 | -0.021 | -0.146 | 29
A10 | -0.348 | -0.222 | 13.82 | 0.059 | -0.163 | 33
A8 | -0.340 | -0.216 | 13.72 | -0.041 | -0.257 | 51
A7 | -0.218 | -0.139 | 13.77 | 0.009 | -0.130 | 26
A6 | -0.217 | -0.138 | 13.72 | -0.041 | -0.179 | 36
A5 | -0.241 | -0.153 | 13.79 | 0.029 | -0.124 | 25

## Slide 57: Shimming and Understanding

## Slide 58: MQXFA13 Coil Size Analysis
G. Vallone, G. Ambrosio, D. Cheng, P. Ferracin, L. Garcia Fajardo
July 12, 2023
AUP-CERN Structure WG Meeting

## Slide 59: Introduction
We want to test the impact of the coil pack size on the coil strain, in particular in the ‘wedge/end-spacer transition’ region
  Plot is the error (distance from the average) on the coil size (radial, computed from L+R measurements)
Included in the MQXFS octant model introducing an offset on the coil/filler contact
  All components bonded, separation allowed between the wedge and the spacer, and the coil and the winding pole
    In this configuration we see a large strain spike in MQXFA07
  Double checked that the contact gap is as expected at the start of the simulation
Contact
Offset

## Slide 60: Coil Strain – Nominal Interference
Peak longitudinal strain increases from 2249 µm/m to 2893 µm/m
Nominal
Including Size Error

## Slide 61: Local Size/Prestress Modifiers (1)
Increasing the prestress on the whole magnet might ‘push’ the coil stress over the project-defined limits
Alternatively, we could act on ‘local’ modifiers:
  Shimming the coil pack in the coil ends
    Only feasible as ‘radial shimming’, as ‘steps’ on midplanes could damage the leads (see MQXFA09 ‘Kapton fold’ analysis)
  Increasing the key size in the coil end region
    The coil is not sensitive to ‘steps’ in the key size (see missing key analysis during bladder operation, e.g. MQXFA12)

## Slide 62: Local Size/Prestress Modifiers (2)
FE analysis considering:
  Radial shimming (100 µm) in the end-shoes
    Available shimming region relatively small, as we do not want steps over the cable
  Key size increased (100 µm) along the whole ‘short’ shell
Coil/Collar Shimming
Key Shimming

## Slide 63: Local Size/Prestress Modifiers - Results
Radial shimming in the end-shoes goes in the wrong direction
    Very short shimming space available
    To be understood – probably LQ effect + blocking long. prestress
Key shimming can remove completely the effect of the undersized coil ends (considering the A13 case)

## Slide 64: 7/25/2023
What if in the previous computations we look at:
Azimuthal prestress on the pole at the longitudinal location of the wedge-spacer interface

## Slide 65
 The longitudinal strain depends on the azimuthal prestress at cold at the same location

## Slide 66: Mechanism
The local azimuthal pre-stress generates/contributes to local axial pre-stress by Poisson effect
When the magnetic forces exceed the axial pre-stress the coil is less rigid  kink

## Slide 67: Coil 157 CMM in Lead End
Average of transition and non-transition sides
Chart: Distance from Lead End (mm)
| 70 | 100 | 150 | 180 | 207 | 220 | 260 | 300
Average | -119 | -123 | -137 | -151.5 | -173 | -163 | -137.5 | -99
Distance from LE | NT side | T side | Average
mm | um | um | um
70 | -121 | -117 | -119
100 | -125 | -121 | -123
150 | -140 | -134 | -137
180 | -155 | -148 | -151.5
207 | -179 | -167 | -173
220 | -171 | -155 | -163
260 | -139 | -136 | -137.5
300 | -102 | -96 | -99
X-sections in addition to 70 and 207 (standard locations)

## Slide 68: Back up Slides

## Slide 69: From Specs Mtg

## Slide 70: MQXFA07
Analysis of voltage rise (by V. Marinozzi) came to conclusion that quench #10 (at 4.5 K) started very close to voltage tap A4
  This info can be use to “calibrate” position of Quench Antenna elements wrt coil 214
This analysis confirmed that limiting quenches in coil 214 are starting in the Lead End area

## Slide 72: Inspection Plan
Before MQXFA07 dis-assembly:
Magnetic measurements at LBNL
After MQXFA07 dis-assembly:
Coil visual inspection
  Compare coil 214 to other MQXFA07 coil
  Compare MQXFA07 coils to prototype coils
Other tests:
  Heater-Coil Hipot
Lead end + some Straight Section, and Return end will be cut and sent to CERN for tomography
  Picture analysis looking for conductor issues
  Compare to prototype coil P06 and MQXFB coils
Coil sections at locations highlighted by tomography
  Micrographic inspection looking for broken sub-elements

## Slide 73: MQXFA training

## Slide 74
TURN 2 (INNER LAYER B1)
TURN 4 (LAST FULL TURN POLE BLOCK)
TURN 5 (TRANSITION B1 to B2)
TURN 6 (FIRST FULL TURN B2)
A04
A03
CABLE SECTIONS FOR WHICH FIELD IS SHOWN IN NEXT SLIDES
A04-A03
A04-A03
A05

## Slide 75
TURN 4 (LAST FULL TURN POLE BLOCK)
At 15.31 kA

## Slide 77
“The collapsed cable was on the 5th turn from the pole tip at the LE (between spacers B2-IC1 and B2-IC2), so the area is included in the A3-A4 multiturn block. A sketch showing the area is attached.
The issue noted the next morning was the same area. Before resuming in the morning it was noted that the strands were out of place a bit so we unwound the ½ turn to put them back in position before continuing.”
Info by Jesse

## Slide 78: Quench Antenna analysis
According to Anis the QA shows that the quench location (QL) is at 2010.8 mm from magnetic center toward the lead end.
  “I redid the calculation using the updated drawing. The quench location in coil 214 (QA channel Z4300) is at z=2010.8 mm (toward the LE) from the magnetic center (512.2 mm from the top surface of the splice box).”
  Center of QA element wrt bottom edge is 50 mm
According to Joe the QA shows that the quench location (QL) is at ~2060 mm from magnetic center toward the lead end.

## Slide 79: Quench Start Location Computation
 | Coordinates (mm)
Top surface of the splice box in magnet | 0
Top surface of the magnet yoke | 179.7
QXFA 214 Quench location (from top surface of the splice box) | 512.2
QXFA 214 Quench location (from top surface of the magnet yoke) | 332.5
Length from top yoke to bottom yoke | 4563
Measured length of QXFA 214 | 4525.4
QXFA coil length in CAD model | 4523
Shim thickness at QXFA 214 coil each end | 18.8
The center of that QA element is 50 mm toward the lead end. | 50
QXFA 214 Quench location (from QXFA 214 lead end splice block) | 263.7

## Slide 80: Updated Plot
Nominal distance coil end to first pin hole at LE: 319.3 mm
“Yes, measurement for coil 214 was 319.8 from coil end to first pin hole at LE” (Jesse)

## Slide 81
Summary of QA data on Q#9 and Q#10
Quench #9 (and the other quenches like it) seems to show large flux redistribution relatively early wrt when the quench detection threshold is exceeded (i.e. start at -22ms). There seems to be one main location (ZQA at z=2000; i.e. signal Z4300) which shows large slow rising redistribution (V=18mV) while other ZQA are much less affected, and neither does the activity seem to ‘spread’ very much to them. This gives an ‘asymmetric’ look to the ‘heat map’ representations of the flux/voltage events. The azimuthal location of Z4300 may be particularly oriented to pick up the flux redistribution event, or it may just be very local and relatively somehow slow spreading (?). The TQA location affected most is the the Q3 transition-side antenna (T150), with good symmetry with the neighboring T120 and T180 QA. The flux excursion is seen to be a relatively slow oscillation.
Quench #10 shows some small redistribution (<5mV) but very quickly followed by a large (~25mV), fast redistribution that is seen simultaneously in several ZQA with similar amplitude. The quench detection threshold is exceeded within 10ms. The largest amplitude is in the antenna at Z=1900 (signal Z4200), which is shifted slightly compared to Q#9. The Z4300 antenna has different character than it did in Q#9 and the amplitude of three antennas are pretty similar in this event (Z4150, Z4200, Z4300) and the activity seems more symmetric. The TQA location affected most is T180 with a bit of asymmetry that actually shows the T210 (Q4) more active than the T150. Since the voltage taps don’t show a shift in quench location towards midplane, this may instead indicate a difference in the direction of flux redistribution (see next page). The TQA flux excursion here is much faster (and of a bit larger amplitude) than that of Q#9.
The TQA having largest signal (T180) in Q#10 also had large ‘noise’ (pickup of mech. vibrations?) – this was not seen in this signal on any other quench (two previous quenches (Q#6 and Q#7) showed 4kHz and 2kHz noise on a different signal (T240)). This noise was roughly of frequency 12kHz, but was broad and did not really look like electrical pickup).
J. DiMarco
07Sep2021
Slides by Joe DiMarco

## Slide 82
A07
Q9
Slides by Joe DiMarco, 11/11/2021

## Slide 83
A07
Q10
Slides by Joe DiMarco, 11/11/2021

## Slide 85
Magnet Top
Magnet Bottom

## Slide 86
Z=0 is the magnetic center (position determined from the MM measurement and the drawing at the end of the MM test plan)
MQXFA07 Quench #10 4.5 K , 20 A/s, 0.9 A/s2 IQ = 15832 AQI = 24.3 MIIts
Location = Coil 214 (Q3) A3-A4 + A4-A7
Slides by Anis

## Slide 87
Z=0 is the magnetic center (position determined from the MM measurement and the drawing at the end of the MM test plan)

## Slide 88: Back up Slides

## Slide 89
TURN 1 (INNER LAYER POLE)
At 15.31 kA

## Slide 90
TURN 4 (LAST FULL TURN POLE BLOCK)
At 15.31 kA

## Slide 92: QXFA239 – Length, Gaps
Coil length within spec.
(207 error in initial pole gap setting)

## Slide 93: QXFA239 - Reaction
Temperatures and dwell times all within spec.

## Slide 94: QXFA239 - Electrical
Final electrical checks – all passed

## Slide 95: QXFA239 - Electrical