## Slide 1: MQXFA12b – End Shell Inspection Crack Considerations
G. Vallone, G. Ambrosio, D. Cheng, P. Ferracin, L. Garcia Fajardo, J. Herrera
July 31, 2024
For discussion

## Slide 2: Introduction
Tapered loading keys increase the stress in the short shells at the magnet ends
With the nominal coil size, these were designed to have a ~20% margin with the MQXFAP1b target prestress level (130 MPa at cold on the central shell)

## Slide 3: Shell Stress – Limiting Locations
Three dangerous locations identified with FE analysis
Limiting point:
  ‘Weld strip’ cut-out
    Fillet radius=0.5 mm due to weld strips geometry limitations
Triangle
Weld block
Weld strip

## Slide 4: Shell Stress – Limiting Locations
The peak stress is on the weld strip cut-out, on the magnet end side
Weld strip cut-out
Lead
End
Arrow points to magnet center

## Slide 5: Shell Stress - Limits
Load factor from grade IV analysis, assuming 130 MPa shell stress at cold (MQXFAP1b):
  Load factor of 1.24 on the weld strip cut out with a 2 mm crack
Valid for AP1b case (130 MPa at cold, central shell)

## Slide 6: Shell Stress - Cool-Down, Measured
We can reasonably assume a central shell stress ~140 MPa at cold
  10 MPa stress increase with respect to the A12b case
  Not sure what happened on A15, but seems an outlier (but we better not be in that situation)
  ~8% load increase

## Slide 7: Assembly – Full Key - 2
We do not have a ‘precise’ measurement on the shell stress, just an estimate
  SG were removed after full loading
The predicted stress in the shell is higher than expected
  86 MPa (measured), 75 (model) ~ 11 MPa delta ~14%

## Slide 8: Load Factor – From Old Study
Design load factor: 1.24
New load factor (8% load increase, 14% model error) ~ 1.00
  Means no margin

## Slide 9: Maximum Crack Size (Version 1…)
Quick estimate (non-conservative), assume:
  If we want a load factor of 1.2, we have:

## Slide 10: Crack Size?!?
I think there is an error in the design criteria
  The actual flaw size specified in class AA is 1.2 mm
  Am I missing something? It would mean that we are fine!
ASTM B594-19
Actual Inspection
Design Criteria
Heng’s Paper

## Slide 11: Crack Analysis – Interaction Integral Method
‘Design criteria’ crack analysis performed with weight functions
  Pre-computed ‘influence coefficients’ of the separation forces on a crack in any region
  K1c=24 MPa m2, K1 ~24*0.8=19.2 MPa m2
We can also compute the stress intensity factors on a real crack, on the short shell submodel
  Global model: reference model with 133 MPa after cooldown stress on the central shell

## Slide 12: Crack Analysis – Tested Geometries (5)
Edge Crack normal to the XY plane seems the worst configuration (see back-up slides)

## Slide 13: Crack Face Normal to XY Plane
K1, worst angle ~16 MPa m2 (2a = 2 mm)
Seems lower than what was obtained with the weight functions
  However, getting closer to the corner increases K1
  Assuming 17 MPa m2, this would be a ~30% margin over fracture
z | K1
225 | 15.1
250 | 15.6
259 | 16.7

## Slide 14: Crack Face Normal to XY Plane
SIF decreases with crack size

## Slide 15: Conclusion
We have two factors reducing the margin:
  Higher prestress
  Higher than expected end-shell stress
  This brings the load factor from 1.24 to 1.0 (no margin)
The load factor was estimated on a 1.77 mm crack
  This seems to be non-consistent with the AA inspection criterion applied to our shells
  This means that, for a required load factor of 1.2 we need a crack < 1.24 mm
    Acceptable
A LEFM analysis was performed
  Preliminary results suggest that the actual margin for a 2 mm round crack is ~30%

## Slide 16: Summary
(Back up slides)
Subsurface cracks do not seem dangerous

## Slide 17: Crack Face Normal to XY Plane
K1, worst angle ~16 MPa m2 (2a = 2 mm)
Seems lower than what was obtained with the weight functions
  However, getting closer to the corner increases K1
z | K1
225 | 15.1
250 | 15.6
259 | 16.7

## Slide 18: Crack Analysis – Tested Geometries (1)
Sub-surface crack in the XY plane (2a = 2 mm)
Can change x, y, z
Values seem low (2 mm diameter crack, very close to the edge)

## Slide 19: Crack Analysis – Tested Geometries (2)
Sub-surface crack in the XY plane (2a = 2 mm)
Can change x, y, z
Low stress

## Slide 20: Crack Analysis – Tested Geometries (3)
Sub-surface crack in the XY plane, normal to the edge (2a = 2 mm)
Very close to the edge
Low stress

## Slide 21: Crack Analysis – Tested Geometries (4)
Sub-surface crack in the XY plane, normal to the edge, near the corner (2a = 2 mm)
Worst case orientation not clear
Low stress – seems always the case for sub-surface cracks

## Slide 22: Crack Analysis – Tested Geometries (5)
Edge Crack normal to the XY plane
Seems the worst configuration

## Slide 23: Crack Face Normal to XY Plane
K1, worst angle ~16 MPa m2 (2a = 2 mm)
Seems lower than what was obtained with the weight functions
  However, getting closer to the corner increases K1
z | K1
225 | 15.1
250 | 15.6
259 | 16.7

## Slide 24: Crack Analysis – Elasto-Plastic
K1 is mostly used in linear elastic fracture mechanics
Checking how much we would be wrong with an equivalent J-integral evaluation on a plastic model
  Assuming ~plane strain around the crack tip for the conversion
  Seems ok to just use linear properties
Etg | K1 | Jintegral | K1J
79.0 | 15.1 | 2.8 | 15.7
1.0 | 15.1 | 2.9 | 15.8
0.1 | 14.4 | 2.6 | 15.1

## Slide 25: Crack Analysis – Tested Geometries (5)
Edge crack normal to the corner

## Slide 26: Inspection - Shell Stress – Limiting Location
More images of the weld strip cut-out
Would inspect the region near the corner
  ~50 mm from the filled center on both sides
  See last slide for maximum allowed crack ‘signal’
Peak stress location

## Slide 27: Sample Set-Up
Typical flat bottom specimen
Not sure if we can just do the same but with a smaller size
  If they specify these ‘class’ sizes, probably the noise becomes too large when reducing it
  We would need an expert opinion on this