## Slide 1: FBK IV analysis* @ Ferrara *tested by FBK M. Andreotti, R. Calabrese, D. Casazza, A. Cotta Ramusino, S. Chiozzi, R. D’amico, M. Fiorini, T. Giammaria, M. Guarise, E. Luppi, I. Neri, L. Pierini, L. Tomassetti, in collaboration with the Bologna group
DUNE photo-sensor meeting
22/10/2024

## Slide 2: Content
General info
Differences with CACTUS typical data
Results
Changes in the algorithm
Additional results

## Slide 3: General info
Samples
100 SiPM strips
FBK model (HD pre-production)
Aim
Compare the IV characterization methods
  CACTUS : relative derivative →
  Vendor : 2nd logarithmic derivative method →

## Slide 4: Differences with our typical data
Disclaimer: The CACTUS analysis algorithm is somehow optimized for HPK strips, due to a higher population of measurements
Differences with CACTUS standard measurements
Higher Vstep : 50 mV vs [10 – 20] mV
Lower noise : probably due to different instrumentation

## Slide 5: Results – VBD distribution

## Slide 6: Results – mean VBD per strip

## Slide 7: Differences with our typical data
Disclaimer: The CACTUS analysis algorithm is somehow optimized for HPK strips, due to a higher population of measurements
Differences with CACTUS standard measurements
Higher Vstep : 50 mV vs [10 – 20] mV
Lower noise : probably due to different instrumentation

## Slide 8: Differences with our typical data
Disclaimer: The CACTUS analysis algorithm is somehow optimized for HPK strips, due to a higher population of measurements
Differences with CACTUS standard measurements
Higher Vstep : 50 mV vs [10 – 20] mV
Lower noise : probably due to different instrumentation
The range of the parabolic fit is not optimized

## Slide 9: Changes in the algorithm
Raise NFIT* (5 → 8) in favor of VBD spread
*Minimum number of points for the parabolic fit around the first guess of VBD
Current (A)
Current (A)
NFIT = 5
NFIT = 8

## Slide 10: Results - NFIT - VBD distribution
NFIT = 5
NFIT = 8
~ same mean value (Δ = 2 mV)
Smaller spread

## Slide 11: Results - NFIT - VBD distribution
NFIT = 8

## Slide 12: Conclusions
Received IV characterizations data from FBK
  100 strips (for HD pre-production)
Analysis with standard CACTUS algorithm
Differences with our data → tune the algorithm
  Optimization of fit range
  Impact on the results

## Slide 13: BACKUP

## Slide 14: Reverse IV analysis methods
CACTUS
FBK