## Slide 1: 302.4.01 Magnets Vertical Test at BNL Weekly Status
Febin Kurian
4-Nov-2024

## Slide 2: MQXFA18-Training Summary
Spontaneous quench test program at 1.9K; Ramp to 16530 A
(Q1= Coil 160, Q2=Coil 246, Q3=Coil 243, Q4= Coil 154)
Chart: MQXFA 18 Vertical Test All tests at 1.9 K, 20A/s unless specified otherwise
| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22 | 23 | 24 | 27 | 28 | 29 | 30 | 31 | 32 | 33 | 34 | 35
Quench(Q1) | 14.832 | 15.571 | 15.687 | 15.879 | 16.08 | 16.106 | 16.118 | 16.165 | 16.225 | 16.32 | 16.282 | 16.441 | 16.354 | 16.141
Trip | 16.23
Quench(Q3)
Quench(Q4)
Inominal(kA) | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23
I_Acceptance (kA) | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53 | 16.53
No Quench | 16.53 | 16.23 | 16.53 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23 | 16.23

## Slide 3: MQXFA13b-Quench Location Summary
Chart: MQXFA18 Longitudinal quench location from Quench Antenna
| 61 | 1261 | 11 | 311 | -1389 | -139 | -1189 | -689 | -189 | -639 | -939 | 261 | 111 | -589
Quench No. | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 22 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22
Q1 (160) | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15 | 16 | 17 | 18 | 19 | 20 | 21 | 22

## Slide 4: MQXFA18 – Remaining
Magnet is warmed up
  Expected to be taken out of dewar and disconnected by tomorrow
  Outgoing warm outgoing measurements

## Slide 5: Next Magnet - MQXFA12b
Magnet is under incoming-inspections
  Expected to finish all horizontal tests today
  Expected to be moved to dewar on Tuesday (11/12/24)
  HiPot Failure:
    Coil to magnet shell (shell grounded) : Passed (3.680 kV)
    Quench Heaters (All) to shell(shell grounded): Arc fail (at 1.59 kV)
    Quench heaters(1-4) to shell (shell grounded): passed (3.680kV)
    Quench heaters(1-4) to Coil (shell grounded): Arc fail (at 0.94kV)
  After repairing the insulation CLIQ lead, hipot again
    Quench heaters(1-4) to Coil (shell grounded): Arc fail (at 0.78kV)

## Slide 6: Second Top Hat Repair
  Heaters: All Passed Hi Pot
  V-taps: Undergoing pin-by-pin hipot
    Did not pass hipot in the past: VT3, VT4,VT5
    Passed Hipot: VT1, VT2, VT6

## Slide 7: CRYOGENIC STATUS
CTI 4000 system status
  Running
Linde 1610 system status
  Running