## Slide 1: FNAL On Hold Coils
QXFA # | Description | Repaired (Y/N) | Passed Electrical | Passed CMM
121 | Deflected leads after reaction | n/a |  | 
125 | Midplane damage using file after VPI | Y |  | 
127 | QH to coil short caused by S2 bead. Repaired, passed coil acceptance review & shipped to LBNL. Returned to FNAL for S2 glass bead inspection/removal (completed May 2023). | Y |  | 
140 | QH to coil shorts caused by S2 beads. 2 repairs  2 repair impregnations | Y |  | 
142 | Heater to coil hipot failure in MQXFA14 | Y |  | 
146 | Mid plane delamination | n/a |  |