## Slide 1: QXFA121 Reacted Coil Lead Displacement
Fred Nobrega
Giorgio Ambrosio
Coil Working Group Meeting
February 12, 2020

## Slide 2: QXFA121 Prep for Impregnation
The mandrel block stuck to the base plate. During the removal process the technician bumped the tip of the L2 lead. The lead was displaced in the plane of the mid-plane shim.
DR11968 was written.

## Slide 3: Layer 2 Lead
No visible strand damage.

## Slide 4: Bending Strain
Single wire bending strain | mm | inches | inches | inches
Radius after bending | 548.132 | 66.25 | 33.31 | 21.58
Strand Dia | 0.85 | 0.715 | 0.715 | 0.715
Stain | 0.00078 | 0.00025 | 0.0005 | 0.00078
Strain due to bending |  |  |  |  | 
 | mm | inches | inches | inches | 
Radius before bending | infinite |  |  |  | 
Radius after bending | 548.132 | 66.25 | 33.31 | 21.58 | 
Cable width | 18.15 | 0.715 | 0.715 | 0.715 | 
Drop from horizontal | 19.8 mm | 1/4" | 1/2" | ~3/4" | 
Max strain | 0.0166 | 0.0054 | 0.0107 | 0.0166 | 
criteria | 0.0005 |  |  |  | 
damage threshold | 0.0020 |  |  |  | 

## Slide 5: Mitigation
Tap threaded holes to mandrel blocks to extract mandrel
Modify size of tab on the bottom of mandrel blocks that need to be removed.
Clamp lead to SS midplane shim after removal of 1st mandrel block.