## Slide 1: MQXF125 Midplane Repair Options
Fred Nobrega – FNAL
Coil Working Group Meeting – Wednesday Jan 27, 2021

## Slide 2: Discrepancy 12166
Description
  After coil QXF125 impregnation and during epoxy flash removal, too much epoxy and fiberglass was filed exposing the corner of the cable.
Cause
  Improper use of file angle and pressure
Repair options
  Build up with Stycast then sand to shape
  Remove L2 midplane G11 insulation & replace with S2 glass, 2nd impregnation.
Details in following slides.

## Slide 3: QXFA125 Damaged Area
Exposed Cable
Lead End
Lead End
50 mm
Chamfer length = 90 mm

## Slide 4
\\tdserver1\project\HFM\LARP\QXF Coils\QXFA Coils\QXFA 125\DR Post Impregnation Filed Lead\QXFA125\Picture \A007 - 20201013_095629
4/64 = 0.0625” (1.588 mm)
1/64 = 0.016” (0.397 mm)
Lead End
Lead End

## Slide 5: QXFA125 CMM Scan
Midplane
Coil OD
COIL OD
0.145 mm cable insulation
0.100 mm trace
0.310 mm S2 glass
0.555 mm nominal thickness
Midplane
0.145 mm cable insulation
0.125 mm G11
0.270 mm nominal thickness

## Slide 6: Deformed Cable Strand
Quadruplet cable edge
(worst configuration for A125 damage)
Triplet cable edge
R1= 0.4 mm
R2= 0.45 mm

## Slide 7: Midplane Repair, Stycast
Build up with Stycast
Sand to shape with new tool.
Midplane
Coil OD

## Slide 8: Midplane Repair, 2nd Impregnation
Remove 90 mm of L2 G11 midplane.
Add 2 layers S2 glass
Perform 2nd full impregnation
QXFA127 before
QXFA127 after
QXFA213 before
QXFA127 after
Coil Midplane
Coil Outer Diameter