## Slide 1: Coils on Hold
Jesse Schmalzle
November 14, 2024

## Slide 2: DRs
DRs
216 also in storage – removed from magnet 09 after Kapton pinched at midplane

## Slide 3: QXFA210
Coil 210 – 2 cable strands broken during prep for impregnation.
  Location 1 cm beyond coil end saddle, at start of Nb3Sn to NbTi splice.
  Damage is at inner edge of inner layer coil lead.
  Cable solder filled starting 5 cm before damaged area to aid in current sharing.

## Slide 4: QXFA228 / QXFA238
  Coil 228 – coil to pole resistance below spec.
    Standard coil to pole hipot at 100 volts – passes with all pole segments connected EXCEPT NL segment.
    NL pole segment reaches 52 volts with leakage current of 14.1 µA.
  Coil 238 – coil to pole connection.
    Standard coil to pole hipot at 100 volts – passes with all pole segments connected EXCEPT LE segment.
    LE pole segment shows 120 kOhm coil to LE pole segment.

## Slide 5: QXFA254
Fiberglass cable insulation damage and cable scratches noted during prep for reaction.
  Damage caused by razor blade when trimming fiberglass interlayer insulation after coil curing.
  2 locations, each area ~ 2.5” long:
    Inner layer coil midplane, transition side, 39” from NL end.
    Outer layer coil midplane, transition side, 90” from NL end.
  Inspection and photos before and after reaction.
    Inner layer – scratches in copper.
    Outer layer – scratches in copper, 4 small black spots observed under magnification after reaction.
  Silicone mold putty impression made for detailed inspections.

## Slide 6: QXFA254