## Slide 1: FBK IV analysis* @ Ferrara (part 2) *tested by FBK M. Andreotti, R. Calabrese, D. Casazza, A. Cotta Ramusino, S. Chiozzi, R. D’amico, M. Fiorini, T. Giammaria, M. Guarise, E. Luppi, I. Neri, L. Pierini, L. Tomassetti
DUNE photo-sensor meeting
12/11/2024

## Slide 2: Last meeting
Analysis of data from FBK HD pre-production
Differences with CACTUS typical data
Results
https://indico.fnal.gov/event/66659/contributions/302064/attachments/182669/250861/DUNE_meeting_Tommaso_Giammaria_22_10_2024.pdf

## Slide 3: General info
Samples
100 SiPM strips
FBK model (HD pre-production)
Aim
Compare the IV characterization methods
  CACTUS : Normalized First Derivative (NFD) →
  Vendor : 2nd logarithmic derivative (SLD) →

## Slide 4: General info
News
Received results from FBK (both NFD and SLD methods)
Discussed with FBK about different VBD estimators
IV curve types (room T)
Packaging IV:
  Strip (or single SiPM ?) level
  Large Vstep: 50 mV (CACTUS: 20 mV)
Parametric IV, also called Wafer Level (WL) IV:
  WL → same temperature for all the SiPMs → more stable
  Larger Vstep: 100 mV (!!)

## Slide 5: Single IV curve – packaging
NFD
SLD

## Slide 6: Single IV curve – parametric (or WL)
NFD
SLD

## Slide 7: Results – VBD distribution
IV curve type
Packaging IV
Parametric IV
Method
NFD
SLD

## Slide 8: Results – VBD distribution
IV curve type
Packaging IV
Parametric IV
Method
NFD
SLD

## Slide 9: Results – VBD distribution – packaging - differences

## Slide 10: Results – VBD distribution
IV curve type
Packaging IV
Parametric IV
Method
NFD
SLD

## Slide 11: Results – VBD distribution
IV curve type
Packaging IV
Parametric IV
Method
NFD
SLD

## Slide 12: Results – VBD distribution – parametric - differences

## Slide 13: Conclusions
Comparison of CACTUS/FBK analyses on the same data set
  Parametric (wafer level) IV (100 mV step)
  Packaging IV (50 mV step)
Need a finer resolution for grouping SiPMs
  waiting for data with higher resolution* from FBK
  *50 mV step and 10 mV step

## Slide 14: BACKUP

## Slide 15: Results – VBD distribution - packaging – max

## Slide 16: Results – VBD distribution - parametric – max

## Slide 17: Reverse IV analysis methods
CACTUS
FBK

## Slide 18: 100 mV step, SLD maximum