## Slide 1: QXFA254 Coil Review
Jesse Schmalzle
December 12, 2024

## Slide 2: Outline
Coil Fab DRs
Additional Info
  Coil length, Pole gaps
  Reaction plots
  Electrical Data
Notes:
  Series coil.
  After to change for B6 adjustment.

## Slide 3: QXFA254 - DRs
DRs posted to interface traveler.
Critical = Affecting Form, Fit or Function
(as found)

## Slide 4: QXFA254 – Length, Gaps
Coil length within spec.
(207 error in initial pole gap setting)

## Slide 5: QXFA254 - Reaction
Temperatures and dwell times all within spec.

## Slide 6: QXFA254 - Electrical
Final electrical checks – all passed

## Slide 7: QXFA254 - Electrical

## Slide 8: QXFA254 - DRs
Cable scratch details & photos on following slides

## Slide 9: 254 Cable Scratches
Fiberglass cable insulation damage and cable scratches noted during prep for reaction.
  Damage caused by razor blade when trimming fiberglass interlayer insulation after coil curing.
  2 locations, each area ~ 2.5” long:
    Inner layer coil midplane, transition side, 39” from NL end.
    Outer layer coil midplane, transition side, 90” from NL end.
  Inspection and photos before and after reaction.
    Inner layer – scratches in copper.
    Outer layer – scratches in copper, 4 small black spots observed under magnification after reaction.

## Slide 10: 254 Cable Scratches
  Before Reaction - Inner layer coil midplane, transition side, 39” from NL end:

## Slide 11: 254 Cable Scratches
  Before Reaction - Outer layer coil midplane, transition side, 90” from NL end:

## Slide 12: 254 Cable Scratches
  After Reaction - Inner layer coil midplane, transition side, 39” from NL end:

## Slide 13: 254 Cable Scratches
  After Reaction - Inner layer coil midplane, transition side, 39” from NL end:

## Slide 14: 254 Cable Scratches
  After Reaction - Outer layer coil midplane, transition side, 90” from NL end:

## Slide 15: 254 Cable Scratches
  After Reaction - Outer layer coil midplane, transition side, 90” from NL end:

## Slide 16: 254 Cable Scratches
  After Reaction - Outer layer coil midplane, transition side, 90” from NL end:
    4 small black spots observed along the scratch:

## Slide 17: 254 Cable Scratches
  After Reaction - Outer layer coil midplane, transition side, 90” from NL end:
    The 2 largest spots:

## Slide 18: 254 Cable Scratches
  Impression of the sample cable for measurement with confocal microscope.
Amazing Mold Putty (alumilite.com)
Alumilite silicone mold putty:

## Slide 19: 254 Cable Scratches
  Impression of the scratched area on coil 254 for measurement with confocal microscope.