## Slide 1: MQXF125 Midplane Repair
Fred Nobrega – CAM/L3 CAM/L3
MQXFAP20 Coil Acceptance Review
December 12, 2024

## Slide 2: Discrepancy 12166
Description
  After coil QXF125 impregnation and during epoxy flash removal, too much epoxy and fiberglass was filed exposing the corner of the cable.
Cause
  Improper use of file angle and pressure
Repair options
  Build up with Stycast then sand to shape
  Remove L2 midplane G11 insulation & replace with S2 glass, 2nd impregnation.
Details in following slides.

## Slide 3: QXFA125 Damaged Area
Exposed Cable
Lead End
Lead End
50 mm
Chamfer length = 90 mm

## Slide 4
\\tdserver1\project\HFM\LARP\QXF Coils\QXFA Coils\QXFA 125\DR Post Impregnation Filed Lead\QXFA125\Picture \A007 - 20201013_095629
4/64 = 0.0625” (1.588 mm)
1/64 = 0.016” (0.397 mm)
Lead End
Lead End

## Slide 5: QXFA125 CMM Scan
Midplane
Coil OD
COIL OD
0.145 mm cable insulation
0.100 mm trace
0.310 mm S2 glass
0.555 mm nominal thickness
Midplane
0.145 mm cable insulation
0.125 mm G11
0.270 mm nominal thickness

## Slide 6: Deformed Cable Strand
Quadruplet cable edge
(worst configuration for A125 damage)
Triplet cable edge
R1= 0.4 mm
R2= 0.45 mm

## Slide 7: Midplane Repair, Stycast
QXFA125 OD View
QXFA125
ID View
3D printed sanding tool