## Slide 1: QXFA121 Reacted Coil Lead Displacement
Fred Nobrega
Giorgio Ambrosio
Coil Working Group Meeting
February 12, 2020

## Slide 2: QXFA121 Prep for Impregnation
The mandrel block stuck to the base plate. During the removal process the technician bumped the tip of the L2 lead. The lead was displaced in the plane of the mid-plane shim.
DR11968 was written.

## Slide 3: Layer 2 Lead
No visible strand damage.

## Slide 4: Bending Strain Computations
Single wire bending strain | mm | inches | inches | inches
Radius after bending | 548.132 | 66.25 | 33.31 | 21.58
Strand Diameter | 0.85 | 0.715 | 0.715 | 0.715
Max Strain | 0.00078 | 0.00025 | 0.0005 | 0.00078
Strain due to bending of “soldered” cable |  |  |  |  | 
 | mm | inches | inches | inches | 
Radius before bending | infinite |  |  |  | 
Radius after bending | 548.132 | 66.25 | 33.31 | 21.58 | 
Cable width | 18.15 | 0.715 | 0.715 | 0.715 | 
Drop from horizontal | 19.8 mm | 1/4" | 1/2" | ~3/4" | 
Max strain | 0.0166 | 0.0054 | 0.0107 | 0.0166 | 
AUP criteria | 0.0005 |  |  |  | 
damage threshold | 0.0020 |  |  |  | 

## Slide 5: https://indico.fnal.gov/event/67067/contributions/303826/attachments/183787/252721/EDMS_2788659_february2023_third_attempt.pptx